## Slide 1: Results
Experimental investigation of temperatures and heat flows for orthogonal cutting 1045/4140 steel by thermal imaging

## Slide 2: Gliederung
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 3: Gliederung
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 4: Experimental Setup Design of Experiment
Thermal camera
Workpiece
Tool
Cutting process
Area covered by the thermal camera

## Slide 5: Experimental Setup Design of Experiment for AISI 1045
Experiments | Cutting Velocity [m/min] | Uncut chip thickness [µm] | Integration time [µs] | Cutting Force [N] | Passive Force [N] | Heat treatment
VP41_1_H200_V100_C45_MF_425 | 100 | 200 | 425 | 1500 | 1000 | Normalized
VP41_2_H200_V100_C45_MF_425 | 100 | 200 | 425 | 1565 | 1005 | Normalized
VP42_1_H300_V100_C45_MF_425 | 100 | 300 | 425 | 2250 | 1159 | Normalized
VP42_2_H300_V100_C45_MF_285 | 100 | 300 | 285 | 2136 | 1079 | Normalized
VP43_1_H400_V100_C45_MF_285 | 100 | 400 | 285 | 2716 | 1118 | Normalized
VP45_2_H200_V150_C45_MF_425 | 150 | 200 | 425 | 1448 | 688 | Normalized
VP46_1_H300_V150_C45_MF_285 | 150 | 300 | 285 | 2006 | 801 | Normalized
VP46_2_H300_V150_C45_MF_285 | 150 | 300 | 285 | 2004 | 875 | Normalized
VP49_1_H400_V150_C45_MF_285 | 150 | 400 | 285 | 2675 | 1046 | Normalized
VP49_2_H400_V150_C45_MF_285 | 150 | 400 | 285 | 2590 | 1000 | Normalized
VP50_1_H500_V150_C45_MF_285 | 150 | 500 | 285 | 3220 | 1120 | Normalized
VP50_2_H500_V150_C45_MF_285 | 150 | 500 | 285 | 3178 | 1162 | Normalized

## Slide 6: Experimental Setup Design of Experiment for AISI 4140 [1/2]
Experiments | Cutting Velocity [m/min] | Uncut chip thickness [µm] | Integration time [µs] | Cutting Force [N] | Passive Force [N] | Heat treatment
VP4_1_H300_V100_ACF_MF_285 | 100 | 300 | 285 | 1520 | 691 | Normalized
VP4_2_H300_V100_ACF_MF_285 | 100 | 300 | 285 | 1560 | 734 | Normalized
VP5_1_H200_V100_ACF_MF_285 | 100 | 200 | 285 | 1105 | 556 | Normalized
VP5_2_H200_V100_ACF_MF_285 | 100 | 200 | 285 | 1113 | 546 | Normalized
VP6_1_H100_V100_ACF_MF_285 | 100 | 100 | 285 | 619 | 361 | Normalized
VP32_1_H200_V150_ACF_MF_285 | 150 | 200 | 285 | 1133 | 519 | Normalized
VP32_2_H200_V150_ACF_MF_285 | 150 | 200 | 285 | 1054 | 496 | Normalized
VP33_1_H300_V150_ACF_MF_285 | 150 | 300 | 285 | 1495 | 538 | Normalized
VP36_1_H200_V100_ABA_MF_285 | 100 | 200 | 285 | 1302 | 400 | Tempered
VP36_2_H200_V100_ABA_MF_425 | 100 | 200 | 425 | 1242 | 436 | Tempered
VP36_3_H200_V100_ABA_MF_425 | 100 | 200 | 425 | 1295 | 410 | Tempered
VP37_1_H200_V150_ABA_MF_425 | 150 | 200 | 425 | 1225 | 373 | Tempered

## Slide 7: Experimental Setup Design of Experiment for AISI 4140 [2/2]
Experiments | Cutting Velocity [m/min] | Uncut chip thickness [µm] | Integration time [µs] | Cutting Force [N] | Passive Force [N] | Heat treatment
VP37_2_H200_V150_ABA_MF_425 | 150 | 200 | 425 | 1260 | 362 | Tempered
VP38_1_H300_V100_ABA_MF_425 | 100 | 300 | 425 | 1846 | 1574 | Tempered
VP38_2_H300_V100_ABA_MF_425 | 100 | 300 | 425 | 2028 | 1633 | Tempered
VP39_1_H300_V150_ABA_MF_425 | 150 | 300 | 425 | 1892 | 1576 | Tempered
VP39_2_H300_V150_ABA_MF_425 | 150 | 300 | 425 | 1936 | 1820 | Tempered

## Slide 8: Experimental Setup Boundary Conditions for AISI 1045
Inputs |  |  |  |  | 
Tool |  | Camera |  | Workpiece | 
Heat Conductivity [W/(mK)] | 75,4 | Pixel pitch (Infrared Camera) [mm/pixel] | 0,015 | Length of the workpiece [mm] | 200
Heat Capacity [J/(cm^3K)] | Interpolation* | Maximum digit level valid (FLIR X) | 8192 | Heat Capacity [J/(kgK)] | Interpolation**
Rake Angle [°] | 6 | Maximum digit level valid (FLIR SC7600) | 16000 | Workpiece Material | AISI 1045 (normalized)
Clearance Angle [°] | 3 | Frame Rate (Infrared Camera) [Hz] | 328 | Width [mm] | 3,5
Assumed percentage of heat conducted away by convection and radiation | 0,03 | Minimum valid temperature for the frames [°C] | 200 | Percentage of the deformation energy converted into heat | 0,9
Cutting edge radius [µm] | < 5 | Emissivity (Experimentally determined - tool and workpiece coated) | 0,85 | Density (based on steel) [kg/m^3] | 7874
*Tool [J/(cm^3K)] |  | 
**Workpiece [J/(kgK)] |  | 
Interpolation

## Slide 9: Experimental Setup Boundary Conditions for AISI 4140
Boundary Conditions |  |  |  |  | 
Tool |  | Camera |  | Workpiece | 
Heat Conductivity [W/(mK)] | 75,4 | Pixel pitch (Infrared Camera) [mm/pixel] | 0,015 | Length of the workpiece [mm] | 80
Heat Capacity [J/(cm^3K)] | Interpolation* | Maximum digit level valid (FLIR X) | 8192 | Heat Capacity [J/(kgK)] | Interpolation**
Rake Angle [°] | 6 | Maximum digit level valid (FLIR SC7600) | 16000 | Workpiece Material | AISI 4140 (normalized / tempered)
Clearance Angle [°] | 3 | Frame Rate (Infrared Camera) [Hz] | 328 | Depth of Cut ap [mm] | 2,8
Assumed percentage of heat conducted away by convection and radiation | 0,03 | Minimum valid temperature for the frames [°C] | 200 | Maximum error of the workpiece position for = 100 [mm/mm] | 0,064
Cutting edge radius [µm] | 66 | Emissivity (Experimentally determined - tool and workpiece coated) | 0,85 | Maximum error of the workpiece position for = 150 [mm/mm] | 0,095
 |  |  |  | Percentage of the deformation energy converted into heat | 0,9
 |  |  |  | Density (based on steel) [kg/m^3] | 7874
Boundary Conditions |  |  |  |  | 
Tool |  | Camera |  | Workpiece | 
Heat Conductivity [W/(mK)] | 75,4 | Pixel pitch (Infrared Camera) [mm/pixel] | 0,015 | Length of the workpiece [mm] | 80
Heat Capacity [J/(cm^3K)] | Interpolation* | Maximum digit level valid (FLIR X) | 8192 | Heat Capacity [J/(kgK)] | Interpolation**
Rake Angle [°] | 6 | Maximum digit level valid (FLIR SC7600) | 16000 | Workpiece Material | AISI 4140 (normalized / tempered)
Clearance Angle [°] | 3 | Frame Rate (Infrared Camera) [Hz] | 328 | Depth of Cut ap [mm] | 2,8
Assumed percentage of heat conducted away by convection and radiation | 0,03 | Minimum valid temperature for the frames [°C] | 200 |  | 0,064
Cutting edge radius [µm] | 66 | Emissivity (Experimentally determined - tool and workpiece coated) | 0,85 |  | 0,095
 |  |  |  | Percentage of the deformation energy converted into heat | 0,9
 |  |  |  | Density (based on steel) [kg/m^3] | 7874
*Tool [J/(cm^3K)] |  | 
**Workpiece [J/(kgK)] |  | 
Interpolation

## Slide 10: Gliederung
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 11: Post processing of thermal pictures Energy balance in the volume control
Tool
Workpiece
Control volume
Inside Energy
Total power produced
  Direct force measurement
Energy from material going inside the control volume
  Always zero ()
Outside Energy
Heat flow into the tool
  Calculation by gradient
Heat flow into the workpiece
  Calculation by heat balance
Energy from the chip going outside
  thermodynamic calculation
Part of deformation energy converted in heat
  90% of the total deformation energy ()
*,
Chip
Notes: In this analysis, the energy flows considered for the volume control are listed above. Then, with the temperature field of the Infrared camera frames, this analysis is able to calculate the heat flow through the tool and the chip and, consequently, the heat partition of the total power produced during the process. About 90% of the deformation energy is converted in heat and the heat flow through the workpiece is calculated by the total balance.

## Slide 12: Post processing of thermal pictures Heat carried away from the tool tip
The heat flow through the tool is calculated as a mean value between the heat flows calculated for the last two isothermals.
Method based on [BOOTHROYD].
  : heat conductivity
  : length of the isothermal
  : temperature gradient normal to line
  : effective tool width
Tool

## Slide 13: Post processing of thermal pictures Heat carried away by the chip
Tool
Chip
End of contact chip - tool
The heat flow is calculated on the end of contact between chip and tool interfaces
Method based on [BOOTHROYD].
  : heat capacity function
  : chip temperature
  : environment temperature
  : velocity of the chip
  : chip thickness
  : chip width

## Slide 14: Gliederung
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Influence of uncut chip thickness and cutting velocity
3.2
Time and spatial varying thermal properties
3.1
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 15: Time and spatial varying thermal properties Temperature at tool tip [°C] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 323.5206 | 271.9162 | 380.5434 | 341.2377 | 357.2232 | 368.2788 | 230.1309 | 364.6832 | 365.8805 | 343.2452 | 364.6607 | 379.6024 | 393.9241 | 390.0437 | 373.423 | 398.9011 | 411.4206 | 425.8531
VP42_1_H300_V100_C45_MF_425 | 442.907 | 491.0974 | 498.6279 | 450.6018 | 444.4791 | 340.6401 | 471.2703 | 433.7598 | 426.1506 | 282.3214 | 323.3509 | 255.7746 | 504.0463 | 485.6611 | 516.0332 | 517.7154 | 520.8733 | 525.9864
VP43_1_H400_V100_C45_MF_285 | 475.9792 | 406.8634 | 496.2303 | 444.492 | 421.7696 | 195.0595
VP45_2_H200_V150_C45_MF_425 | 363.7171 | 378.5227 | 387.0074 | 395.5219 | 410.6586 | 412.4561 | 402.5545 | 408.8741 | 411.6293 | 408.0815 | 415.8895 | 415.7033 | 420.948 | 444.6016 | 447.3969 | 461.0162 | 447.4671 | 441.2219
VP46_1_H300_V150_C45_MF_285 | 425.3031 | 385.6967 | 416.9808 | 388.6194 | 419.6816 | 428.1679 | 436.2967 | 452.2375 | 437.1667 | 384.2404 | 438.4321 | 320.4099 | 442.1594 | 492.6639 | 486.9684 | 492.3859 | 488.9218 | 505.5068
VP49_1_H400_V150_C45_MF_285 | 414.4026 | 414.7684 | 441.6356 | 253.9839 | 421.9092 | 485.0291 | 476.3299 | 470.3219 | 416.562 | 469.1423 | 474.6055 | 474.9649 | 493.8176 | 495.579 | 514.8465 | 506.6511 | 489.6865 | 469.3475
VP50_1_H500_V150_C45_MF_285 | 412.4521 | 377.9897 | 447.9103 | 416.5194 | 457.2466 | 439.4002 | 506.3999 | 468.2151 | 457.8948 | 424.7005 | 430.3532 | 477.8122 | 511.4966 | 514.4709 | 502.4442 | 486.0228 | 490.5698 | 473.5951

## Slide 16: Time and spatial varying thermal properties Internal energy in tool [Joule] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 6.5224 | 6.7965 | 7.0719 | 7.3539 | 7.8868 | 8.1574 | 7.964 | 8.4782 | 8.7992 | 9.1514 | 9.4147 | 9.5462 | 9.7156 | 9.9526 | 9.8572 | 10.3038 | 10.4344 | 10.4692
VP42_1_H300_V100_C45_MF_425 | 8.6795 | 8.9284 | 9.2325 | 9.6003 | 10.0522 | 10.2113 | 10.5446 | 10.7162 | 10.8376 | 10.3466 | 10.6856 | 11.1312 | 11.4614 | 11.5732 | 12.7034 | 12.9454 | 13.1586 | 13.3152
VP43_1_H400_V100_C45_MF_285 | 9.7584 | 9.8709 | 10.4491 | 10.8884 | 11.2608 | 10.6312
VP45_2_H200_V150_C45_MF_425 | 1.5376 | 1.7419 | 1.9444 | 2.1819 | 2.4671 | 2.7856 | 3.1359 | 3.5036 | 3.8728 | 4.1878 | 4.4347 | 4.6127 | 4.8247 | 5.0665 | 5.3337 | 5.7504 | 6.1824 | 6.4363
VP46_1_H300_V150_C45_MF_285 | 2.5631 | 2.8266 | 3.1545 | 3.4264 | 3.8378 | 4.3676 | 4.87 | 5.4523 | 5.947 | 6.3015 | 6.4102 | 6.6173 | 6.1817 | 7.25 | 7.6531 | 8.1454 | 8.6188 | 8.84
VP49_1_H400_V150_C45_MF_285 | 5.0798 | 5.5896 | 6.1222 | 6.2829 | 6.9385 | 7.5386 | 8.1279 | 8.7742 | 9.371 | 9.8999 | 10.1846 | 10.3374 | 10.5043 | 10.7092 | 11.0906 | 11.6349 | 12.2059 | 12.4869
VP50_1_H500_V150_C45_MF_285 | 6.23 | 6.8538 | 7.3979 | 7.8002 | 8.2048 | 8.7882 | 9.527 | 10.2283 | 11.0142 | 11.6462 | 12.0316 | 12.2152 | 12.3571 | 12.5159 | 12.8927 | 13.4692 | 14.2166 | 14.6323
Notes: The higher the chip thickness the higher the internal energy/heat rate
The lower the cutting speed the higher the internal energy in the tool  High Speed cutting

## Slide 17: Time and spatial varying thermal properties Internal energy rate of the tool [W] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214
VP42_1_H300_V100_C45_MF_425 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583
VP43_1_H400_V100_C45_MF_285 | 134 | 134 | 134 | 134 | 134
VP45_2_H200_V150_C45_MF_425 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588
VP46_1_H300_V150_C45_MF_285 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663
VP49_1_H400_V150_C45_MF_285 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717
VP50_1_H500_V150_C45_MF_285 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325
Notes: Heating rate rises with chip thickness
Heating rate decreases with cutting speed
H/v  Heating rate
1,33
2
4
2
3
2,66
3,333

## Slide 18: Time and spatial varying thermal properties Internal energy carried away by chip [W] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 1446.9037 | 1500.714 | 1451.366 | 1450.7175 | 1523.3013 | 1526.934 | 1392.793 | 1493.1362 | 1594.0554 | 1427.9538 | 1554.7901 | 1602.5165 | 1624.0372 | 1635.069 | 1589.2306 | 1724.2013 | 1825.9456 | 1704.9593
VP42_1_H300_V100_C45_MF_425 | 2227.4118 | 2165.4074 | 2208.0209 | 2199.885 | 2261.3844 | 2203.7899 | 2195.2405 | 2222.4003 | 2237.2376 | 2244.5721 | 2246.1977 | 2273.3784 | 2258.7944 | 2343.3527 | 2365.7067 | 2380.7834 | 2543.5444 | 2526.242
VP43_1_H400_V100_C45_MF_285 | 2660.3012 | 2674.8095 | 2734.291 | 2713.5039 | 2756.6819 | 2772.8196
VP45_2_H200_V150_C45_MF_425 | 2211.1666 | 2131.5983 | 2135.074 | 2141.749 | 2208.7243 | 2215.9191 | 2195.4285 | 2209.5729 | 2208.4354 | 2167.633 | 2166.4547 | 2117.3798 | 2194.5496 | 2264.3116 | 2267.3972 | 2317.1508 | 2414.638 | 2425.7515
VP46_1_H300_V150_C45_MF_285 | 3086.5735 | 3075.8261 | 3108.6092 | 3077.5016 | 3148.4235 | 3128.8205 | 3066.2035 | 3055.4101 | 3081.729 | 3082.416 | 3094.5335 | 3131.2069 | 3135.8375 | 3145.0925 | 3184.8716 | 3226.8478 | 3394.0747 | 3375.8082
VP49_1_H400_V150_C45_MF_285 | 3703.6478 | 3636.3396 | 3744.3018 | 3768.0535 | 3889.5999 | 4034.6229 | 3975.9522 | 4006.6247 | 3828.9325 | 3860.761 | 3944.7605 | 3892.4492 | 3953.3381 | 3900.7334 | 3935.8881 | 3961.3381 | 4063.606 | 4015.3245
VP50_1_H500_V150_C45_MF_285 | 4552.4075 | 4621.685 | 4751.0572 | 4866.2372 | 5104.8332 | 5095.3821 | 5000.6533 | 4892.1433 | 4847.5272 | 4814.495 | 4792.0381 | 4843.6789 | 4845.0776 | 4887.454 | 5004.1952 | 5045.1906 | 5110.3196 | 4981.0634
Notes: Heat carried away by chip rises with hsp*vc
Heat carried away by chip increases with cutting length for small chip thickness
Why?????
vc* hsp ~ chip ; lc ↑ → chip = const. (gilt nicht für Vp41 , VP42)
chip ↑ → Bchip ↑ (für Vp41 , VP42)
vc* hsp ~ ( 𝒒) ̇^´chip ; lc ↑ → ( 𝒒) ̇^´chip = const. (gilt nicht für Vp41 , VP42)
( 𝒒) ̇^´chip ↑ → Bchip ↑ (für Vp41 , VP42)

## Slide 19: Time and spatial varying thermal properties Heat partition to the chip for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 0.60694 | 0.62951 | 0.60676 | 0.60854 | 0.63899 | 0.63612 | 0.57706 | 0.62093 | 0.66525 | 0.59274 | 0.64887 | 0.66995 | 0.68124 | 0.68587 | 0.66664 | 0.72446 | 0.76721 | 0.71637
VP42_1_H300_V100_C45_MF_425 | 0.64915 | 0.63576 | 0.65008 | 0.64768 | 0.66579 | 0.64883 | 0.64075 | 0.65156 | 0.651 | 0.65515 | 0.6604 | 0.66746 | 0.6593 | 0.68398 | 0.69456 | 0.69385 | 0.74128 | 0.74377
VP43_1_H400_V100_C45_MF_285 | 0.64724 | 0.65635 | 0.66524 | 0.66103 | 0.67155 | 0.6804
VP45_2_H200_V150_C45_MF_425 | 0.67329 | 0.65163 | 0.6527 | 0.65474 | 0.67163 | 0.67741 | 0.6685 | 0.66906 | 0.66967 | 0.65823 | 0.65878 | 0.64473 | 0.66823 | 0.68563 | 0.68656 | 0.7006 | 0.7372 | 0.74156
VP46_1_H300_V150_C45_MF_285 | 0.68413 | 0.68175 | 0.68902 | 0.67814 | 0.69377 | 0.68774 | 0.67482 | 0.67723 | 0.67652 | 0.68321 | 0.68433 | 0.69244 | 0.69505 | 0.69551 | 0.70006 | 0.71522 | 0.7479 | 0.74824
VP49_1_H400_V150_C45_MF_285 | 0.61522 | 0.59901 | 0.61758 | 0.62149 | 0.64463 | 0.66867 | 0.65894 | 0.66084 | 0.63231 | 0.63757 | 0.64982 | 0.6428 | 0.65742 | 0.64795 | 0.65305 | 0.65652 | 0.67024 | 0.66469
VP50_1_H500_V150_C45_MF_285 | 0.6265 | 0.63812 | 0.65803 | 0.67398 | 0.70702 | 0.70043 | 0.68971 | 0.67757 | 0.67139 | 0.66681 | 0.65798 | 0.66806 | 0.66678 | 0.67553 | 0.69019 | 0.69354 | 0.70406 | 0.68549
Notes: No influence of level of heat partition inside the chip by chip thickness
Rising heat partition inside the chip, especially for lower chip thickness  Hypo: tool is heating up and is conducts less heat away
Hypo: The lower the chip thickness the lower the influence of friction at the rake face
1 = Bchip + Btool + BWP
Btool = konst. ; Bchip ↑ → BWP ↓

## Slide 20: Time and spatial varying thermal properties Heat flow into the tool [W] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 602.102 | 615.3419 | 568.4783 | 554.1279 | 539.9916 | 526.5104 | 530.2351 | 500.7551 | 488.2428 | 500.5791 | 498.1336 | 496.6459 | 491.6364 | 481.0465 | 474.3701 | 475.4144 | 477.9226 | 490.1465
VP42_1_H300_V100_C45_MF_425 | 564.7501 | 568.4098 | 558.5991 | 556.8689 | 558.8854 | 546.4127 | 540.5213 | 528.6276 | 527.6142 | 567.2462 | 611.3753 | 546.6174 | 541.9427 | 491.1245 | 501.469 | 477.8016 | 475.726 | 445.5474
VP43_1_H400_V100_C45_MF_285 | 547.0138 | 336.4551 | 624.8956 | 551.3233 | 518.1474
VP45_2_H200_V150_C45_MF_425 | 702.7248 | 724.5544 | 726.2465 | 702.3922 | 731.6837 | 716.9092 | 718.2641 | 704.6531 | 694.8251 | 676.254 | 653.4898 | 642.9929 | 623.8868 | 603.5658 | 590.8439 | 576.7407 | 566.9826 | 417.9774
VP46_1_H300_V150_C45_MF_285 | 1030.1126 | 1041.1344 | 1016.5965 | 1021.8164 | 969.6198 | 924.2656 | 892.7249 | 890.7576 | 867.1375 | 836.3842 | 782.5403 | 749.4627 | 777.7226 | 751.9924 | 700.299 | 733.3886 | 698.8831 | 628.8686
VP49_1_H400_V150_C45_MF_285 | 1033.2187 | 1021.4917 | 1016.1496 | 976.9083 | 909.3068 | 886.1217 | 863.6786 | 860.3197 | 868.0137 | 862.1206 | 833.7533 | 824.1827 | 830.4098 | 806.4759 | 785.1121 | 772.4722 | 754.216 | 609.7427
VP50_1_H500_V150_C45_MF_285 | 1152.0342 | 1099.9662 | 1046.0801 | 1015.1071 | 985.5852 | 964.9986 | 941.3677 | 918.9017 | 918.3261 | 921.5727 | 891.982 | 870.1249 | 848.7689 | 823.323 | 793.0764 | 774.5049 | 765.2386 | 555.4084

## Slide 21: Time and spatial varying thermal properties Heat flow into the tool [W] for different vc and hsp 2
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_1_H200_V100_C45_MF_425 | 630.7384 | 639.527 | 613.6531 | 611.6321 | 618.6951 | 577.82 | 561.5337 | 554.39 | 558.917 | 546.616 | 541.513 | 534.4577 | 528.4082 | 510.1898 | 515.0817 | 499.3092 | 493.6822 | 529.9883
VP41_2_H200_V100_C45_MF_425 | 602.102 | 615.3419 | 568.4783 | 554.1279 | 539.9916 | 526.5104 | 530.2351 | 500.7551 | 488.2428 | 500.5791 | 498.1336 | 496.6459 | 491.6364 | 481.0465 | 474.3701 | 475.4144 | 477.9226 | 490.1465
VP42_1_H300_V100_C45_MF_425 | 564.7501 | 568.4098 | 558.5991 | 556.8689 | 558.8854 | 546.4127 | 540.5213 | 528.6276 | 527.6142 | 567.2462 | 611.3753 | 546.6174 | 541.9427 | 491.1245 | 501.469 | 477.8016 | 475.726 | 445.5474
VP43_1_H400_V100_C45_MF_285 | 547.0138 | 336.4551 | 624.8956 | 551.3233 | 518.1474
VP45_2_H200_V150_C45_MF_425 | 702.7248 | 724.5544 | 726.2465 | 702.3922 | 731.6837 | 716.9092 | 718.2641 | 704.6531 | 694.8251 | 676.254 | 653.4898 | 642.9929 | 623.8868 | 603.5658 | 590.8439 | 576.7407 | 566.9826 | 417.9774
VP46_1_H300_V150_C45_MF_285 | 1030.1126 | 1041.1344 | 1016.5965 | 1021.8164 | 969.6198 | 924.2656 | 892.7249 | 890.7576 | 867.1375 | 836.3842 | 782.5403 | 749.4627 | 777.7226 | 751.9924 | 700.299 | 733.3886 | 698.8831 | 628.8686
VP46_2_H300_V150_C45_MF_285 | 1051.5497 | 1043.7934 | 1081.1728 | 1060.0878 | 979.2914 | 957.1255 | 899.0267 | 880.2931 | 874.9413 | 860.8147 | 821.8786 | 792.4546 | 778.2683 | 758.9629 | 734.5505 | 719.4085 | 725.8784 | 603.0034
VP49_1_H400_V150_C45_MF_285 | 1033.2187 | 1021.4917 | 1016.1496 | 976.9083 | 909.3068 | 886.1217 | 863.6786 | 860.3197 | 868.0137 | 862.1206 | 833.7533 | 824.1827 | 830.4098 | 806.4759 | 785.1121 | 772.4722 | 754.216 | 609.7427
VP49_2_H400_V150_C45_MF_285 | 974.296 | 1034.734 | 988.4383 | 937.1056 | 902.2009 | 880.8273 | 855.6692 | 854.155 | 839.5339 | 812.8372 | 822.659 | 812.4342 | 792.2629 | 778.8118 | 753.3403 | 731.5271 | 755.3802 | 586.4244
VP50_1_H500_V150_C45_MF_285 | 1152.0342 | 1099.9662 | 1046.0801 | 1015.1071 | 985.5852 | 964.9986 | 941.3677 | 918.9017 | 918.3261 | 921.5727 | 891.982 | 870.1249 | 848.7689 | 823.323 | 793.0764 | 774.5049 | 765.2386 | 555.4084
VP50_2_H500_V150_C45_MF_285 | 1134.4763 | 1117.3896 | 1057.0297 | 1026.7027 | 984.8355 | 958.5802 | 955.3913 | 930.8623 | 911.478 | 942.3928 | 910.105 | 881.2064 | 848.3989 | 823.1871 | 802.1761 | 795.7454 | 779.5438 | 548.4773
Notes: For small chip thickness no influence of cutting speed
Heat flux into the tool rises with chip thickness decreasingly,
Less rise for smaller cutting speeds
Decreases for higher chip thickness over time constant for small chip thickness hypo: tool gets to hot to carry heat away
Hypo: The higher the chip thickness the higher the frictional influence
Thermal number? Vc *hsp??

## Slide 22: Time and spatial varying thermal properties Heat partition into the tool for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 0.25257 | 0.25812 | 0.23766 | 0.23244 | 0.22651 | 0.21934 | 0.21969 | 0.20824 | 0.20376 | 0.20779 | 0.20789 | 0.20763 | 0.20623 | 0.20179 | 0.19899 | 0.19975 | 0.20081 | 0.20594
VP42_1_H300_V100_C45_MF_425 | 0.16459 | 0.16688 | 0.16446 | 0.16395 | 0.16455 | 0.16087 | 0.15777 | 0.15498 | 0.15353 | 0.16557 | 0.17975 | 0.16048 | 0.15818 | 0.14335 | 0.14723 | 0.13925 | 0.13864 | 0.13118
VP43_1_H400_V100_C45_MF_285 | 0.16569 | 0.11544 | 0.18464 | 0.16695 | 0.15887
VP45_2_H200_V150_C45_MF_425 | 0.21398 | 0.2215 | 0.22201 | 0.21472 | 0.22249 | 0.21916 | 0.21871 | 0.21337 | 0.21069 | 0.20535 | 0.19871 | 0.19579 | 0.18997 | 0.18276 | 0.17891 | 0.17438 | 0.1731 | 0.12778
VP46_1_H300_V150_C45_MF_285 | 0.22832 | 0.23077 | 0.22533 | 0.22516 | 0.21366 | 0.20316 | 0.19647 | 0.19743 | 0.19036 | 0.18538 | 0.17305 | 0.16574 | 0.17238 | 0.1663 | 0.15393 | 0.16255 | 0.154 | 0.13939
VP49_1_H400_V150_C45_MF_285 | 0.17163 | 0.16827 | 0.1676 | 0.16113 | 0.1507 | 0.14686 | 0.14314 | 0.1419 | 0.14334 | 0.14237 | 0.13734 | 0.13611 | 0.13809 | 0.13396 | 0.13027 | 0.12802 | 0.1244 | 0.10094
VP50_1_H500_V150_C45_MF_285 | 0.15854 | 0.15187 | 0.14488 | 0.14059 | 0.1365 | 0.13265 | 0.12984 | 0.12727 | 0.12719 | 0.12764 | 0.12247 | 0.12001 | 0.11681 | 0.1138 | 0.10938 | 0.10647 | 0.10543 | 0.076435
Notes: Heat partition inside tool higher for low cutting speed  Puls
No influence of chip thickness  Puls
Remains constant over time

## Slide 23: Time and spatial varying thermal properties Heat flow into the workpiece [W] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 334.9241 | 267.874 | 372.1673 | 379.0844 | 320.637 | 346.9419 | 490.553 | 410.8037 | 313.8619 | 480.5586 | 343.2364 | 292.8493 | 268.2562 | 267.8144 | 320.3292 | 180.3724 | 76.1199 | 184.8823
VP42_1_H300_V100_C45_MF_425 | 639.1159 | 672.2175 | 629.9304 | 639.7965 | 576.2806 | 646.3478 | 690.2699 | 659.8696 | 671.7833 | 614.2135 | 543.6809 | 586.0388 | 625.2947 | 591.5546 | 538.8589 | 572.6928 | 412.0075 | 424.761
VP43_1_H400_V100_C45_MF_285 | 902.8935 | 1064.0178 | 751.0218 | 840.1052 | 830.1032
VP45_2_H200_V150_C45_MF_425 | 370.2289 | 415.0105 | 409.8426 | 427.0219 | 348.1828 | 338.3349 | 370.4276 | 388.3001 | 394.5278 | 449.258 | 468.6462 | 523.7475 | 465.6839 | 434.6487 | 444.2851 | 413.4729 | 293.7905 | 427.4342
VP46_1_H300_V150_C45_MF_285 | 394.9693 | 394.6948 | 386.4496 | 438.81 | 420.0847 | 496.3395 | 584.7915 | 565.4876 | 606.3858 | 592.8551 | 644.8967 | 641.3009 | 598.0952 | 624.8856 | 664.255 | 551.4188 | 445.1702 | 506.9785
VP49_1_H400_V150_C45_MF_285 | 1283.212 | 1412.7203 | 1302.4576 | 1317.9473 | 1234.9287 | 1113.0908 | 1194.2046 | 1195.9647 | 1358.4791 | 1332.5437 | 1292.0377 | 1338.7934 | 1229.6206 | 1312.8691 | 1305.8981 | 1300.0251 | 1245.0871 | 1415.8298
VP50_1_H500_V150_C45_MF_285 | 1561.9353 | 1521.0002 | 1423.0227 | 1338.8156 | 1129.7415 | 1214.2203 | 1308.3904 | 1409.1149 | 1454.3067 | 1484.0923 | 1598.9794 | 1536.6077 | 1572.5305 | 1524.2512 | 1453.1399 | 1454.9055 | 1382.7588 | 1729.9051
Notes: Heat flux inside work piece decreases with cutting speed and chip thickness
Heat flux into workpiece decreases over cutting length for small chip thickness
How over time?
How is this possible?

## Slide 24: Time and spatial varying thermal properties Heat partition into the workpiece for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 0.14049 | 0.11237 | 0.15559 | 0.15902 | 0.1345 | 0.14454 | 0.20325 | 0.17083 | 0.13099 | 0.19948 | 0.14324 | 0.12243 | 0.11253 | 0.11234 | 0.13437 | 0.075787 | 0.031983 | 0.077682
VP42_1_H300_V100_C45_MF_425 | 0.18626 | 0.19736 | 0.18546 | 0.18837 | 0.16967 | 0.1903 | 0.20148 | 0.19346 | 0.19548 | 0.17928 | 0.15985 | 0.17206 | 0.18251 | 0.17266 | 0.15821 | 0.1669 | 0.12007 | 0.12506
VP43_1_H400_V100_C45_MF_285 | 0.21967 | 0.26109 | 0.18272 | 0.20466 | 0.20222
VP45_2_H200_V150_C45_MF_425 | 0.11273 | 0.12687 | 0.12529 | 0.13054 | 0.10588 | 0.10343 | 0.11279 | 0.11758 | 0.11963 | 0.13642 | 0.14251 | 0.15948 | 0.1418 | 0.13161 | 0.13453 | 0.12502 | 0.089696 | 0.13067
VP46_1_H300_V150_C45_MF_285 | 0.087544 | 0.087483 | 0.085656 | 0.096694 | 0.092568 | 0.1091 | 0.1287 | 0.12534 | 0.13312 | 0.13141 | 0.14261 | 0.14182 | 0.13257 | 0.13819 | 0.14601 | 0.12222 | 0.098096 | 0.11237
VP49_1_H400_V150_C45_MF_285 | 0.21316 | 0.23272 | 0.21482 | 0.21738 | 0.20467 | 0.18447 | 0.19792 | 0.19726 | 0.22434 | 0.22006 | 0.21284 | 0.22109 | 0.20448 | 0.21808 | 0.21668 | 0.21546 | 0.20536 | 0.23437
VP50_1_H500_V150_C45_MF_285 | 0.21495 | 0.21001 | 0.19709 | 0.18543 | 0.15647 | 0.16691 | 0.18046 | 0.19516 | 0.20142 | 0.20555 | 0.21955 | 0.21193 | 0.21641 | 0.21068 | 0.20042 | 0.2 | 0.19051 | 0.23807
Notes: Heat partition into workpiece independent from vc and hsp does not fit to K&H
Decreases for small chip thickness

## Slide 25: Time and spatial varying thermal properties Friction coefficient µ for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136
VP42_1_H300_V100_C45_MF_425 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572
VP43_1_H400_V100_C45_MF_285 | 0.54011 | 0.54011 | 0.54011 | 0.54011 | 0.54011 | 0.54011
VP45_2_H200_V150_C45_MF_425 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074
VP46_1_H300_V150_C45_MF_285 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265
VP49_1_H400_V150_C45_MF_285 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174
VP50_1_H500_V150_C45_MF_285 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012

## Slide 26: Time and spatial varying thermal properties Heat partition ratios for hsp = 200 µm, vc = 100 m/min
Chart: Workpiece position [mm]
| 113,62 | 118,70 | 123,78 | 128,86 | 133,94 | 139,02 | 144,11 | 149,19 | 154,27 | 159,35 | 164,43 | 169,51 | 174,59 | 179,67 | 184,76 | 189,84 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 - Summe von Percent - Heat inside tool/Total heat | 0.21913 | 0.22468 | 0.20433 | 0.199 | 0.19307 | 0.18613 | 0.18666 | 0.17509 | 0.17049 | 0.1747 | 0.17462 | 0.1743 | 0.17279 | 0.16835 | 0.16555 | 0.16626 | 0.16731 | 0.17245
VP41_2_H200_V100_C45_MF_425 - Summe von Percent - Heat through chip/Total heat | 0.60694 | 0.62951 | 0.60676 | 0.60854 | 0.63899 | 0.63612 | 0.57706 | 0.62093 | 0.66525 | 0.59274 | 0.64887 | 0.66995 | 0.68124 | 0.68587 | 0.66664 | 0.72446 | 0.76721 | 0.71637
VP41_2_H200_V100_C45_MF_425 - Summe von Percent - Heat through workpiece/Total heat | 0.14049 | 0.11237 | 0.15559 | 0.15902 | 0.1345 | 0.14454 | 0.20325 | 0.17083 | 0.13099 | 0.19948 | 0.14324 | 0.12243 | 0.11253 | 0.11234 | 0.13437 | 0.075787 | 0.031983 | 0.077682
Work piece
Tool
Chip

## Slide 27: Temperature distribution for orthogonal cutting Temperature distribution for hsp = 200 µm, vc = 100 m/min
Chart: 
| 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 20.1655 | 233.9058 | 323.6939 | 226.8855 | 302.6419 | 295.3236 | 312.5295 | 395.5563 | 472.6004
Chart: 
| 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 9.1003 | 139.5096 | 217.2265 | 342.4747 | 220.7361 | 385.738 | 453.9045 | 581.5819
Workpiece position : 124 mm
Workpiece position : 200 mm
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
[°C]
[W]
[°C]

## Slide 28: Time and spatial varying thermal properties Heat partition ratios for hsp = 200 µm, vc = 150 m/min
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 116,16 | 123,78 | 131,40 | 139,02 | 146,65 | 154,27 | 161,89 | 169,51 | 177,13 | 184,76 | 192,38 | 200,00
VP45_2_H200_V150_C45_MF_425 - Summe von Percent - Heat inside tool/Total heat | 0.21398 | 0.2215 | 0.22201 | 0.21472 | 0.22249 | 0.21916 | 0.21871 | 0.21337 | 0.21069 | 0.20535 | 0.19871 | 0.19579 | 0.18997 | 0.18276 | 0.17891 | 0.17438 | 0.1731 | 0.12778
VP45_2_H200_V150_C45_MF_425 - Summe von Percent - Heat through chip/Total heat | 0.67329 | 0.65163 | 0.6527 | 0.65474 | 0.67163 | 0.67741 | 0.6685 | 0.66906 | 0.66967 | 0.65823 | 0.65878 | 0.64473 | 0.66823 | 0.68563 | 0.68656 | 0.7006 | 0.7372 | 0.74156
VP45_2_H200_V150_C45_MF_425 - Summe von Percent - Heat through workpiece/Total heat | 0.11273 | 0.12687 | 0.12529 | 0.13054 | 0.10588 | 0.10343 | 0.11279 | 0.11758 | 0.11963 | 0.13642 | 0.14251 | 0.15948 | 0.1418 | 0.13161 | 0.13453 | 0.12502 | 0.089696 | 0.13067
Work piece
Tool
Chip

## Slide 29
Time and spatial varying thermal properties Temperature distribution for hsp = 200 µm, vc = 150 m/min
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
[°C]
[W]
Chart: 
| 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 203.3038 | 323.357 | 360.8375 | 407.538 | 511.4623 | 703.7264
Chart: 
| 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 208.0108 | 282.9195 | 182.1045 | 160.2704 | 184.049 | 263.4118 | 378.4255
Workpiece position : 124 mm
Workpiece position : 200 mm
[°C]
Notes: With higher cutting speed and lower chip thickness more heat is transferred over tip

## Slide 30: Time and spatial varying thermal properties Heat partition ratios for hsp = 300 µm, vc = 100 m/min
Chart: Workpiece position [mm]
| 113,62 | 118,70 | 123,78 | 128,86 | 133,94 | 139,02 | 144,11 | 149,19 | 154,27 | 159,35 | 164,43 | 169,51 | 174,59 | 179,67 | 184,76 | 189,84 | 194,92 | 200,00
VP42_1_H300_V100_C45_MF_425 - Summe von Percent - Heat inside tool/Total heat | 0.16459 | 0.16688 | 0.16446 | 0.16395 | 0.16455 | 0.16087 | 0.15777 | 0.15498 | 0.15353 | 0.16557 | 0.17975 | 0.16048 | 0.15818 | 0.14335 | 0.14723 | 0.13925 | 0.13864 | 0.13118
VP42_1_H300_V100_C45_MF_425 - Summe von Percent - Heat through chip/Total heat | 0.64915 | 0.63576 | 0.65008 | 0.64768 | 0.66579 | 0.64883 | 0.64075 | 0.65156 | 0.651 | 0.65515 | 0.6604 | 0.66746 | 0.6593 | 0.68398 | 0.69456 | 0.69385 | 0.74128 | 0.74377
VP42_1_H300_V100_C45_MF_425 - Summe von Percent - Heat through workpiece/Total heat | 0.18626 | 0.19736 | 0.18546 | 0.18837 | 0.16967 | 0.1903 | 0.20148 | 0.19346 | 0.19548 | 0.17928 | 0.15985 | 0.17206 | 0.18251 | 0.17266 | 0.15821 | 0.1669 | 0.12007 | 0.12506
Tool
Work piece
Chip

## Slide 31
Time and spatial varying thermal properties Temperature distribution for hsp = 300 µm, vc = 100 m/min
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
[°C]
[W]
Chart: 
| 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 76.8222 | 100.5985 | 97.966 | 177.9767 | 275.9327 | 295.056 | 338.89 | 408.5537 | 536.928
Chart: 
| 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 61.0974 | 88.2377 | 126.5558 | 197.9065 | 238.4206 | 238.8037 | 309.4507 | 352.8802 | 366.4979
Workpiece position : 124 mm
Workpiece position : 200 mm
[°C]

## Slide 32: Time and spatial varying thermal properties Heat partition ratios for hsp = 300 µm, vc = 150 m/min
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 116,16 | 123,78 | 131,40 | 139,02 | 146,65 | 154,27 | 161,89 | 169,51 | 177,13 | 184,76 | 192,38 | 200,00
VP46_1_H300_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.22832 | 0.23077 | 0.22533 | 0.22516 | 0.21366 | 0.20316 | 0.19647 | 0.19743 | 0.19036 | 0.18538 | 0.17305 | 0.16574 | 0.17238 | 0.1663 | 0.15393 | 0.16255 | 0.154 | 0.13939
VP46_1_H300_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.68413 | 0.68175 | 0.68902 | 0.67814 | 0.69377 | 0.68774 | 0.67482 | 0.67723 | 0.67652 | 0.68321 | 0.68433 | 0.69244 | 0.69505 | 0.69551 | 0.70006 | 0.71522 | 0.7479 | 0.74824
VP46_1_H300_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.087544 | 0.087483 | 0.085656 | 0.096694 | 0.092568 | 0.1091 | 0.1287 | 0.12534 | 0.13312 | 0.13141 | 0.14261 | 0.14182 | 0.13257 | 0.13819 | 0.14601 | 0.12222 | 0.098096 | 0.11237
VP46_2_H300_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.2328 | 0.23108 | 0.2369 | 0.2326 | 0.2168 | 0.21001 | 0.19804 | 0.19367 | 0.19298 | 0.18938 | 0.18195 | 0.17522 | 0.17053 | 0.16653 | 0.16262 | 0.15907 | 0.1607 | 0.13231
VP46_2_H300_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.69408 | 0.6853 | 0.67724 | 0.68756 | 0.69731 | 0.68802 | 0.6971 | 0.6837 | 0.68455 | 0.69855 | 0.68372 | 0.69243 | 0.69087 | 0.69032 | 0.70817 | 0.70888 | 0.74403 | 0.76151
VP46_2_H300_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.073127 | 0.08362 | 0.085861 | 0.079838 | 0.085895 | 0.10197 | 0.10486 | 0.12263 | 0.12246 | 0.11207 | 0.13433 | 0.13235 | 0.1386 | 0.14315 | 0.12921 | 0.13204 | 0.095271 | 0.10619
Work piece
Tool
Chip

## Slide 33
Time and spatial varying thermal properties Temperature distribution for hsp = 300 µm, vc = 150 m/min
Chart: 
| 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 31.9529 | 186.5284 | 236.7895 | 325.124 | 417.3095 | 509.687 | 657.2823 | 876.3003
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
[°C]
[W]
Chart: 
| 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 19.7059 | 178.4143 | 169.0574 | 179.0231 | 263.8184 | 339.1859 | 352.3603 | 446.9513 | 562.8532
Workpiece position : 124 mm
Workpiece position : 200 mm
[°C]

## Slide 34: Time and spatial varying thermal properties Heat partition ratios for hsp = 400 µm, vc = 100 m/min
Chart: Workpiece position [mm]
| 113,62 | 118,70 | 123,78 | 128,86 | 133,94
Summe von Percent - Heat inside tool/Total heat | 0.16569 | 0.11544 | 0.18464 | 0.16695 | 0.15887
Summe von Percent - Heat through chip/Total heat | 0.64724 | 0.65635 | 0.66524 | 0.66103 | 0.67155
Summe von Percent - Heat through workpiece/Total heat | 0.18707 | 0.22821 | 0.15012 | 0.17201 | 0.16958
Tool
Work piece
Chip

## Slide 35: Time and spatial varying thermal properties Heat partition ratios for hsp = 400 µm, vc = 150 m/min
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 116,16 | 123,78 | 131,40 | 139,02 | 146,65 | 154,27 | 161,89 | 169,51 | 177,13 | 184,76 | 192,38 | 200,00
VP49_1_H400_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.17163 | 0.16827 | 0.1676 | 0.16113 | 0.1507 | 0.14686 | 0.14314 | 0.1419 | 0.14334 | 0.14237 | 0.13734 | 0.13611 | 0.13809 | 0.13396 | 0.13027 | 0.12802 | 0.1244 | 0.10094
VP49_1_H400_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.61522 | 0.59901 | 0.61758 | 0.62149 | 0.64463 | 0.66867 | 0.65894 | 0.66084 | 0.63231 | 0.63757 | 0.64982 | 0.6428 | 0.65742 | 0.64795 | 0.65305 | 0.65652 | 0.67024 | 0.66469
VP49_1_H400_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.21316 | 0.23272 | 0.21482 | 0.21738 | 0.20467 | 0.18447 | 0.19792 | 0.19726 | 0.22434 | 0.22006 | 0.21284 | 0.22109 | 0.20448 | 0.21808 | 0.21668 | 0.21546 | 0.20536 | 0.23437
VP49_2_H400_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.16603 | 0.17757 | 0.16844 | 0.16027 | 0.15375 | 0.15029 | 0.14684 | 0.14538 | 0.14423 | 0.13885 | 0.14019 | 0.13942 | 0.13611 | 0.13255 | 0.12854 | 0.12481 | 0.12963 | 0.10041
VP49_2_H400_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.60865 | 0.63929 | 0.63015 | 0.67285 | 0.68218 | 0.6776 | 0.69015 | 0.66985 | 0.68514 | 0.68118 | 0.66279 | 0.67321 | 0.68914 | 0.70214 | 0.68701 | 0.71862 | 0.69867 | 0.66834
VP49_2_H400_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.22532 | 0.18314 | 0.2014 | 0.16688 | 0.16407 | 0.17211 | 0.16301 | 0.18477 | 0.17062 | 0.17996 | 0.19701 | 0.18736 | 0.17474 | 0.16531 | 0.18446 | 0.15657 | 0.1717 | 0.23125
Tool
Work piece
Chip

## Slide 36
Chart: 
| 560.0 | 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 80.7151 | 320.6505 | 164.6276 | 258.5114 | 292.081 | 307.2485 | 295.4871 | 320.948 | 442.4843 | 487.8577
Time and spatial varying thermal properties Temperature distribution for hsp = 400 µm, vc = 150 m/min [1/2]
Chart: 
| 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 68.689 | 268.2742 | 250.5316 | 437.5165 | 522.3134 | 526.7539 | 484.8667 | 611.3435 | 820.1525
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
[°C]
[W]
Workpiece position : 124 mm
Workpiece position : 200 mm
[°C]

## Slide 37
Chart: 
| 560.0 | 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 192.8838 | 257.8368 | 210.0623 | 233.8197 | 235.1887 | 246.4138 | 260.4695 | 317.5629 | 415.2001 | 462.272
Time and spatial varying thermal properties Temperature distribution for hsp = 400 µm, vc = 150 m/min [2/2]
Chart: 
| 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 237.8927 | 166.411 | 165.4571 | 350.3633 | 437.1715 | 468.495 | 479.0329 | 604.9173 | 808.0161
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
Workpiece position : 124 mm
Workpiece position : 200 mm
[°C]

## Slide 38: Time and spatial varying thermal properties Heat partition ratios for hsp = 500 µm, vc = 150 m/min
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 116,16 | 123,78 | 131,40 | 139,02 | 146,65 | 154,27 | 161,89 | 169,51 | 177,13 | 184,76 | 192,38 | 200,00
VP50_1_H500_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.15854 | 0.15187 | 0.14488 | 0.14059 | 0.1365 | 0.13265 | 0.12984 | 0.12727 | 0.12719 | 0.12764 | 0.12247 | 0.12001 | 0.11681 | 0.1138 | 0.10938 | 0.10647 | 0.10543 | 0.076435
VP50_1_H500_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.6265 | 0.63812 | 0.65803 | 0.67398 | 0.70702 | 0.70043 | 0.68971 | 0.67757 | 0.67139 | 0.66681 | 0.65798 | 0.66806 | 0.66678 | 0.67553 | 0.69019 | 0.69354 | 0.70406 | 0.68549
VP50_1_H500_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.21495 | 0.21001 | 0.19709 | 0.18543 | 0.15647 | 0.16691 | 0.18046 | 0.19516 | 0.20142 | 0.20555 | 0.21955 | 0.21193 | 0.21641 | 0.21068 | 0.20042 | 0.2 | 0.19051 | 0.23807
VP50_2_H500_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.1587 | 0.15596 | 0.14703 | 0.14362 | 0.13746 | 0.13424 | 0.13379 | 0.13049 | 0.12693 | 0.13108 | 0.12731 | 0.12272 | 0.11893 | 0.1145 | 0.11184 | 0.11094 | 0.10843 | 0.076291
VP50_2_H500_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.6415 | 0.65939 | 0.65955 | 0.69394 | 0.73029 | 0.71535 | 0.71119 | 0.69405 | 0.69127 | 0.67765 | 0.68556 | 0.67657 | 0.68968 | 0.68217 | 0.69574 | 0.69898 | 0.70165 | 0.67331
VP50_2_H500_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.1998 | 0.18465 | 0.19342 | 0.16244 | 0.13225 | 0.15042 | 0.15502 | 0.17546 | 0.18179 | 0.19127 | 0.18713 | 0.20071 | 0.19138 | 0.20333 | 0.19242 | 0.19008 | 0.18992 | 0.2504
Tool
Work piece
Chip

## Slide 39
Chart: 
| 600.0 | 560.0 | 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 63.8527 | 560.2505 | 251.2757 | 252.2608 | 230.2662 | 211.3697 | 220.3811 | 278.852 | 347.0043 | 400.8129 | 385.539
Chart: 
| 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 279.47 | 190.28 | 318.99 | 368.67 | 455.56 | 463.8 | 546.98 | 679.2 | 834.14
Time and spatial varying thermal properties Temperature distribution for hsp = 500 µm, vc = 150 m/min
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
Workpiece position : 124 mm
Workpiece position : 200 mm
[°C]

## Slide 40: Time and spatial varying thermal properties Conclusion
XYZ

## Slide 41: Time and spatial varying thermal properties Means to enhance quality of measurement
Determine emissivity of chip/tool/workpiece
  Collect chips
  Heating + Pyrometer + Camera
  e (DL)
  Regression of Tcam (DL, ecam) for IT
Enhance quantity of valid pixels
  Expand field of measurement
  Measurement with multiple integration times
  Overlap pictures via algorithm
Determine workpiece directly
  Separate measurements for the work piece
  Compare Heat flows with Ptotal

## Slide 42: Gliederung
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Influence of uncut chip thickness and cutting velocity
3.2
Time and spatial varying thermal properties
3.1
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 43: Influence of uncut chip thickness and cutting velocity Workpiece position 124 mm
ap = 3,5 mm, = 6°, = 3°, < 5 µm, uncoated, workpiece position: 124 mm
Chart: Heat partition (chip)
| 100,00 | 150,00
200,00 | 0.60676 | 0.66906
300,00 | 0.65008 | 0.67723
400,00 | 0.66524 | 0.66084
500,00 | 0.67757
Chart: Heat partition (tool)
| 100,00 | 150,00
200,00 | 0.26863 | 0.21337
300,00 | 0.16446 | 0.19743
400,00 | 0.18464 | 0.1419
500,00 | 0.12727
Chart: Heat flow (chip) [W]
| 100,00 | 150,00
200,00 | 1451.366 | 2209.5729
300,00 | 2208.0209 | 3055.4101
400,00 | 2734.291 | 4006.6247
500,00 | 4892.1433
Chart: Heat flow (workpiece) [W]
| 100,00 | 150,00
200,00 | 236.0741 | 388.3001
300,00 | 629.9304 | 565.4876
400,00 | 617.0218 | 1195.9647
500,00 | 1409.1149
Chart: Heat partition (workpiece)
| 100,00 | 150,00
200,00 | 0.10334 | 0.11758
300,00 | 0.18546 | 0.12534
400,00 | 0.15012 | 0.19726
500,00 | 0.19516
hsp [µm]
Cutting velocity [m/min]
Chart: Heat flow (tool) [W]
| 100,00 | 150,00
200,00 | 613.6531 | 704.6531
300,00 | 558.5991 | 890.7576
400,00 | 758.8956 | 860.3197
500,00 | 918.9017

## Slide 44: Influence of uncut chip thickness and cutting velocity Workpiece position 200 mm
ap = 3,5 mm, = 6°, = 3°, < 5 µm, uncoated, workpiece position: 200 mm
Chart: Heat flow (chip) [W]
| 100,00 | 150,00
200,00 | 1704.9593 | 2425.7515
300,00 | 2526.242 | 3375.8082
400,00 | 4015.3245
500,00 | 4981.0634
Chart: Heat partition (chip)
| 100,00 | 150,00
200,00 | 0.71637 | 0.74156
300,00 | 0.74377 | 0.74824
400,00 | 0.66469
500,00 | 0.68549
Chart: Heat partition (tool)
| 100,00 | 150,00
200,00 | 0.20594 | 0.12778
300,00 | 0.13118 | 0.13939
400,00 | 0.10094
500,00 | 0.076435
Chart: Heat flow (workpiece) [W]
| 100,00 | 150,00
200,00 | 184.8823 | 427.4342
300,00 | 424.761 | 506.9785
400,00 | 1415.8298
500,00 | 1729.9051
Chart: Heat partition (workpiece)
| 100,00 | 150,00
200,00 | 0.077682 | 0.13067
300,00 | 0.12506 | 0.11237
400,00 | 0.23437
500,00 | 0.23807
Chart: Heat flow (tool) [W]
| 100,00 | 150,00
200,00 | 490.1465 | 417.9774
300,00 | 445.5474 | 628.8686
400,00 | 609.7427
500,00 | 555.4084
hsp [µm]
Cutting velocity [m/min]

## Slide 45: Gliederung
Influence of uncut chip thickness and cutting velocity
4.2
Time and spatial varying thermal properties
4.1
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 46: Gliederung
Influence of uncut chip thickness and cutting velocity
4.2
Time and spatial varying thermal properties
4.1
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 47: Time and spatial varying thermal properties Temperature at tool tip [°C] for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 305.7037 | 359.0087 | 373.894 | 312.2685 | 360.8156 | 366.7087 | 372.1807 | 380.9632
VP33_1_H300_V150_ACF_MF_285 | 335.7945 | 135.8712 | 362.3886 | 327.2749 | 342.5201 | 288.9588 | 288.0323 | 371.5422
VP36_1_H200_V100_ABA_MF_285 | 316.5908 | 315.1712 | 292.0169 | 280.8572 | 296.6303 | 309.9306 | 325.7267 | 344.5932 | 350.3726 | 358.5259 | 358.7022
VP37_1_H200_V150_ABA_MF_425 | 295.4657 | 318.1522 | 324.3459 | 341.6017 | 341.4323 | 309.9544 | 304.425 | 330.101
VP38_1_H300_V100_ABA_MF_425 | 341.7368 | 363.4779 | 348.2248 | 327.5525 | 326.8533 | 353.8151 | 364.2259 | 384.6232 | 398.1447 | 397.0859 | 406.7007
VP39_1_H300_V150_ABA_MF_425 | 352.8635 | 312.1887 | 375.9718 | 370.9857 | 404.1945 | 383.358 | 380.4667 | 382.8193
VP4_1_H300_V100_ACF_MF_285 | 294.5303 | 293.4045 | 314.7375 | 289.1686 | 324.354 | 328.7716 | 294.2745 | 336.7471 | 273.9328 | 159.8445 | 413.0847
VP5_1_H200_V100_ACF_MF_285 | 354.8135 | 260.6953 | 252.9006 | 241.9538 | 266.5126 | 318.9569 | 244.8525 | 305.5209 | 287.8376 | 391.1507 | 350.3544
VP6_1_H100_V100_ACF_MF_285 | 207.9595 | 232.7021 | 240.8276 | 356.2291 | 253.0614 | 397.676 | 433.4986

## Slide 48: Time and spatial varying thermal properties Internal energy in tool [Joule] for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 0.5496 | 0.80782 | 1.0833 | 1.2851 | 1.645 | 2.0291 | 2.4 | 2.5047
VP33_1_H300_V150_ACF_MF_285 | 1.1127 | 1.3071 | 1.6818 | 1.1978 | 1.675 | 2.253 | 2.7183 | 2.9855
VP36_1_H200_V100_ABA_MF_285 | 0.75171 | 0.95339 | 1.2146 | 1.3612 | 1.4699 | 1.555 | 1.6303 | 1.6805 | 1.7328 | 1.7881 | 1.8598
VP37_1_H200_V150_ABA_MF_425 | 0.57231 | 0.67533 | 0.8089 | 0.99411 | 1.1883 | 1.4484 | 1.6506 | 1.6177
VP38_1_H300_V100_ABA_MF_425 | 0.97041 | 1.2301 | 1.4664 | 1.8019 | 2.0327 | 2.2325 | 2.4148 | 2.5202 | 2.5836 | 2.7293 | 2.8055
VP39_1_H300_V150_ABA_MF_425 | 0.85018 | 0.92941 | 1.2235 | 1.4735 | 1.6777 | 2.1493 | 2.5398 | 2.703
VP4_1_H300_V100_ACF_MF_285 | 0.97925 | 1.258 | 1.586 | 2.0673 | 2.2472 | 2.6177 | 2.7775 | 2.9476 | 3.0778 | 3.4084 | 3.9398
VP5_1_H200_V100_ACF_MF_285 | 0.62438 | 0.61766 | 0.77684 | 1.0456 | 1.1331 | 1.5858 | 1.464 | 1.6027 | 1.7143 | 2.5029 | 2.5716
VP6_1_H100_V100_ACF_MF_285 | 0.57683 | 0.69313 | 0.77616 | 0.994 | 0.88849 | 1.1495 | 1.1785

## Slide 49: Time and spatial varying thermal properties Internal energy rate of the tool [W] for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 12.7277 | 12.7277 | 12.7277 | 12.7277 | 12.7277 | 12.7277 | 12.7277 | 12.7277
VP33_1_H300_V150_ACF_MF_285 | 11.4532 | 11.4532 | 11.4532 | 11.4532 | 11.4532 | 11.4532 | 11.4532 | 11.4532
VP36_1_H200_V100_ABA_MF_285 | 4.3945 | 4.3945 | 4.3945 | 4.3945 | 4.3945 | 4.3945 | 4.3945 | 4.3945 | 4.3945 | 4.3945 | 4.3945
VP37_1_H200_V150_ABA_MF_425 | 7.3294 | 7.3294 | 7.3294 | 7.3294 | 7.3294 | 7.3294 | 7.3294 | 7.3294
VP38_1_H300_V100_ABA_MF_425 | 7.9584 | 7.9584 | 7.9584 | 7.9584 | 7.9584 | 7.9584 | 7.9584 | 7.9584 | 7.9584 | 7.9584 | 7.9584
VP39_1_H300_V150_ABA_MF_425 | 12.297 | 12.297 | 12.297 | 12.297 | 12.297 | 12.297 | 12.297 | 12.297
VP4_1_H300_V100_ACF_MF_285 | 11.8029 | 11.8029 | 11.8029 | 11.8029 | 11.8029 | 11.8029 | 11.8029 | 11.8029 | 11.8029 | 11.8029 | 11.8029
VP5_1_H200_V100_ACF_MF_285 | 8.4246 | 8.4246 | 8.4246 | 8.4246 | 8.4246 | 8.4246 | 8.4246 | 8.4246 | 8.4246 | 8.4246 | 8.4246
VP6_1_H100_V100_ACF_MF_285 | 4.3497 | 4.3497 | 4.3497 | 4.3497 | 4.3497 | 4.3497 | 4.3497

## Slide 50: Time and spatial varying thermal properties Internal energy carried away by chip [W] for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 1440.7798 | 1409.6175 | 1575.8269 | 1597.1321 | 1524.1344 | 1545.9622 | 1536.5762 | 1737.7919
VP33_1_H300_V150_ACF_MF_285 | 2279.2673 | 2211.4647 | 2145.7486 | 2226.8733 | 2243.05 | 2163.0123 | 2214.0318 | 2501.462
VP36_1_H200_V100_ABA_MF_285 | 1000.0666 | 1041.6505 | 1032.0091 | 1055.0515 | 1047.0781 | 1066.5142 | 1083.8348 | 1046.1131 | 1047.9808 | 1055.4452 | 979.5612
VP37_1_H200_V150_ABA_MF_425 | 1513.4059 | 1492.3547 | 1566.5455 | 1580.8656 | 1538.5796 | 1605.1663 | 1659.9065 | 1664.4079
VP38_1_H300_V100_ABA_MF_425 | 1528.9569 | 1564.0366 | 1499.5168 | 1499.2694 | 1597.8732 | 1498.4805 | 1622.2786 | 1571.0286 | 1567.6816 | 1690.7209 | 1574.3611
VP39_1_H300_V150_ABA_MF_425 | 2317.0557 | 2233.4372 | 2208.7731 | 2303.8621 | 2295.3274 | 2294.6617 | 2216.7907 | 2434.1194
VP4_1_H300_V100_ACF_MF_285 | 1399.4917 | 1334.4974 | 1360.9848 | 1420.2373 | 1446.1944 | 1440.8875 | 1460.274 | 1468.3725 | 1477.692 | 1662.3925 | 1658.4424
VP5_1_H200_V100_ACF_MF_285 | 1068.9325 | 963.4712 | 959.7932 | 991.5921 | 986.4712 | 1017.9059 | 1014.6047 | 1066.8849 | 1058.5964 | 1094.6674 | 1151.3422
VP6_1_H100_V100_ACF_MF_285 | 501.0422 | 496.3653 | 525.5356 | 505.9998 | 519.2836 | 528.8747 | 522.0725

## Slide 51: Time and spatial varying thermal properties Heat partition to the chip for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 0.56276 | 0.55058 | 0.61628 | 0.62383 | 0.59531 | 0.60384 | 0.59703 | 0.67702
VP33_1_H300_V150_ACF_MF_285 | 0.67654 | 0.65923 | 0.63691 | 0.66383 | 0.66652 | 0.64203 | 0.6579 | 0.74249
VP36_1_H200_V100_ABA_MF_285 | 0.51458 | 0.53225 | 0.52788 | 0.54077 | 0.53502 | 0.54609 | 0.55439 | 0.53565 | 0.53821 | 0.54204 | 0.50258
VP37_1_H200_V150_ABA_MF_425 | 0.55082 | 0.54419 | 0.57125 | 0.57647 | 0.56052 | 0.58308 | 0.60111 | 0.6052
VP38_1_H300_V100_ABA_MF_425 | 0.5311 | 0.54203 | 0.52436 | 0.52653 | 0.56233 | 0.52513 | 0.57092 | 0.55288 | 0.54578 | 0.5925 | 0.55172
VP39_1_H300_V150_ABA_MF_425 | 0.52306 | 0.50865 | 0.49861 | 0.52469 | 0.52274 | 0.52479 | 0.50377 | 0.55316
VP4_1_H300_V100_ACF_MF_285 | 0.60646 | 0.58066 | 0.59059 | 0.61545 | 0.6267 | 0.62778 | 0.63623 | 0.63719 | 0.64381 | 0.72706 | 0.72533
VP5_1_H200_V100_ACF_MF_285 | 0.63678 | 0.57561 | 0.57421 | 0.59241 | 0.59017 | 0.60982 | 0.60867 | 0.63828 | 0.63154 | 0.6567 | 0.68279
VP6_1_H100_V100_ACF_MF_285 | 0.5272 | 0.52829 | 0.55933 | 0.536 | 0.55182 | 0.56375 | 0.55028

## Slide 52: Time and spatial varying thermal properties Heat flow into the tool [W] for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 556.4072 | 603.7772 | 604.8082 | 623.2733 | 624.2343 | 629.8136 | 712.0943 | 313.8649
VP33_1_H300_V150_ACF_MF_285 | 729.3436 | 788.1397 | 743.2446 | 850.6799 | 872.6318 | 946.9996 | 948.4236 | 542.6406
VP36_1_H200_V100_ABA_MF_285 | 548.377 | 545.5842 | 646.5583 | 655.6584 | 678.5535 | 586.1828 | 589.7718 | 588.613 | 543.4482 | 385.465 | 196.1034
VP37_1_H200_V150_ABA_MF_425 | 578.3997 | 604.9081 | 597.1974 | 642.8969 | 599.5582 | 682.2016 | 673.7179 | 359.8966
VP38_1_H300_V100_ABA_MF_425 | 542.3998 | 581.5204 | 517.4702 | 595.1662 | 624.8957 | 643.3261 | 636.7192 | 578.5419 | 507.2736 | 510.927 | 135.9759
VP39_1_H300_V150_ABA_MF_425 | 728.2056 | 717.4364 | 693.7266 | 717.2665 | 617.5927 | 748.3198 | 850.0767 | 624.6815
VP4_1_H300_V100_ACF_MF_285 | 499.6376 | 493.2403 | 500.4005 | 530.3183 | 514.5962 | 543.8055 | 557.0382 | 545.3328 | 526.916 | 737.7693 | 140.8039
VP5_1_H200_V100_ACF_MF_285 | 373.3381 | 385.5974 | 412.904 | 444.3073 | 449.4878 | 441.9678 | 466.0595 | 418.7901 | 419.6496 | 401.4418 | 136.4207
VP6_1_H100_V100_ACF_MF_285 | 365.5636 | 346.6279 | 358.9071 | 292.8281 | 285.1845 | 282.6005 | 109.3694

## Slide 53: Time and spatial varying thermal properties Heat partition into the tool for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 0.21733 | 0.23583 | 0.23653 | 0.24344 | 0.24382 | 0.246 | 0.27668 | 0.12228
VP33_1_H300_V150_ACF_MF_285 | 0.21649 | 0.23494 | 0.22061 | 0.25359 | 0.2593 | 0.28109 | 0.28182 | 0.16107
VP36_1_H200_V100_ABA_MF_285 | 0.28217 | 0.27878 | 0.33072 | 0.33606 | 0.34672 | 0.30015 | 0.30167 | 0.30139 | 0.2791 | 0.19796 | 0.10061
VP37_1_H200_V150_ABA_MF_425 | 0.21052 | 0.22058 | 0.21777 | 0.23443 | 0.21843 | 0.24781 | 0.24398 | 0.13086
VP38_1_H300_V100_ABA_MF_425 | 0.18841 | 0.20153 | 0.18095 | 0.20902 | 0.21992 | 0.22545 | 0.22408 | 0.2036 | 0.17661 | 0.17905 | 0.047652
VP39_1_H300_V150_ABA_MF_425 | 0.16439 | 0.16339 | 0.1566 | 0.16335 | 0.14065 | 0.17114 | 0.19318 | 0.14196
VP4_1_H300_V100_ACF_MF_285 | 0.21651 | 0.21462 | 0.21715 | 0.22981 | 0.223 | 0.23693 | 0.2427 | 0.23664 | 0.22957 | 0.32267 | 0.061581
VP5_1_H200_V100_ACF_MF_285 | 0.2224 | 0.23037 | 0.24703 | 0.26544 | 0.26891 | 0.26478 | 0.27959 | 0.25055 | 0.25036 | 0.24083 | 0.080903
VP6_1_H100_V100_ACF_MF_285 | 0.38465 | 0.36892 | 0.38199 | 0.31019 | 0.30305 | 0.30124 | 0.11528

## Slide 54: Time and spatial varying thermal properties Heat flow into the workpiece [W] for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 563.037 | 546.8293 | 376.3628 | 339.8185 | 411.8552 | 384.4481 | 325.0215 | 515.1814
VP33_1_H300_V150_ACF_MF_285 | 360.4008 | 354.9887 | 480.0186 | 277.0399 | 249.6313 | 259 | 202.8577 | 324.9092
VP36_1_H200_V100_ABA_MF_285 | 395.0174 | 369.8375 | 276.4439 | 240.3053 | 231.4406 | 300.2961 | 281.4047 | 318.267 | 355.7418 | 506.2608 | 773.4107
VP37_1_H200_V150_ABA_MF_425 | 655.7249 | 645.0666 | 578.5865 | 518.5669 | 606.77 | 465.5521 | 427.7871 | 725.8956
VP38_1_H300_V100_ABA_MF_425 | 807.5081 | 739.9544 | 842.7033 | 753.0367 | 618.7442 | 711.7226 | 582.5152 | 691.9426 | 797.3957 | 651.8814 | 1143.1922
VP39_1_H300_V150_ABA_MF_425 | 1384.558 | 1440.0645 | 1527.3196 | 1369.8094 | 1478.0178 | 1329.5587 | 1333.5143 | 1341.5808
VP4_1_H300_V100_ACF_MF_285 | 408.5077 | 470.4923 | 443.0534 | 357.0814 | 346.8464 | 310.5191 | 277.8999 | 290.7334 | 290.6041 | -113.6965 | 487.2191
VP5_1_H200_V100_ACF_MF_285 | 236.3751 | 324.764 | 298.7932 | 237.9332 | 235.5314 | 209.314 | 186.258 | 185.8154 | 197.9708 | 170.813 | 398.4663
VP6_1_H100_V100_ACF_MF_285 | 83.7701 | 96.5804 | 55.1309 | 145.2013 | 136.5651 | 126.6624 | 317.2984

## Slide 55: Time and spatial varying thermal properties Heat partition into the workpiece for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 0.21992 | 0.21359 | 0.14719 | 0.13273 | 0.16087 | 0.15016 | 0.12629 | 0.20071
VP33_1_H300_V150_ACF_MF_285 | 0.10698 | 0.10582 | 0.14248 | 0.082585 | 0.074178 | 0.076877 | 0.060279 | 0.09644
VP36_1_H200_V100_ABA_MF_285 | 0.20325 | 0.18897 | 0.1414 | 0.12317 | 0.11826 | 0.15376 | 0.14394 | 0.16296 | 0.1827 | 0.26 | 0.39681
VP37_1_H200_V150_ABA_MF_425 | 0.23866 | 0.23523 | 0.21098 | 0.1891 | 0.22105 | 0.16911 | 0.15492 | 0.26394
VP38_1_H300_V100_ABA_MF_425 | 0.2805 | 0.25644 | 0.29468 | 0.26446 | 0.21775 | 0.24942 | 0.205 | 0.24351 | 0.27761 | 0.22845 | 0.40062
VP39_1_H300_V150_ABA_MF_425 | 0.31255 | 0.32796 | 0.34478 | 0.31196 | 0.33661 | 0.30407 | 0.30305 | 0.30488
VP4_1_H300_V100_ACF_MF_285 | 0.17702 | 0.20472 | 0.19226 | 0.15474 | 0.1503 | 0.13529 | 0.12108 | 0.12616 | 0.12661 | -0.049726 | 0.21309
VP5_1_H200_V100_ACF_MF_285 | 0.14081 | 0.19402 | 0.17876 | 0.14215 | 0.14091 | 0.1254 | 0.11174 | 0.11117 | 0.11811 | 0.10247 | 0.23631
VP6_1_H100_V100_ACF_MF_285 | 0.088144 | 0.10279 | 0.058677 | 0.15381 | 0.14512 | 0.13501 | 0.33444

## Slide 56: Time and spatial varying thermal properties Friction coefficient µ for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 0.59167 | 0.59167 | 0.59167 | 0.59167 | 0.59167 | 0.59167 | 0.59167 | 0.59167
VP33_1_H300_V150_ACF_MF_285 | 0.48325 | 0.48325 | 0.48325 | 0.48325 | 0.48325 | 0.48325 | 0.48325 | 0.48325
VP36_1_H200_V100_ABA_MF_285 | 0.42608 | 0.42608 | 0.42608 | 0.42608 | 0.42608 | 0.42608 | 0.42608 | 0.42608 | 0.42608 | 0.42608 | 0.42608
VP37_1_H200_V150_ABA_MF_425 | 0.42314 | 0.42314 | 0.42314 | 0.42314 | 0.42314 | 0.42314 | 0.42314 | 0.42314
VP38_1_H300_V100_ABA_MF_425 | 1.052 | 1.052 | 1.052 | 1.052 | 1.052 | 1.052 | 1.052 | 1.052 | 1.052 | 1.052 | 1.052
VP39_1_H300_V150_ABA_MF_425 | 1.0281 | 1.0281 | 1.0281 | 1.0281 | 1.0281 | 1.0281 | 1.0281 | 1.0281
VP4_1_H300_V100_ACF_MF_285 | 0.58779 | 0.58779 | 0.58779 | 0.58779 | 0.58779 | 0.58779 | 0.58779 | 0.58779 | 0.58779 | 0.58779 | 0.58779
VP5_1_H200_V100_ACF_MF_285 | 0.64224 | 0.64224 | 0.64224 | 0.64224 | 0.64224 | 0.64224 | 0.64224 | 0.64224 | 0.64224 | 0.64224 | 0.64224
VP6_1_H100_V100_ACF_MF_285 | 0.73325 | 0.73325 | 0.73325 | 0.73325 | 0.73325 | 0.73325 | 0.73325

## Slide 57: Time and spatial varying thermal properties Heat partition ratios for hsp = 100 µm, vc = 100 m/min (ACF)
Chart: Workpiece position [mm]
| 49,51 | 54,59 | 59,67 | 64,76 | 69,84 | 74,92 | 80,00
Summe von Percent - Heat inside tool/Total heat | 0.38465 | 0.36892 | 0.38199 | 0.31019 | 0.30305 | 0.30124 | 0.11528
Summe von Percent - Heat through chip/Total heat | 0.5272 | 0.52829 | 0.55933 | 0.536 | 0.55182 | 0.56375 | 0.55028
Summe von Percent - Heat through workpiece/Total heat | 0.088144 | 0.10279 | 0.058677 | 0.15381 | 0.14512 | 0.13501 | 0.33444
Work piece
Tool
Chip

## Slide 58
Chart: 
| 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
 | 28.7261 | 36.5382 | 32.1285 | 69.731 | 98.8777 | 103.4594 | 106.5801
Time and spatial varying thermal properties Temperature distribution for hsp = 100 µm, vc = 100 m/min (ACF)
Workpiece position : 49,51 mm
Workpiece position : 80 mm
Chart: 
| 280.0 | 240.0 | 200.0
 | 240.4105 | 329.2442 | 393.1837
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
[°C]
[°C]

## Slide 59: Time and spatial varying thermal properties Heat partition ratios for hsp = 200 µm, vc = 100 m/min (ACF)
Chart: Workpiece position [mm]
| 29,19 | 34,27 | 39,35 | 44,43 | 49,51 | 54,59 | 59,67 | 64,76 | 69,84 | 74,92 | 80,00
Summe von Percent - Heat inside tool/Total heat | 0.2224 | 0.23037 | 0.24703 | 0.26544 | 0.26891 | 0.26478 | 0.27959 | 0.25055 | 0.25036 | 0.24083 | 0.080903
Summe von Percent - Heat through chip/Total heat | 0.63678 | 0.57561 | 0.57421 | 0.59241 | 0.59017 | 0.60982 | 0.60867 | 0.63828 | 0.63154 | 0.6567 | 0.68279
Summe von Percent - Heat through workpiece/Total heat | 0.14081 | 0.19402 | 0.17876 | 0.14215 | 0.14091 | 0.1254 | 0.11174 | 0.11117 | 0.11811 | 0.10247 | 0.23631
Work piece
Tool
Chip

## Slide 60
Time and spatial varying thermal properties Temperature distribution for hsp = 200 µm, vc = 100 m/min (ACF)
Workpiece position : 80 mm
Workpiece position : 34,27 mm
Chart: 
| 360.0 | 320.0 | 280.0 | 240.0 | 200.0
 | 22.5899 | 184.5007 | 296.2311 | 347.2808 | 407.0649
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
Chart: 
| 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
 | 56.6767 | 134.1579 | 177.1651 | 187.0125 | 140.8678 | 119.5719 | 136.4204
[°C]
[°C]

## Slide 61: Time and spatial varying thermal properties Heat partition ratios for hsp = 300 µm, vc = 100 m/min (ACF)
Chart: Workpiece position [mm]
| 29,19 | 34,27 | 39,35 | 44,43 | 49,51 | 54,59 | 59,67 | 64,76 | 69,84 | 74,92 | 80,00
Summe von Percent - Heat inside tool/Total heat | 0.21651 | 0.21462 | 0.21715 | 0.22981 | 0.223 | 0.23693 | 0.2427 | 0.23664 | 0.22957 | 0.32267 | 0.061581
Summe von Percent - Heat through chip/Total heat | 0.60646 | 0.58066 | 0.59059 | 0.61545 | 0.6267 | 0.62778 | 0.63623 | 0.63719 | 0.64381 | 0.72706 | 0.72533
Summe von Percent - Heat through workpiece/Total heat | 0.17702 | 0.20472 | 0.19226 | 0.15474 | 0.1503 | 0.13529 | 0.12108 | 0.12616 | 0.12661 | -0.049726 | 0.21309
Work piece
Tool
Chip

## Slide 62
Time and spatial varying thermal properties Temperature distribution for hsp = 300 µm, vc = 100 m/min (ACF)
Workpiece position : 34,27 mm
Workpiece position : 80 mm
Chart: 
| 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
 | 37.0253 | 72.5513 | 108.0941 | 171.764 | 317.5577 | 418.323 | 443.4006 | 519.4741
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
Chart: 
| 560.0 | 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
 | 47.379 | 100.8963 | 150.7926 | 190.9737 | 231.7964 | 183.7827 | 128.1862 | 118.3794 | 123.4177 | 134.5843
[°C]
[°C]

## Slide 63: Time and spatial varying thermal properties Heat partition ratios for hsp = 200 µm, vc = 150 m/min (ACF)
Chart: Workpiece position [mm]
| 26,65 | 34,27 | 41,89 | 49,51 | 57,13 | 64,76 | 72,38 | 80,00
Summe von Percent - Heat inside tool/Total heat | 0.21733 | 0.23583 | 0.23653 | 0.24344 | 0.24382 | 0.246 | 0.27668 | 0.12228
Summe von Percent - Heat through chip/Total heat | 0.56276 | 0.55058 | 0.61628 | 0.62383 | 0.59531 | 0.60384 | 0.59703 | 0.67702
Summe von Percent - Heat through workpiece/Total heat | 0.21992 | 0.21359 | 0.14719 | 0.13273 | 0.16087 | 0.15016 | 0.12629 | 0.20071
Tool
Work piece
Chip

## Slide 64
Time and spatial varying thermal properties Temperature distribution for hsp = 200 µm, vc = 150 m/min (ACF)
Workpiece position : 34,27 mm
Workpiece position : 80 mm
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
Chart: 
| 360.0 | 320.0 | 280.0 | 240.0 | 200.0
 | 32.2374 | 269.7817 | 405.9462 | 548.0768 | 634.0221
Chart: 
| 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
 | 19.5301 | 120.2908 | 212.0917 | 339.4722 | 270.0335 | 244.3187 | 243.7614 | 273.204 | 329.0703
[°C]
[°C]

## Slide 65: Time and spatial varying thermal properties Heat partition ratios for hsp = 300 µm, vc = 150 m/min (ACF)
Chart: Workpiece position [mm]
| 26,65 | 34,27 | 41,89 | 49,51 | 57,13 | 64,76 | 72,38 | 80,00
Summe von Percent - Heat inside tool/Total heat | 0.21649 | 0.23494 | 0.22061 | 0.25359 | 0.2593 | 0.28109 | 0.28182 | 0.16107
Summe von Percent - Heat through chip/Total heat | 0.67654 | 0.65923 | 0.63691 | 0.66383 | 0.66652 | 0.64203 | 0.6579 | 0.74249
Summe von Percent - Heat through workpiece/Total heat | 0.10698 | 0.10582 | 0.14248 | 0.082585 | 0.074178 | 0.076877 | 0.060279 | 0.09644
Work piece
Tool
Chip

## Slide 66
Time and spatial varying thermal properties Temperature distribution for hsp = 300 µm, vc = 150 m/min (ACF)
Workpiece position : 34,27 mm
Workpiece position : 80 mm
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
Chart: 
| 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
 | 26.2226 | 105.7568 | 390.5428 | 588.6042 | 701.2221 | 729.9227 | 823.4503
Chart: 
| 560.0 | 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
 | 20.4284 | 180.5961 | 281.8903 | 330.7883 | 317.3775 | 433.9738 | 455.5993 | 456.4069 | 505.7701 | 556.6048
[°C]
[°C]

## Slide 67: Time and spatial varying thermal properties Heat partition ratios for hsp = 200 µm, vc = 100 m/min (ABA)
Chart: Workpiece position [mm]
| 29,19 | 34,27 | 39,35 | 44,43 | 49,51 | 54,59 | 59,67 | 64,76 | 69,84 | 74,92 | 80,00
Summe von Percent - Heat inside tool/Total heat | 0.28217 | 0.27878 | 0.33072 | 0.33606 | 0.34672 | 0.30015 | 0.30167 | 0.30139 | 0.2791 | 0.19796 | 0.10061
Summe von Percent - Heat through chip/Total heat | 0.51458 | 0.53225 | 0.52788 | 0.54077 | 0.53502 | 0.54609 | 0.55439 | 0.53565 | 0.53821 | 0.54204 | 0.50258
Summe von Percent - Heat through workpiece/Total heat | 0.20325 | 0.18897 | 0.1414 | 0.12317 | 0.11826 | 0.15376 | 0.14394 | 0.16296 | 0.1827 | 0.26 | 0.39681
Tool
Work piece
Chip

## Slide 68
Time and spatial varying thermal properties Temperature distribution for hsp = 200 µm, vc = 100 m/min (ABA)
Workpiece position : 34,27 mm
Workpiece position : 80 mm
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
Chart: 
| 320.0 | 280.0 | 240.0 | 200.0
 | 348.9817 | 432.9284 | 481.5017 | 600.8778
Chart: 
| 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
 | 136.7369 | 216.0353 | 172.5507 | 151.7713 | 187.7296 | 195.6882
[°C]
[°C]

## Slide 69: Time and spatial varying thermal properties Heat partition ratios for hsp = 200 µm, vc = 150 m/min (ABA)
Chart: Workpiece position [mm]
| 26,65 | 34,27 | 41,89 | 49,51 | 57,13 | 64,76 | 72,38 | 80,00
Summe von Percent - Heat inside tool/Total heat | 0.21052 | 0.22058 | 0.21777 | 0.23443 | 0.21843 | 0.24781 | 0.24398 | 0.13086
Summe von Percent - Heat through chip/Total heat | 0.55082 | 0.54419 | 0.57125 | 0.57647 | 0.56052 | 0.58308 | 0.60111 | 0.6052
Summe von Percent - Heat through workpiece/Total heat | 0.23866 | 0.23523 | 0.21098 | 0.1891 | 0.22105 | 0.16911 | 0.15492 | 0.26394
Tool
Work piece
Chip

## Slide 70
Time and spatial varying thermal properties Temperature distribution for hsp = 200 µm, vc = 150 m/min (ABA)
Workpiece position : 34,27 mm
Workpiece position : 80 mm
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
Chart: 
| 320.0 | 280.0 | 240.0 | 200.0
 | 379.9596 | 449.0781 | 531.9704 | 663.1871
Chart: 
| 360.0 | 320.0 | 280.0 | 240.0 | 200.0
 | 394.8836 | 370.7069 | 345.6125 | 334.0485 | 371.086
[°C]
[°C]

## Slide 71: Time and spatial varying thermal properties Heat partition ratios for hsp = 300 µm, vc = 100 m/min (ABA)
Chart: Workpiece position [mm]
| 29,19 | 34,27 | 39,35 | 44,43 | 49,51 | 54,59 | 59,67 | 64,76 | 69,84 | 74,92 | 80,00
Summe von Percent - Heat inside tool/Total heat | 0.18841 | 0.20153 | 0.18095 | 0.20902 | 0.21992 | 0.22545 | 0.22408 | 0.2036 | 0.17661 | 0.17905 | 0.047652
Summe von Percent - Heat through chip/Total heat | 0.5311 | 0.54203 | 0.52436 | 0.52653 | 0.56233 | 0.52513 | 0.57092 | 0.55288 | 0.54578 | 0.5925 | 0.55172
Summe von Percent - Heat through workpiece/Total heat | 0.2805 | 0.25644 | 0.29468 | 0.26446 | 0.21775 | 0.24942 | 0.205 | 0.24351 | 0.27761 | 0.22845 | 0.40062
Tool
Work piece
Chip

## Slide 72
Time and spatial varying thermal properties Temperature distribution for hsp = 300 µm, vc = 100 m/min (ABA)
Workpiece position : 34,27 mm
Workpiece position : 80 mm
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
Chart: 
| 320.0 | 280.0 | 240.0 | 200.0
 | 279.0333 | 394.3367 | 521.4622 | 625.6618
Chart: 
| 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
 | 269.089 | 148.0405 | 118.6223 | 102.7499 | 121.9189 | 134.1162
[°C]
[°C]

## Slide 73: Time and spatial varying thermal properties Heat partition ratios for hsp = 300 µm, vc = 150 m/min (ABA)
Chart: Workpiece position [mm]
| 26,65 | 34,27 | 41,89 | 49,51 | 57,13 | 64,76 | 72,38 | 80,00
Summe von Percent - Heat inside tool/Total heat | 0.16439 | 0.16339 | 0.1566 | 0.16335 | 0.14065 | 0.17114 | 0.19318 | 0.14196
Summe von Percent - Heat through chip/Total heat | 0.52306 | 0.50865 | 0.49861 | 0.52469 | 0.52274 | 0.52479 | 0.50377 | 0.55316
Summe von Percent - Heat through workpiece/Total heat | 0.31255 | 0.32796 | 0.34478 | 0.31196 | 0.33661 | 0.30407 | 0.30305 | 0.30488
Tool
Work piece
Chip

## Slide 74
Time and spatial varying thermal properties Temperature distribution for hsp = 300 µm, vc = 150 m/min (ABA)
Workpiece position : 34,27 mm
Workpiece position : 80 mm
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
Chart: 
| 360.0 | 320.0 | 280.0 | 240.0 | 200.0
 | 267.2732 | 415.2822 | 657.1116 | 685.0424 | 806.4234
Chart: 
| 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
 | 4.409 | 110.5122 | 213.6097 | 276.3639 | 318.2904 | 362.6025 | 444.8879 | 531.3348 | 645.5502
[°C]
[°C]

## Slide 75: Gliederung
Influence of uncut chip thickness and cutting velocity
4.2
Time and spatial varying thermal properties
4.1
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 76: Influence of uncut chip thickness and cutting velocity Workpiece position 34 mm (ACF)
Chart: Heat flow (chip) [W]
| 100,00 | 150,00
200,00 | 963.4712 | 1409.6175
300,00 | 1334.4974 | 2211.4647
Chart: Heat flow (tool) [W]
| 100,00 | 150,00
200,00 | 385.5974 | 603.7772
300,00 | 493.2403 | 788.1397
Chart: Heat flow (workpiece) [W]
| 100,00 | 150,00
200,00 | 324.764 | 546.8293
300,00 | 470.4923 | 354.9887
Chart: Heat partition (chip)
| 100,00 | 150,00
200,00 | 0.57561 | 0.55058
300,00 | 0.58066 | 0.65923
Chart: Heat partition (tool)
| 100,00 | 150,00
200,00 | 0.23037 | 0.23583
300,00 | 0.21462 | 0.23494
Chart: Heat partition (workpiece)
| 100,00 | 150,00
200,00 | 0.19402 | 0.21359
300,00 | 0.20472 | 0.10582
ap = 2,8 mm, = 6°, = 3°, = 66 µm, normalized, uncoated, workpiece position: 34mm

## Slide 77: Influence of uncut chip thickness and cutting velocity Workpiece position 80 mm (ACF)
Chart: Heat flow (chip) [W]
| 100,00 | 150,00
100,00 | 522.0725
200,00 | 1151.3422 | 1737.7919
300,00 | 1658.4424 | 2501.462
Chart: Heat flow (tool) [W]
| 100,00 | 150,00
100,00 | 109.3694
200,00 | 136.4207 | 313.8649
300,00 | 140.8039 | 542.6406
Chart: Heat flow (workpiece) [W]
| 100,00 | 150,00
100,00 | 317.2984
200,00 | 398.4663 | 515.1814
300,00 | 487.2191 | 324.9092
Chart: Heat partition (chip)
| 100,00 | 150,00
100,00 | 0.55028
200,00 | 0.68279 | 0.67702
300,00 | 0.72533 | 0.74249
Chart: Heat partition (tool)
| 100,00 | 150,00
100,00 | 0.11528
200,00 | 0.080903 | 0.12228
300,00 | 0.061581 | 0.16107
Chart: Heat partition (workpiece)
| 100,00 | 150,00
100,00 | 0.33444
200,00 | 0.23631 | 0.20071
300,00 | 0.21309 | 0.09644
ap = 2,8 mm, = 6°, = 3°, = 66 µm, normalized, uncoated, workpiece position: 80 mm

## Slide 78: Influence of uncut chip thickness and cutting velocity Workpiece position 34 mm (ABA)
Chart: Heat partition (workpiece)
| 100,00 | 150,00
200,00 | 0.18897 | 0.23523
300,00 | 0.25644 | 0.32796
Chart: Heat flow (chip) [W]
| 100,00 | 150,00
200,00 | 1041.6505 | 1492.3547
300,00 | 1564.0366 | 2233.4372
Chart: Heat flow (tool) [W]
| 100,00 | 150,00
200,00 | 545.5842 | 604.9081
300,00 | 581.5204 | 717.4364
Chart: Heat flow (workpiece) [W]
| 100,00 | 150,00
200,00 | 369.8375 | 645.0666
300,00 | 739.9544 | 1440.0645
Chart: Heat partition (tool)
| 100,00 | 150,00
200,00 | 0.27878 | 0.22058
300,00 | 0.20153 | 0.16339
Chart: Heat partition (chip)
| 100,00 | 150,00
200,00 | 0.53225 | 0.54419
300,00 | 0.54203 | 0.50865
ap = 2,8 mm, = 6°, = 3°, = 66 µm, tempered, uncoated, workpiece position: 34 mm

## Slide 79: Influence of uncut chip thickness and cutting velocity Workpiece position 80 mm (ABA)
Chart: Heat partition (workpiece)
| 100,00 | 150,00
200,00 | 0.39681 | 0.26394
300,00 | 0.40062 | 0.30488
Chart: Heat flow (chip) [W]
| 100,00 | 150,00
200,00 | 979.5612 | 1664.4079
300,00 | 1574.3611 | 2434.1194
Chart: Heat flow (tool) [W]
| 100,00 | 150,00
200,00 | 196.1034 | 359.8966
300,00 | 135.9759 | 624.6815
Chart: Heat flow (workpiece) [W]
| 100,00 | 150,00
200,00 | 773.4107 | 725.8956
300,00 | 1143.1922 | 1341.5808
Chart: Heat partition (tool)
| 100,00 | 150,00
200,00 | 0.10061 | 0.13086
300,00 | 0.047652 | 0.14196
Chart: Heat partition (chip)
| 100,00 | 150,00
200,00 | 0.50258 | 0.6052
300,00 | 0.55172 | 0.55316
ap = 2,8 mm, = 6°, = 3°, = 66 µm, tempered, uncoated, workpiece position: 80 mm