## Slide 1: Results – Method 3
Experimental investigation of temperatures and heat flows for orthogonal cutting 1045 steel by thermal imaging

## Slide 2: Gliederung
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 3: Gliederung
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 4: Experimental Setup Design of Experiment
Thermal camera
Workpiece
Tool
Cutting process
Area covered by the thermal camera

## Slide 5: Experimental Setup Design of Experiment for AISI 1045
Experiments | Cutting Velocity [m/min] | Uncut chip thickness [µm] | Integration time [µs] | Cutting Force [N] | Passive Force [N] | Heat treatment | Contact length [mm]
VP41_1_H200_V100_C45_MF_425 | 100 | 200 | 425 | 1500 | 1000 | Normalized | 1,54
VP41_2_H200_V100_C45_MF_425 | 100 | 200 | 425 | 1565 | 1005 | Normalized | 1,59
VP42_1_H300_V100_C45_MF_425 | 100 | 300 | 425 | 2250 | 1159 | Normalized | 1,84
VP42_2_H300_V100_C45_MF_285 | 100 | 300 | 285 | 2136 | 1079 | Normalized | 1,9
VP43_1_H400_V100_C45_MF_285 | 100 | 400 | 285 | 2716 | 1118 | Normalized | 2,06
VP45_2_H200_V150_C45_MF_425 | 150 | 200 | 425 | 1448 | 688 | Normalized | 1,72
VP46_1_H300_V150_C45_MF_285 | 150 | 300 | 285 | 2006 | 801 | Normalized | 2,05
VP46_2_H300_V150_C45_MF_285 | 150 | 300 | 285 | 2004 | 875 | Normalized | 2,09
VP49_1_H400_V150_C45_MF_285 | 150 | 400 | 285 | 2675 | 1046 | Normalized | 2,27
VP49_2_H400_V150_C45_MF_285 | 150 | 400 | 285 | 2590 | 1000 | Normalized | 2,32
VP50_1_H500_V150_C45_MF_285 | 150 | 500 | 285 | 3220 | 1120 | Normalized | 2,51
VP50_2_H500_V150_C45_MF_285 | 150 | 500 | 285 | 3178 | 1162 | Normalized | 2,41

## Slide 6: Experimental Setup Boundary Conditions for AISI 1045
Boundary Conditions |  |  |  |  | 
Tool |  | Camera |  | Workpiece | 
Heat Conductivity [W/(mK)] | 75,4 | Pixel pitch (Infrared Camera) [mm/pixel] | 0,015 | Length of the workpiece [mm] | 200
Heat Capacity [J/(cm^3K)] | Interpolation* | Maximum digit level valid (FLIR X) | 8192 | Heat Capacity [J/(kgK)] | Interpolation**
Rake Angle [°] | 6 | Maximum digit level valid (FLIR SC7600) | 16000 | Workpiece Material | AISI 1045 (normalized)
Clearance Angle [°] | 3 | Frame Rate (Infrared Camera) [Hz] | 328 | Depth of Cut ap [mm] | 3,5
Assumed percentage of heat conducted away by convection and radiation | 0,03 | Minimum valid temperature for the frames [°C] | 200 | Maximum error of the workpiece position for = 100 [mm/mm] | 0,0255
Cutting edge radius [µm] | < 5 | Emissivity (Experimentally determined - tool and workpiece coated) | 0,85 | Maximum error of the workpiece position for = 150 [mm/mm] | 0,038
 |  |  |  | Percentage of the deformation energy converted into heat | 0,9
 |  |  |  | Density (based on steel) [kg/m^3] | 7874
Boundary Conditions |  |  |  |  | 
Tool |  | Camera |  | Workpiece | 
Heat Conductivity [W/(mK)] | 75,4 | Pixel pitch (Infrared Camera) [mm/pixel] | 0,015 | Length of the workpiece [mm] | 200
Heat Capacity [J/(cm^3K)] | Interpolation* | Maximum digit level valid (FLIR X) | 8192 | Heat Capacity [J/(kgK)] | Interpolation**
Rake Angle [°] | 6 | Maximum digit level valid (FLIR SC7600) | 16000 | Workpiece Material | AISI 1045 (normalized)
Clearance Angle [°] | 3 | Frame Rate (Infrared Camera) [Hz] | 328 | Depth of Cut ap [mm] | 3,5
Assumed percentage of heat conducted away by convection and radiation | 0,03 | Minimum valid temperature for the frames [°C] | 200 |  | 0,0255
Cutting edge radius [µm] | < 5 | Emissivity (Experimentally determined - tool and workpiece coated) | 0,85 |  | 0,038
 |  |  |  | Percentage of the deformation energy converted into heat | 0,9
 |  |  |  | Density (based on steel) [kg/m^3] | 7874
*Tool [J/(cm^3K)] |  | 
**Workpiece [J/(kgK)] |  | 
Interpolation

## Slide 7: Experimental Setup Heat capacity data
Tool Material |  |  | Workpiece Material |  |  | 
Temperature [°C] | Heat Capacity [J/(cm³K)] | Heat Conductivity [W/(mK)] | Temperature [°C] | Heat Capacity [J/(kgK)] | Heat Conductivity [W/(mK)] | Density [Kg/m³]
20 | 3,2 | 100 | 20 | 474,62 | 48,03 | 7820,9
100 | 3,24 | 94,8 | 100 | 487,94 | 47,21 | 7794,3
200 | 3,59 | 88,3 | 200 | 501,2 | 45,82 | 7764,2
300 | 3,79 | 81,9 | 300 | 521,29 | 42,74 | 7732
400 | 3,9 | 75,4 | 400 | 545,69 | 39,1 | 7697,4
500 | 3,97 | 68,9 | 500 | 572,7 | 35,35 | 7660,4
600 | 4,05 | 66,7 | 600 | 601,83 | 31,73 | 7620,9
700 | 4,14 | 64,8 | 700 | 632,89 | 28,33 | 7578,7
 |  |  | 800 | 696,29 | 23,52 | 7579,4
 |  |  | 900 | 693,79 | 25,25 | 7528,3
 |  |  | 1000 | 691,3 | 26,61 | 7475
 |  |  | 1100 | 688,81 | 27,9 | 7419,7
 |  |  | 1200 | 686,34 | 29,34 | 7362,3
*Data base for interpolation

## Slide 8: Gliederung
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 9: Post processing of thermal pictures Energy balance in the volume control
Tool
Workpiece
Control volume
Inside Energy
Total power produced
  Direct force measurement
Energy from material going inside the control volume
  Always zero ()
Outside Energy
Heat flow into the tool
  Calculation by gradient
Heat flow into the workpiece
  Calculation by heat balance
Energy from the chip going outside
  thermodynamic calculation
Part of deformation energy converted in heat
  90% of the total deformation energy ()
***,
Chip
End of contact
Notes: In this analysis, the energy flows considered for the volume control are listed above. Then, with the temperature field of the Infrared camera frames, this analysis is able to calculate the heat flow through the tool and the chip and, consequently, the heat partition of the total power produced during the process. About 90% of the deformation energy is converted in heat and the heat flow through the workpiece is calculated by the total balance.

## Slide 10: Post processing of thermal pictures Heat carried away from the tool tip
The heat flow through the tool is calculated as a mean value between the heat flows calculated for the last two isothermals.
Method based on [BOOTHROYD].
  : heat conductivity
  : length of the isothermal
  : temperature gradient normal to line
  : effective tool width
Tool

## Slide 11: Post processing of thermal pictures Temperature gradient – calculation method
Each line along the tool is consisted of pixels, and each pixel has a corresponding temperature ().
Gradients for the red pixel on the x () and y () directions:
The resultant vector for and is normal to the isotherm line on the pixel that it was calculated. So, the total gradient that crosses the line is:
Tool
Isothermal line

## Slide 12: Post processing of thermal pictures Heat carried away by the chip
Tool
Chip
End of contact chip - tool
The heat flow is calculated on the end of contact between chip and tool interfaces
Method based on [BOOTHROYD].
  : heat capacity function
  : chip temperature
  : environment temperature
  : velocity of the chip
  : chip thickness
  : chip width

## Slide 13: Gliederung
Influence of uncut chip thickness and cutting velocity
3.2
Time and spatial varying thermal properties
3.1
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 14: Time and spatial varying thermal properties Temperature at tool tip [°C] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 323.5206 | 271.9162 | 380.5434 | 341.2377 | 357.2232 | 368.2788 | 230.1309 | 364.6832 | 365.8805 | 343.2452 | 364.6607 | 379.6024 | 393.9241 | 390.0437 | 373.423 | 398.9011 | 411.4206 | 425.8531
VP42_1_H300_V100_C45_MF_425 | 442.907 | 491.0974 | 498.6279 | 450.6018 | 444.4791 | 340.6401 | 471.2703 | 433.7598 | 426.1506 | 282.3214 | 323.3509 | 255.7746 | 504.0463 | 485.6611 | 516.0332 | 517.7154 | 520.8733 | 525.9864
VP45_2_H200_V150_C45_MF_425 | 363.7171 | 378.5227 | 387.0074 | 395.5219 | 410.6586 | 412.4561 | 402.5545 | 408.8741 | 411.6293 | 408.0815 | 415.8895 | 415.7033 | 420.948 | 444.6016 | 447.3969 | 461.0162 | 447.4671 | 441.2219
VP46_1_H300_V150_C45_MF_285 | 425.3031 | 385.6967 | 416.9808 | 388.6194 | 419.6816 | 428.1679 | 436.2967 | 452.2375 | 437.1667 | 384.2404 | 438.4321 | 320.4099 | 442.1594 | 492.6639 | 486.9684 | 492.3859 | 488.9218 | 505.5068
VP49_1_H400_V150_C45_MF_285 | 414.4026 | 414.7684 | 441.6356 | 253.9839 | 421.9092 | 485.0291 | 476.3299 | 470.3219 | 416.562 | 469.1423 | 474.6055 | 474.9649 | 493.8176 | 495.579 | 514.8465 | 506.6511 | 489.6865 | 469.3475
VP50_1_H500_V150_C45_MF_285 | 412.4521 | 377.9897 | 447.9103 | 416.5194 | 457.2466 | 439.4002 | 506.3999 | 468.2151 | 457.8948 | 424.7005 | 430.3532 | 477.8122 | 511.4966 | 514.4709 | 502.4442 | 486.0228 | 490.5698 | 473.5951

## Slide 15: Time and spatial varying thermal properties Internal energy in tool [Joule] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 6.5224 | 6.7965 | 7.0719 | 7.3539 | 7.8868 | 8.1574 | 7.964 | 8.4782 | 8.7992 | 9.1514 | 9.4147 | 9.5462 | 9.7156 | 9.9526 | 9.8572 | 10.3038 | 10.4344 | 10.4692
VP42_1_H300_V100_C45_MF_425 | 8.6795 | 8.9284 | 9.2325 | 9.6003 | 10.0522 | 10.2113 | 10.5446 | 10.7162 | 10.8376 | 10.3466 | 10.6856 | 11.1312 | 11.4614 | 11.5732 | 12.7034 | 12.9454 | 13.1586 | 13.3152
VP45_2_H200_V150_C45_MF_425 | 1.5376 | 1.7419 | 1.9444 | 2.1819 | 2.4671 | 2.7856 | 3.1359 | 3.5036 | 3.8728 | 4.1878 | 4.4347 | 4.6127 | 4.8247 | 5.0665 | 5.3337 | 5.7504 | 6.1824 | 6.4363
VP46_1_H300_V150_C45_MF_285 | 2.5631 | 2.8266 | 3.1545 | 3.4264 | 3.8378 | 4.3676 | 4.87 | 5.4523 | 5.947 | 6.3015 | 6.4102 | 6.6173 | 6.1817 | 7.25 | 7.6531 | 8.1454 | 8.6188 | 8.84
VP49_1_H400_V150_C45_MF_285 | 5.0798 | 5.5896 | 6.1222 | 6.2829 | 6.9385 | 7.5386 | 8.1279 | 8.7742 | 9.371 | 9.8999 | 10.1846 | 10.3374 | 10.5043 | 10.7092 | 11.0906 | 11.6349 | 12.2059 | 12.4869
VP50_1_H500_V150_C45_MF_285 | 6.23 | 6.8538 | 7.3979 | 7.8002 | 8.2048 | 8.7882 | 9.527 | 10.2283 | 11.0142 | 11.6462 | 12.0316 | 12.2152 | 12.3571 | 12.5159 | 12.8927 | 13.4692 | 14.2166 | 14.6323
Notes: The higher the chip thickness the higher the internal energy/heat rate
The lower the cutting speed the higher the internal energy in the tool  High Speed cutting

## Slide 16: Time and spatial varying thermal properties Internal energy rate of the tool [W] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 81.2563 | 81.2563 | 81.2563 | 81.2563 | 81.2563 | 81.2563 | 81.2563 | 81.2563 | 81.2563 | 81.2563 | 81.2563 | 81.2563 | 81.2563 | 81.2563 | 81.2563 | 81.2563 | 81.2563 | 81.2563
VP42_1_H300_V100_C45_MF_425 | 89.3678 | 89.3678 | 89.3678 | 89.3678 | 89.3678 | 89.3678 | 89.3678 | 89.3678 | 89.3678 | 89.3678 | 89.3678 | 89.3678 | 89.3678 | 89.3678 | 89.3678 | 89.3678 | 89.3678 | 89.3678
VP45_2_H200_V150_C45_MF_425 | 98.0306 | 98.0306 | 98.0306 | 98.0306 | 98.0306 | 98.0306 | 98.0306 | 98.0306 | 98.0306 | 98.0306 | 98.0306 | 98.0306 | 98.0306 | 98.0306 | 98.0306 | 98.0306 | 98.0306 | 98.0306
VP46_1_H300_V150_C45_MF_285 | 123.8518 | 123.8518 | 123.8518 | 123.8518 | 123.8518 | 123.8518 | 123.8518 | 123.8518 | 123.8518 | 123.8518 | 123.8518 | 123.8518 | 123.8518 | 123.8518 | 123.8518 | 123.8518 | 123.8518 | 123.8518
VP49_1_H400_V150_C45_MF_285 | 143.3393 | 143.3393 | 143.3393 | 143.3393 | 143.3393 | 143.3393 | 143.3393 | 143.3393 | 143.3393 | 143.3393 | 143.3393 | 143.3393 | 143.3393 | 143.3393 | 143.3393 | 143.3393 | 143.3393 | 143.3393
VP50_1_H500_V150_C45_MF_285 | 163.4899 | 163.4899 | 163.4899 | 163.4899 | 163.4899 | 163.4899 | 163.4899 | 163.4899 | 163.4899 | 163.4899 | 163.4899 | 163.4899 | 163.4899 | 163.4899 | 163.4899 | 163.4899 | 163.4899 | 163.4899
Notes: Heating rate rises with chip thickness
Heating rate decreases with cutting speed
H/v  Heating rate
1,33
2
4
2
3
2,66
3,333

## Slide 17: Time and spatial varying thermal properties Total Power [W] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 2383.9299 | 2383.9299 | 2392.0116 | 2383.9299 | 2383.9299 | 2400.3862 | 2413.5811 | 2404.695 | 2396.1601 | 2409.0915 | 2396.1601 | 2392.0116 | 2383.9299 | 2383.9299 | 2383.9299 | 2379.9881 | 2379.9881 | 2379.9881
VP42_1_H300_V100_C45_MF_425 | 3431.2778 | 3406.0346 | 3396.5504 | 3396.5504 | 3396.5504 | 3396.5504 | 3426.0318 | 3410.8975 | 3436.6351 | 3426.0318 | 3401.2539 | 3406.0346 | 3426.0318 | 3426.0318 | 3406.0346 | 3431.2778 | 3431.2778 | 3396.5504
VP45_2_H200_V150_C45_MF_425 | 3284.1203 | 3271.1632 | 3271.1632 | 3271.1632 | 3288.5908 | 3271.1632 | 3284.1203 | 3302.5261 | 3297.7883 | 3293.1451 | 3288.5908 | 3284.1203 | 3284.1203 | 3302.5261 | 3302.5261 | 3307.3644 | 3275.411 | 3271.1632
VP46_1_H300_V150_C45_MF_285 | 4511.6553 | 4511.6553 | 4511.6553 | 4538.128 | 4538.128 | 4549.4256 | 4543.7199 | 4511.6553 | 4555.2523 | 4511.6553 | 4521.9706 | 4521.9706 | 4511.6553 | 4521.9706 | 4549.4256 | 4511.6553 | 4538.128 | 4511.6553
VP49_1_H400_V150_C45_MF_285 | 6020.0784 | 6070.5515 | 6062.9091 | 6062.9091 | 6033.8354 | 6033.8354 | 6033.8354 | 6062.9091 | 6055.4253 | 6055.4253 | 6070.5515 | 6055.4253 | 6013.3686 | 6020.0784 | 6026.8984 | 6033.8354 | 6062.9091 | 6040.897
VP50_1_H500_V150_C45_MF_285 | 7266.3769 | 7242.6514 | 7220.16 | 7220.16 | 7220.16 | 7274.601 | 7250.4115 | 7220.16 | 7220.16 | 7220.16 | 7282.9994 | 7250.4115 | 7266.3769 | 7235.0281 | 7250.4115 | 7274.601 | 7258.317 | 7266.3769

## Slide 18: Time and spatial varying thermal properties Internal energy carried away by chip [W] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 1446.9037 | 1500.714 | 1451.366 | 1450.7175 | 1523.3013 | 1526.934 | 1392.793 | 1493.1362 | 1594.0554 | 1427.9538 | 1554.7901 | 1602.5165 | 1624.0372 | 1635.069 | 1589.2306 | 1724.2013 | 1825.9456 | 1704.9593
VP42_1_H300_V100_C45_MF_425 | 2227.4118 | 2165.4074 | 2208.0209 | 2199.885 | 2261.3844 | 2203.7899 | 2195.2405 | 2222.4003 | 2237.2376 | 2244.5721 | 2246.1977 | 2273.3784 | 2258.7944 | 2343.3527 | 2365.7067 | 2380.7834 | 2543.5444 | 2526.242
VP45_2_H200_V150_C45_MF_425 | 2211.1666 | 2131.5983 | 2135.074 | 2141.749 | 2208.7243 | 2215.9191 | 2195.4285 | 2209.5729 | 2208.4354 | 2167.633 | 2166.4547 | 2117.3798 | 2194.5496 | 2264.3116 | 2267.3972 | 2317.1508 | 2414.638 | 2425.7515
VP46_1_H300_V150_C45_MF_285 | 3086.5735 | 3075.8261 | 3108.6092 | 3077.5016 | 3148.4235 | 3128.8205 | 3066.2035 | 3055.4101 | 3081.729 | 3082.416 | 3094.5335 | 3131.2069 | 3135.8375 | 3145.0925 | 3184.8716 | 3226.8478 | 3394.0747 | 3375.8082
VP49_1_H400_V150_C45_MF_285 | 3703.6478 | 3636.3396 | 3744.3018 | 3768.0535 | 3889.5999 | 4034.6229 | 3975.9522 | 4006.6247 | 3828.9325 | 3860.761 | 3944.7605 | 3892.4492 | 3953.3381 | 3900.7334 | 3935.8881 | 3961.3381 | 4063.606 | 4015.3245
VP50_1_H500_V150_C45_MF_285 | 4552.4075 | 4621.685 | 4751.0572 | 4866.2372 | 5104.8332 | 5095.3821 | 5000.6533 | 4892.1433 | 4847.5272 | 4814.495 | 4792.0381 | 4843.6789 | 4845.0776 | 4887.454 | 5004.1952 | 5045.1906 | 5110.3196 | 4981.0634
Notes: Heat carried away by chip rises with hsp*vc
Heat carried away by chip increases with cutting length for small chip thickness
Why?????
vc* hsp ~ chip ; lc ↑ → chip = const. (gilt nicht für Vp41 , VP42)
chip ↑ → Bchip ↑ (für Vp41 , VP42)
vc* hsp ~ ( 𝒒) ̇^´chip ; lc ↑ → ( 𝒒) ̇^´chip = const. (gilt nicht für Vp41 , VP42)
( 𝒒) ̇^´chip ↑ → Bchip ↑ (für Vp41 , VP42)

## Slide 19: Time and spatial varying thermal properties Heat partition to the chip for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 0.60694 | 0.62951 | 0.60676 | 0.60854 | 0.63899 | 0.63612 | 0.57706 | 0.62093 | 0.66525 | 0.59274 | 0.64887 | 0.66995 | 0.68124 | 0.68587 | 0.66664 | 0.72446 | 0.76721 | 0.71637
VP42_1_H300_V100_C45_MF_425 | 0.64915 | 0.63576 | 0.65008 | 0.64768 | 0.66579 | 0.64883 | 0.64075 | 0.65156 | 0.651 | 0.65515 | 0.6604 | 0.66746 | 0.6593 | 0.68398 | 0.69456 | 0.69385 | 0.74128 | 0.74377
VP45_2_H200_V150_C45_MF_425 | 0.67329 | 0.65163 | 0.6527 | 0.65474 | 0.67163 | 0.67741 | 0.6685 | 0.66906 | 0.66967 | 0.65823 | 0.65878 | 0.64473 | 0.66823 | 0.68563 | 0.68656 | 0.7006 | 0.7372 | 0.74156
VP46_1_H300_V150_C45_MF_285 | 0.68413 | 0.68175 | 0.68902 | 0.67814 | 0.69377 | 0.68774 | 0.67482 | 0.67723 | 0.67652 | 0.68321 | 0.68433 | 0.69244 | 0.69505 | 0.69551 | 0.70006 | 0.71522 | 0.7479 | 0.74824
VP49_1_H400_V150_C45_MF_285 | 0.61522 | 0.59901 | 0.61758 | 0.62149 | 0.64463 | 0.66867 | 0.65894 | 0.66084 | 0.63231 | 0.63757 | 0.64982 | 0.6428 | 0.65742 | 0.64795 | 0.65305 | 0.65652 | 0.67024 | 0.66469
VP50_1_H500_V150_C45_MF_285 | 0.6265 | 0.63812 | 0.65803 | 0.67398 | 0.70702 | 0.70043 | 0.68971 | 0.67757 | 0.67139 | 0.66681 | 0.65798 | 0.66806 | 0.66678 | 0.67553 | 0.69019 | 0.69354 | 0.70406 | 0.68549
Notes: No influence of level of heat partition inside the chip by chip thickness
Rising heat partition inside the chip, especially for lower chip thickness  Hypo: tool is heating up and is conducts less heat away
Hypo: The lower the chip thickness the lower the influence of friction at the rake face
1 = Bchip + Btool + BWP
Btool = konst. ; Bchip ↑ → BWP ↓

## Slide 20: Time and spatial varying thermal properties Heat flow into the tool [W] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 296.7308 | 285.0898 | 271.4271 | 251.3813 | 239.1616 | 225.3367 | 222.8657 | 211.0822 | 207.3911 | 204.4271 | 198.6509 | 194.1535 | 190.0542 | 187.7385 | 186.3446 | 184.8568 | 181.847 | 181.5074
VP42_1_H300_V100_C45_MF_425 | 240.7143 | 225.4677 | 215.0172 | 212.5696 | 211.5558 | 209.6329 | 203.7713 | 199.2611 | 196.3132 | 201.6313 | 191.2401 | 188.3152 | 184.299 | 192.1077 | 187.4606 | 187.7868 | 186.9708 | 185.1207
VP45_2_H200_V150_C45_MF_425 | 666.4566 | 693.6177 | 650.613 | 585.8999 | 563.6151 | 532.6492 | 538.6694 | 524.3068 | 512.2306 | 485.1009 | 397.314 | 326.7697 | 289.6577 | 259.1433 | 249.9004 | 245.2318 | 253.6974 | 215.2119
VP46_1_H300_V150_C45_MF_285 | 761.3751 | 709.8275 | 626.913 | 438.5668 | 385.1048 | 415.0474 | 453.6587 | 507.8638 | 498.8761 | 445.4664 | 392.7979 | 344.7096 | 314.509 | 296.421 | 287.4633 | 301.3534 | 297.6066 | 292.6013
VP49_1_H400_V150_C45_MF_285 | 657.3361 | 640.9174 | 634.6521 | 563.079 | 538.4333 | 532.4081 | 526.1402 | 538.1241 | 567.2921 | 554.7518 | 485.2432 | 455.7353 | 408.0721 | 371.7731 | 351.8103 | 349.1599 | 345.3738 | 309.5919
VP50_1_H500_V150_C45_MF_285 | 695.0366 | 678.7571 | 659.9735 | 575.4805 | 510.1921 | 498.9458 | 504.1942 | 503.1715 | 482.4206 | 468.1789 | 438.0328 | 399.2551 | 364.6854 | 340.7688 | 323.8124 | 328.4409 | 327.9524 | 311.0184

## Slide 21: Time and spatial varying thermal properties Heat flow into the tool [W] for different vc and hsp 2
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_1_H200_V100_C45_MF_425 | 354.025 | 317.8978 | 303.864 | 295.6485 | 281.1588 | 272.6297 | 249.5201 | 238.501 | 230.6826 | 223.8934 | 219.9017 | 213.7972 | 209.9211 | 206.5222 | 203.9027 | 200.3398 | 197.3643 | 196.3237
VP41_2_H200_V100_C45_MF_425 | 296.7308 | 285.0898 | 271.4271 | 251.3813 | 239.1616 | 225.3367 | 222.8657 | 211.0822 | 207.3911 | 204.4271 | 198.6509 | 194.1535 | 190.0542 | 187.7385 | 186.3446 | 184.8568 | 181.847 | 181.5074
VP42_1_H300_V100_C45_MF_425 | 240.7143 | 225.4677 | 215.0172 | 212.5696 | 211.5558 | 209.6329 | 203.7713 | 199.2611 | 196.3132 | 201.6313 | 191.2401 | 188.3152 | 184.299 | 192.1077 | 187.4606 | 187.7868 | 186.9708 | 185.1207
VP45_2_H200_V150_C45_MF_425 | 666.4566 | 693.6177 | 650.613 | 585.8999 | 563.6151 | 532.6492 | 538.6694 | 524.3068 | 512.2306 | 485.1009 | 397.314 | 326.7697 | 289.6577 | 259.1433 | 249.9004 | 245.2318 | 253.6974 | 215.2119
VP46_1_H300_V150_C45_MF_285 | 761.3751 | 709.8275 | 626.913 | 438.5668 | 385.1048 | 415.0474 | 453.6587 | 507.8638 | 498.8761 | 445.4664 | 392.7979 | 344.7096 | 314.509 | 296.421 | 287.4633 | 301.3534 | 297.6066 | 292.6013
VP46_2_H300_V150_C45_MF_285 | 778.9238 | 733.7627 | 702.412 | 518.9932 | 389.3844 | 397.4375 | 426.4725 | 488.566 | 501.3785 | 507.2428 | 404.4267 | 378.3801 | 336.3305 | 304.3469 | 295.4198 | 306.3993 | 310.4842 | 298.6851
VP49_1_H400_V150_C45_MF_285 | 657.3361 | 640.9174 | 634.6521 | 563.079 | 538.4333 | 532.4081 | 526.1402 | 538.1241 | 567.2921 | 554.7518 | 485.2432 | 455.7353 | 408.0721 | 371.7731 | 351.8103 | 349.1599 | 345.3738 | 309.5919
VP49_2_H400_V150_C45_MF_285 | 672.7332 | 668.4006 | 637.4501 | 529.6212 | 495.0194 | 491.3911 | 490.8974 | 534.2497 | 526.7908 | 500.0742 | 467.8841 | 422.6231 | 377.9773 | 355.1405 | 337.0202 | 326.1294 | 342.1555 | 301.5085
VP50_1_H500_V150_C45_MF_285 | 695.0366 | 678.7571 | 659.9735 | 575.4805 | 510.1921 | 498.9458 | 504.1942 | 503.1715 | 482.4206 | 468.1789 | 438.0328 | 399.2551 | 364.6854 | 340.7688 | 323.8124 | 328.4409 | 327.9524 | 311.0184
VP50_2_H500_V150_C45_MF_285 | 707.875 | 686.7554 | 661.0773 | 590.4186 | 533.607 | 526.463 | 512.3632 | 529.1135 | 489.0438 | 493.7701 | 455.682 | 403.5326 | 367.61 | 347.0516 | 333.6189 | 333.6806 | 333.2732 | 313.9374
Notes: For small chip thickness no influence of cutting speed
Heat flux into the tool rises with chip thickness decreasingly,
Less rise for smaller cutting speeds
Decreases for higher chip thickness over time constant for small chip thickness hypo: tool gets to hot to carry heat away
Hypo: The higher the chip thickness the higher the frictional influence
Thermal number? Vc *hsp??

## Slide 22: Time and spatial varying thermal properties Heat partition into the tool for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 0.12447 | 0.11959 | 0.11347 | 0.10545 | 0.10032 | 0.093875 | 0.092338 | 0.087779 | 0.086551 | 0.084856 | 0.082904 | 0.081167 | 0.079723 | 0.078752 | 0.078167 | 0.077671 | 0.076407 | 0.076264
VP42_1_H300_V100_C45_MF_425 | 0.070153 | 0.066197 | 0.063305 | 0.062584 | 0.062285 | 0.061719 | 0.059477 | 0.058419 | 0.057124 | 0.058853 | 0.056226 | 0.055289 | 0.053794 | 0.056073 | 0.055038 | 0.054728 | 0.05449 | 0.054503
VP45_2_H200_V150_C45_MF_425 | 0.20293 | 0.21204 | 0.19889 | 0.17911 | 0.17138 | 0.16283 | 0.16402 | 0.15876 | 0.15533 | 0.14731 | 0.12082 | 0.0995 | 0.088199 | 0.078468 | 0.075669 | 0.074147 | 0.077455 | 0.065791
VP46_1_H300_V150_C45_MF_285 | 0.16876 | 0.15733 | 0.13895 | 0.09664 | 0.08486 | 0.091231 | 0.099843 | 0.11257 | 0.10952 | 0.098737 | 0.086864 | 0.07623 | 0.06971 | 0.065551 | 0.063187 | 0.066794 | 0.065579 | 0.064855
VP49_1_H400_V150_C45_MF_285 | 0.10919 | 0.10558 | 0.10468 | 0.092873 | 0.089236 | 0.088237 | 0.087198 | 0.088757 | 0.093683 | 0.091612 | 0.079934 | 0.075261 | 0.067861 | 0.061756 | 0.058373 | 0.057867 | 0.056965 | 0.051249
VP50_1_H500_V150_C45_MF_285 | 0.095651 | 0.093717 | 0.091407 | 0.079705 | 0.070662 | 0.068587 | 0.06954 | 0.06969 | 0.066816 | 0.064843 | 0.060145 | 0.055067 | 0.050188 | 0.0471 | 0.044661 | 0.045149 | 0.045183 | 0.042802
Notes: Heat partition inside tool higher for low cutting speed  Puls
No influence of chip thickness  Puls
Remains constant over time

## Slide 23: Time and spatial varying thermal properties Heat flow into the workpiece [W] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 640.2953 | 598.1261 | 669.2185 | 681.831 | 621.467 | 648.1155 | 797.9224 | 700.4765 | 594.7136 | 776.7106 | 642.719 | 595.3417 | 569.8385 | 561.1224 | 608.3546 | 470.93 | 372.1954 | 493.5213
VP42_1_H300_V100_C45_MF_425 | 963.1517 | 1015.1595 | 973.5123 | 984.0958 | 923.6102 | 983.1276 | 1027.0199 | 989.2361 | 1003.0843 | 979.8284 | 963.8161 | 944.3409 | 982.9383 | 890.5715 | 852.8673 | 862.7076 | 700.7627 | 685.1877
VP45_2_H200_V150_C45_MF_425 | 406.4971 | 445.9472 | 485.4761 | 543.5142 | 516.2514 | 522.5949 | 550.0224 | 568.6464 | 577.1224 | 640.4111 | 724.822 | 839.9707 | 799.9129 | 779.0713 | 785.2286 | 744.9818 | 607.0756 | 630.1998
VP46_1_H300_V150_C45_MF_285 | 663.7067 | 726.0017 | 776.1331 | 1022.0596 | 1004.5997 | 1005.5577 | 1023.8577 | 948.3814 | 974.6471 | 983.7729 | 1034.6392 | 1046.0541 | 1061.3088 | 1080.457 | 1077.0907 | 983.454 | 846.4467 | 843.2458
VP49_1_H400_V150_C45_MF_285 | 1659.0945 | 1793.2945 | 1683.9552 | 1731.7766 | 1605.8022 | 1466.8044 | 1531.7431 | 1518.1602 | 1659.2007 | 1639.9125 | 1640.5478 | 1707.2408 | 1651.9583 | 1747.5719 | 1739.1999 | 1723.3374 | 1653.9293 | 1715.9807
VP50_1_H500_V150_C45_MF_285 | 2018.9328 | 1942.2092 | 1809.1293 | 1778.4423 | 1605.1346 | 1680.2731 | 1745.564 | 1824.8451 | 1890.2121 | 1937.4861 | 2052.9285 | 2007.4775 | 2056.614 | 2006.8053 | 1922.4038 | 1900.9695 | 1820.045 | 1974.2951
Notes: Heat flux inside work piece decreases with cutting speed and chip thickness
Heat flux into workpiece decreases over cutting length for small chip thickness
How over time?
How is this possible?

## Slide 24: Time and spatial varying thermal properties Heat partition into the workpiece for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 0.26859 | 0.2509 | 0.27977 | 0.28601 | 0.26069 | 0.27 | 0.3306 | 0.2913 | 0.24819 | 0.32241 | 0.26823 | 0.24889 | 0.23903 | 0.23538 | 0.25519 | 0.19787 | 0.15639 | 0.20736
VP42_1_H300_V100_C45_MF_425 | 0.2807 | 0.29805 | 0.28662 | 0.28973 | 0.27193 | 0.28945 | 0.29977 | 0.29002 | 0.29188 | 0.286 | 0.28337 | 0.27726 | 0.2869 | 0.25994 | 0.2504 | 0.25142 | 0.20423 | 0.20173
VP45_2_H200_V150_C45_MF_425 | 0.12378 | 0.13633 | 0.14841 | 0.16615 | 0.15698 | 0.15976 | 0.16748 | 0.17219 | 0.175 | 0.19447 | 0.22041 | 0.25577 | 0.24357 | 0.2359 | 0.23777 | 0.22525 | 0.18534 | 0.19265
VP46_1_H300_V150_C45_MF_285 | 0.14711 | 0.16092 | 0.17203 | 0.22522 | 0.22137 | 0.22103 | 0.22533 | 0.21021 | 0.21396 | 0.21805 | 0.2288 | 0.23133 | 0.23524 | 0.23894 | 0.23675 | 0.21798 | 0.18652 | 0.1869
VP49_1_H400_V150_C45_MF_285 | 0.27559 | 0.29541 | 0.27775 | 0.28563 | 0.26613 | 0.2431 | 0.25386 | 0.2504 | 0.274 | 0.27082 | 0.27025 | 0.28194 | 0.27471 | 0.29029 | 0.28857 | 0.28561 | 0.27279 | 0.28406
VP50_1_H500_V150_C45_MF_285 | 0.27785 | 0.26816 | 0.25057 | 0.24632 | 0.22231 | 0.23098 | 0.24075 | 0.25274 | 0.2618 | 0.26834 | 0.28188 | 0.27688 | 0.28303 | 0.27737 | 0.26514 | 0.26132 | 0.25075 | 0.2717
Notes: Heat partition into workpiece independent from vc and hsp does not fit to K&H
Decreases for small chip thickness

## Slide 25: Time and spatial varying thermal properties Friction coefficient µ for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136
VP42_1_H300_V100_C45_MF_425 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572
VP45_2_H200_V150_C45_MF_425 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074
VP46_1_H300_V150_C45_MF_285 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265
VP49_1_H400_V150_C45_MF_285 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174
VP50_1_H500_V150_C45_MF_285 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012

## Slide 26: Time and spatial varying thermal properties Heat partition ratios for hsp = 200 µm, vc = 100 m/min
Chart: Workpiece position [mm]
| 113,62 | 118,70 | 123,78 | 128,86 | 133,94 | 139,02 | 144,11 | 149,19 | 154,27 | 159,35 | 164,43 | 169,51 | 174,59 | 179,67 | 184,76 | 189,84 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 - Summe von Percent - Heat inside tool/Total heat | 0.12447 | 0.11959 | 0.11347 | 0.10545 | 0.10032 | 0.093875 | 0.092338 | 0.087779 | 0.086551 | 0.084856 | 0.082904 | 0.081167 | 0.079723 | 0.078752 | 0.078167 | 0.077671 | 0.076407 | 0.076264
VP41_2_H200_V100_C45_MF_425 - Summe von Percent - Heat through chip/Total heat | 0.60694 | 0.62951 | 0.60676 | 0.60854 | 0.63899 | 0.63612 | 0.57706 | 0.62093 | 0.66525 | 0.59274 | 0.64887 | 0.66995 | 0.68124 | 0.68587 | 0.66664 | 0.72446 | 0.76721 | 0.71637
VP41_2_H200_V100_C45_MF_425 - Summe von Percent - Heat through workpiece/Total heat | 0.26859 | 0.2509 | 0.27977 | 0.28601 | 0.26069 | 0.27 | 0.3306 | 0.2913 | 0.24819 | 0.32241 | 0.26823 | 0.24889 | 0.23903 | 0.23538 | 0.25519 | 0.19787 | 0.15639 | 0.20736
Tool
Work piece
Chip
VP41_2

## Slide 27: Temperature distribution for orthogonal cutting Temperature distribution for hsp = 200 µm, vc = 100 m/min
[°C]
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
Workpiece position : 124 mm
Workpiece position : 200 mm
Chart: 
| 200.0 | 250.0 | 300.0 | 350.0 | 400.0 | 450.0 | 500.0 | 550.0 | 600.0
Heat flow through the isothermal lines | 339.6816 | 293.7062 | 236.0262 | 172.7628 | 118.4482 | 80.4727 | 50.9191 | 29.5994 | 12.5991
Chart: 
| 200.0 | 250.0 | 300.0 | 350.0 | 400.0 | 450.0 | 500.0 | 550.0 | 600.0
Heat flow through the isothermal lines | 147.5285 | 138.6991 | 126.4536 | 114.534 | 101.7444 | 83.2813 | 58.56 | 34.6065 | 12.2568

## Slide 28: Time and spatial varying thermal properties Heat partition ratios for hsp = 200 µm, vc = 150 m/min
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 116,16 | 123,78 | 131,40 | 139,02 | 146,65 | 154,27 | 161,89 | 169,51 | 177,13 | 184,76 | 192,38 | 200,00
VP45_2_H200_V150_C45_MF_425 - Summe von Percent - Heat inside tool/Total heat | 0.20293 | 0.21204 | 0.19889 | 0.17911 | 0.17138 | 0.16283 | 0.16402 | 0.15876 | 0.15533 | 0.14731 | 0.12082 | 0.0995 | 0.088199 | 0.078468 | 0.075669 | 0.074147 | 0.077455 | 0.065791
VP45_2_H200_V150_C45_MF_425 - Summe von Percent - Heat through chip/Total heat | 0.67329 | 0.65163 | 0.6527 | 0.65474 | 0.67163 | 0.67741 | 0.6685 | 0.66906 | 0.66967 | 0.65823 | 0.65878 | 0.64473 | 0.66823 | 0.68563 | 0.68656 | 0.7006 | 0.7372 | 0.74156
VP45_2_H200_V150_C45_MF_425 - Summe von Percent - Heat through workpiece/Total heat | 0.12378 | 0.13633 | 0.14841 | 0.16615 | 0.15698 | 0.15976 | 0.16748 | 0.17219 | 0.175 | 0.19447 | 0.22041 | 0.25577 | 0.24357 | 0.2359 | 0.23777 | 0.22525 | 0.18534 | 0.19265
Work piece
Tool
Chip
VP45_2

## Slide 29
Time and spatial varying thermal properties Temperature distribution for hsp = 200 µm, vc = 150 m/min
[°C]
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
Workpiece position : 124 mm
Workpiece position : 200 mm
Chart: 
| 200.0 | 250.0 | 300.0
Heat flow through the isothermal lines | 426.2762 | 111.9011 | 53.1325
Chart: 
| 200.0 | 250.0 | 300.0 | 350.0 | 400.0 | 450.0
Heat flow through the isothermal lines | 117.1813 | 88.843 | 61.985 | 43.8111 | 28.2654 | 13.6725
Notes: With higher cutting speed and lower chip thickness more heat is transferred over tip

## Slide 30: Time and spatial varying thermal properties Heat partition ratios for hsp = 300 µm, vc = 100 m/min
Chart: Workpiece position [mm]
| 113,62 | 118,70 | 123,78 | 128,86 | 133,94 | 139,02 | 144,11 | 149,19 | 154,27 | 159,35 | 164,43 | 169,51 | 174,59 | 179,67 | 184,76 | 189,84 | 194,92 | 200,00
VP42_1_H300_V100_C45_MF_425 - Summe von Percent - Heat inside tool/Total heat | 0.070153 | 0.066197 | 0.063305 | 0.062584 | 0.062285 | 0.061719 | 0.059477 | 0.058419 | 0.057124 | 0.058853 | 0.056226 | 0.055289 | 0.053794 | 0.056073 | 0.055038 | 0.054728 | 0.05449 | 0.054503
VP42_1_H300_V100_C45_MF_425 - Summe von Percent - Heat through chip/Total heat | 0.64915 | 0.63576 | 0.65008 | 0.64768 | 0.66579 | 0.64883 | 0.64075 | 0.65156 | 0.651 | 0.65515 | 0.6604 | 0.66746 | 0.6593 | 0.68398 | 0.69456 | 0.69385 | 0.74128 | 0.74377
VP42_1_H300_V100_C45_MF_425 - Summe von Percent - Heat through workpiece/Total heat | 0.2807 | 0.29805 | 0.28662 | 0.28973 | 0.27193 | 0.28945 | 0.29977 | 0.29002 | 0.29188 | 0.286 | 0.28337 | 0.27726 | 0.2869 | 0.25994 | 0.2504 | 0.25142 | 0.20423 | 0.20173
Tool
Work piece
Chip
VP42_1

## Slide 31
Time and spatial varying thermal properties Temperature distribution for hsp = 300 µm, vc = 100 m/min
[°C]
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
Workpiece position : 124 mm
Workpiece position : 200 mm
Chart: 
| 200.0 | 250.0 | 300.0 | 350.0 | 400.0 | 450.0 | 500.0 | 550.0
Heat flow through the isothermal lines | 125.6494 | 111.136 | 98.1282 | 79.3237 | 61.0442 | 44.2534 | 28.8177 | 13.1199
Chart: 
| 200.0 | 250.0 | 300.0 | 350.0 | 400.0 | 450.0 | 500.0 | 550.0 | 600.0
 | 95.7529 | 89.5135 | 82.9097 | 76.6459 | 68.1007 | 53.7736 | 39.391 | 23.9617 | 8.2831

## Slide 32: Time and spatial varying thermal properties Heat partition ratios for hsp = 300 µm, vc = 150 m/min
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 116,16 | 123,78 | 131,40 | 139,02 | 146,65 | 154,27 | 161,89 | 169,51 | 177,13 | 184,76 | 192,38 | 200,00
VP46_1_H300_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.16876 | 0.15733 | 0.13895 | 0.09664 | 0.08486 | 0.091231 | 0.099843 | 0.11257 | 0.10952 | 0.098737 | 0.086864 | 0.07623 | 0.06971 | 0.065551 | 0.063187 | 0.066794 | 0.065579 | 0.064855
VP46_1_H300_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.68413 | 0.68175 | 0.68902 | 0.67814 | 0.69377 | 0.68774 | 0.67482 | 0.67723 | 0.67652 | 0.68321 | 0.68433 | 0.69244 | 0.69505 | 0.69551 | 0.70006 | 0.71522 | 0.7479 | 0.74824
VP46_1_H300_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.14711 | 0.16092 | 0.17203 | 0.22522 | 0.22137 | 0.22103 | 0.22533 | 0.21021 | 0.21396 | 0.21805 | 0.2288 | 0.23133 | 0.23524 | 0.23894 | 0.23675 | 0.21798 | 0.18652 | 0.1869
VP46_2_H300_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.17244 | 0.16244 | 0.15391 | 0.11388 | 0.086204 | 0.087204 | 0.093946 | 0.10749 | 0.11059 | 0.11159 | 0.089534 | 0.083666 | 0.073695 | 0.066779 | 0.065401 | 0.06775 | 0.068736 | 0.065536
VP46_2_H300_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.69408 | 0.6853 | 0.67724 | 0.68756 | 0.69731 | 0.68802 | 0.6971 | 0.6837 | 0.68455 | 0.69855 | 0.68372 | 0.69243 | 0.69087 | 0.69032 | 0.70817 | 0.70888 | 0.74403 | 0.76151
VP46_2_H300_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.13348 | 0.15226 | 0.16885 | 0.19856 | 0.21649 | 0.22477 | 0.20896 | 0.20882 | 0.20486 | 0.18986 | 0.22675 | 0.22391 | 0.23544 | 0.2429 | 0.22643 | 0.22337 | 0.18723 | 0.17296
Tool
Work piece
Chip
VP46_1

## Slide 33
Chart: 
| 200.0 | 250.0 | 300.0 | 350.0 | 400.0
Heat flow through the isothermal lines | 384.012 | 208.7836 | 82.6251 | 52.4284 | 38.5033
Chart: 
| 200.0 | 250.0 | 300.0 | 350.0 | 400.0 | 450.0 | 500.0 | 550.0
Heat flow through the isothermal lines | 168.7495 | 136.1339 | 102.8575 | 72.1985 | 50.4499 | 35.9647 | 23.1285 | 8.7851
Time and spatial varying thermal properties Temperature distribution for hsp = 300 µm, vc = 150 m/min
[°C]
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
Workpiece position : 124 mm
Workpiece position : 200 mm

## Slide 34: Time and spatial varying thermal properties Heat partition ratios for hsp = 400 µm, vc = 150 m/min
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 116,16 | 123,78 | 131,40 | 139,02 | 146,65 | 154,27 | 161,89 | 169,51 | 177,13 | 184,76 | 192,38 | 200,00
VP49_1_H400_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.10919 | 0.10558 | 0.10468 | 0.092873 | 0.089236 | 0.088237 | 0.087198 | 0.088757 | 0.093683 | 0.091612 | 0.079934 | 0.075261 | 0.067861 | 0.061756 | 0.058373 | 0.057867 | 0.056965 | 0.051249
VP49_1_H400_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.61522 | 0.59901 | 0.61758 | 0.62149 | 0.64463 | 0.66867 | 0.65894 | 0.66084 | 0.63231 | 0.63757 | 0.64982 | 0.6428 | 0.65742 | 0.64795 | 0.65305 | 0.65652 | 0.67024 | 0.66469
VP49_1_H400_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.27559 | 0.29541 | 0.27775 | 0.28563 | 0.26613 | 0.2431 | 0.25386 | 0.2504 | 0.274 | 0.27082 | 0.27025 | 0.28194 | 0.27471 | 0.29029 | 0.28857 | 0.28561 | 0.27279 | 0.28406
VP49_2_H400_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.11464 | 0.11471 | 0.10863 | 0.09058 | 0.084358 | 0.083842 | 0.084245 | 0.09093 | 0.090504 | 0.085426 | 0.079734 | 0.072528 | 0.064938 | 0.060445 | 0.057503 | 0.055645 | 0.058719 | 0.051626
VP49_2_H400_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.60865 | 0.63929 | 0.63015 | 0.67285 | 0.68218 | 0.6776 | 0.69015 | 0.66985 | 0.68514 | 0.68118 | 0.66279 | 0.67321 | 0.68914 | 0.70214 | 0.68701 | 0.71862 | 0.69867 | 0.66834
VP49_2_H400_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.27671 | 0.24601 | 0.26122 | 0.23657 | 0.23346 | 0.23856 | 0.22561 | 0.23922 | 0.22435 | 0.23339 | 0.25747 | 0.25426 | 0.24592 | 0.23741 | 0.25549 | 0.22574 | 0.24261 | 0.28004
Tool
Work piece
Chip
VP49_1

## Slide 35
Chart: 
| 200.0 | 250.0 | 300.0 | 350.0 | 400.0 | 450.0 | 500.0 | 550.0 | 600.0
Heat flow through the isothermal lines | 166.2526 | 143.9093 | 126.9907 | 109.9916 | 88.8046 | 63.657 | 40.4955 | 20.1056 | 3.1204
Chart: 
| 200.0 | 250.0 | 300.0 | 350.0 | 400.0 | 450.0 | 500.0 | 550.0
Heat flow through the isothermal lines | 394.7848 | 310.043 | 232.8263 | 149.4607 | 92.0884 | 55.7769 | 37.3938 | 19.3476
Time and spatial varying thermal properties Temperature distribution for hsp = 400 µm, vc = 150 m/min [1/2]
[°C]
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
Workpiece position : 124 mm
Workpiece position : 200 mm

## Slide 36
Chart: 
| 200.0 | 250.0 | 300.0 | 350.0 | 400.0 | 450.0 | 500.0 | 550.0 | 600.0
Heat flow through the isothermal lines | 386.8005 | 307.5512 | 201.9429 | 126.9857 | 79.8459 | 55.649 | 38.076 | 22.6642 | 9.2713
Chart: 
| 200.0 | 250.0 | 300.0 | 350.0 | 400.0 | 450.0 | 500.0 | 550.0 | 600.0
Heat flow through the isothermal lines | 154.0593 | 135.7373 | 118.5908 | 105.3782 | 85.9984 | 62.7065 | 43.1938 | 25.8453 | 7.6211
Time and spatial varying thermal properties Temperature distribution for hsp = 400 µm, vc = 150 m/min [2/2]
[°C]
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
Workpiece position : 124 mm
Workpiece position : 200 mm

## Slide 37: Time and spatial varying thermal properties Heat partition ratios for hsp = 500 µm, vc = 150 m/min
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 116,16 | 123,78 | 131,40 | 139,02 | 146,65 | 154,27 | 161,89 | 169,51 | 177,13 | 184,76 | 192,38 | 200,00
VP50_1_H500_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.095651 | 0.093717 | 0.091407 | 0.079705 | 0.070662 | 0.068587 | 0.06954 | 0.06969 | 0.066816 | 0.064843 | 0.060145 | 0.055067 | 0.050188 | 0.0471 | 0.044661 | 0.045149 | 0.045183 | 0.042802
VP50_1_H500_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.6265 | 0.63812 | 0.65803 | 0.67398 | 0.70702 | 0.70043 | 0.68971 | 0.67757 | 0.67139 | 0.66681 | 0.65798 | 0.66806 | 0.66678 | 0.67553 | 0.69019 | 0.69354 | 0.70406 | 0.68549
VP50_1_H500_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.27785 | 0.26816 | 0.25057 | 0.24632 | 0.22231 | 0.23098 | 0.24075 | 0.25274 | 0.2618 | 0.26834 | 0.28188 | 0.27688 | 0.28303 | 0.27737 | 0.26514 | 0.26132 | 0.25075 | 0.2717
VP50_2_H500_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.099021 | 0.095855 | 0.091953 | 0.082591 | 0.074479 | 0.073724 | 0.071749 | 0.074174 | 0.068104 | 0.068681 | 0.063743 | 0.056196 | 0.051533 | 0.048273 | 0.046513 | 0.046522 | 0.046357 | 0.043667
VP50_2_H500_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.6415 | 0.65939 | 0.65955 | 0.69394 | 0.73029 | 0.71535 | 0.71119 | 0.69405 | 0.69127 | 0.67765 | 0.68556 | 0.67657 | 0.68968 | 0.68217 | 0.69574 | 0.69898 | 0.70165 | 0.67331
VP50_2_H500_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.25948 | 0.24475 | 0.24849 | 0.22347 | 0.19523 | 0.21093 | 0.21706 | 0.23178 | 0.24062 | 0.25367 | 0.2507 | 0.26723 | 0.25878 | 0.26956 | 0.25775 | 0.2545 | 0.25199 | 0.28302
Tool
Work piece
Chip
VP50_1

## Slide 38
Chart: 
| 200.0 | 250.0 | 300.0 | 350.0 | 400.0 | 450.0 | 500.0 | 550.0 | 600.0
Heat flow through the isothermal lines | 147.5285 | 138.6991 | 126.4536 | 114.534 | 101.7444 | 83.2813 | 58.56 | 34.6065 | 12.2568
Chart: 
| 200.0 | 250.0 | 300.0 | 350.0 | 400.0 | 450.0 | 500.0 | 550.0 | 600.0
Heat flow through the isothermal lines | 339.6816 | 293.7062 | 236.0262 | 172.7628 | 118.4482 | 80.4727 | 50.9191 | 29.5994 | 12.5991
Time and spatial varying thermal properties Temperature distribution for hsp = 500 µm, vc = 150 m/min
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
[°C]
Workpiece position : 124 mm
Workpiece position : 200 mm

## Slide 39: Time and spatial varying thermal properties Conclusion
XYZ

## Slide 40: Time and spatial varying thermal properties Means to enhance quality of measurement
Determine emissivity of chip/tool/workpiece
  Collect chips
  Heating + Pyrometer + Camera
  e (DL)
  Regression of Tcam (DL, ecam) for IT
Enhance quantity of valid pixels
  Expand field of measurement
  Measurement with multiple integration times
  Overlap pictures via algorithm
Determine workpiece directly
  Separate measurements for the work piece
  Compare Heat flows with Ptotal

## Slide 41: Gliederung
Influence of uncut chip thickness and cutting velocity
3.2
Time and spatial varying thermal properties
3.1
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 42: Influence of uncut chip thickness and cutting velocity Workpiece position 124 mm
ap = 3,5 mm, = 6°, = 3°, < 5 µm, uncoated, workpiece position: 124 mm
Chart: Heat partition (chip)
| 100,00 | 150,00
200,00 | 0.60676 | 0.66906
300,00 | 0.65008 | 0.67723
400,00 | 0.66084
500,00 | 0.67757
Chart: Heat partition (tool)
| 100,00 | 150,00
200,00 | 0.11347 | 0.15876
300,00 | 0.063305 | 0.11257
400,00 | 0.088757
500,00 | 0.06969
Chart: Heat flow (chip) [W]
| 100,00 | 150,00
200,00 | 1451.366 | 2209.5729
300,00 | 2208.0209 | 3055.4101
400,00 | 4006.6247
500,00 | 4892.1433
Chart: Heat flow (workpiece) [W]
| 100,00 | 150,00
200,00 | 669.2185 | 568.6464
300,00 | 973.5123 | 948.3814
400,00 | 1518.1602
500,00 | 1824.8451
Chart: Heat partition (workpiece)
| 100,00 | 150,00
200,00 | 0.27977 | 0.17219
300,00 | 0.28662 | 0.21021
400,00 | 0.2504
500,00 | 0.25274
hsp [µm]
Cutting velocity [m/min]
Chart: Heat flow (tool) [W]
| 100,00 | 150,00
200,00 | 271.4271 | 524.3068
300,00 | 215.0172 | 507.8638
400,00 | 538.1241
500,00 | 503.1715

## Slide 43: Influence of uncut chip thickness and cutting velocity Workpiece position 200 mm
ap = 3,5 mm, = 6°, = 3°, < 5 µm, uncoated, workpiece position: 200 mm
Chart: Heat flow (chip) [W]
| 100,00 | 150,00
200,00 | 1704.9593 | 2425.7515
300,00 | 2526.242 | 3375.8082
400,00 | 4015.3245
500,00 | 4981.0634
Chart: Heat partition (chip)
| 100,00 | 150,00
200,00 | 0.71637 | 0.74156
300,00 | 0.74377 | 0.74824
400,00 | 0.66469
500,00 | 0.68549
Chart: Heat partition (tool)
| 100,00 | 150,00
200,00 | 0.076264 | 0.065791
300,00 | 0.054503 | 0.064855
400,00 | 0.051249
500,00 | 0.042802
Chart: Heat flow (workpiece) [W]
| 100,00 | 150,00
200,00 | 493.5213 | 630.1998
300,00 | 685.1877 | 843.2458
400,00 | 1715.9807
500,00 | 1974.2951
Chart: Heat partition (workpiece)
| 100,00 | 150,00
200,00 | 0.20736 | 0.19265
300,00 | 0.20173 | 0.1869
400,00 | 0.28406
500,00 | 0.2717
Chart: Heat flow (tool) [W]
| 100,00 | 150,00
200,00 | 181.5074 | 215.2119
300,00 | 185.1207 | 292.6013
400,00 | 309.5919
500,00 | 311.0184
hsp [µm]
Cutting velocity [m/min]