## Slide 1: Results
Experimental investigation of temperatures and heat flows for orthogonal cutting 1045/4140 steel by thermal imaging

## Slide 2: Gliederung
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 3: Gliederung
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 4: Experimental Setup Design of Experiment
Thermal camera
Workpiece
Tool
Cutting process
Area covered by the thermal camera

## Slide 5: Experimental Setup Design of Experiment
Experiments | Cutting Velocity [m/min] | Uncut chip thickness [µm] | Integration time [µs] | Cutting Force [N] | Passive Force [N]
VP41_1_H200_V100_C45_MF_425 | 100 | 200 | 425 | 1500 | 1000
VP41_2_H200_V100_C45_MF_425 | 100 | 200 | 425 | 1565 | 1005
VP42_1_H300_V100_C45_MF_425 | 100 | 300 | 425 | 2250 | 1159
VP42_2_H300_V100_C45_MF_285 | 100 | 300 | 285 | 2136 | 1079
VP43_1_H400_V100_C45_MF_285 | 100 | 400 | 285 | 2716 | 1118
VP45_2_H200_V150_C45_MF_425 | 150 | 200 | 425 | 1448 | 688
VP46_1_H300_V150_C45_MF_285 | 150 | 300 | 285 | 2006 | 801
VP46_2_H300_V150_C45_MF_285 | 150 | 300 | 285 | 2004 | 875
VP49_1_H400_V150_C45_MF_285 | 150 | 400 | 285 | 2675 | 1046
VP49_2_H400_V150_C45_MF_285 | 150 | 400 | 285 | 2590 | 1000
VP50_1_H500_V150_C45_MF_285 | 150 | 500 | 285 | 3220 | 1120
VP50_2_H500_V150_C45_MF_285 | 150 | 500 | 285 | 3178 | 1162

## Slide 6: Experimental Setup Boundary Conditions
Boundary Conditions |  |  |  |  | 
Tool |  | Camera |  | Workpiece | 
Heat Conductivity [W/(mK)] | 75,4 | Pixel pitch (Infrared Camera) [mm/pixel] | 0,015 | Length of the workpiece [mm] | 200
Heat Capacity [J/(cm^3K)] | Interpolation* | Maximum digit level valid (FLIR X) | 8192 | Heat Capacity [J/(kgK)] | Interpolation**
Rake Angle [°] | 6 | Maximum digit level valid (FLIR SC7600) | 16000 | Workpiece Material | AISI 1045 (normalized)
Clearance Angle [°] | 3 | Frame Rate (Infrared Camera) [Hz] | 328 | Depth of Cut ap [mm] | 3,5
Assumed percentage of heat conducted away by convection and radiation | 0,03 | Minimum valid temperature for the frames [°C] | 200 | Maximum error of the workpiece position for = 100 [mm/mm] | 0,0255
Cutting edge radius [µm] | < 5 | Emissivity (Experimentally determined - tool and workpiece coated) | 0,85 | Maximum error of the workpiece position for = 150 [mm/mm] | 0,038
 |  |  |  | Percentage of the deformation energy converted into heat | 0,9
 |  |  |  | Density (based on steel) [kg/m^3] | 7874
Boundary Conditions |  |  |  |  | 
Tool |  | Camera |  | Workpiece | 
Heat Conductivity [W/(mK)] | 75,4 | Pixel pitch (Infrared Camera) [mm/pixel] | 0,015 | Length of the workpiece [mm] | 200
Heat Capacity [J/(cm^3K)] | Interpolation* | Maximum digit level valid (FLIR X) | 8192 | Heat Capacity [J/(kgK)] | Interpolation**
Rake Angle [°] | 6 | Maximum digit level valid (FLIR SC7600) | 16000 | Workpiece Material | AISI 1045 (normalized)
Clearance Angle [°] | 3 | Frame Rate (Infrared Camera) [Hz] | 328 | Depth of Cut ap [mm] | 3,5
Assumed percentage of heat conducted away by convection and radiation | 0,03 | Minimum valid temperature for the frames [°C] | 200 |  | 0,0255
Cutting edge radius [µm] | < 5 | Emissivity (Experimentally determined - tool and workpiece coated) | 0,85 |  | 0,038
 |  |  |  | Percentage of the deformation energy converted into heat | 0,9
 |  |  |  | Density (based on steel) [kg/m^3] | 7874
*Tool [J/(cm^3K)] |  | 
**Workpiece [J/(kgK)] |  | 
Interpolation

## Slide 7: Gliederung
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 8: Post processing of thermal pictures Energy balance in the volume control
Tool
Workpiece
Control volume
Inside Energy
Total power produced
  Direct force measurement
Energy from material going inside the control volume
  Always zero ()
Outside Energy
Heat flow into the tool
  Calculation by gradient
Heat flow into the workpiece
  Calculation by heat balance
Energy from the chip going outside
  thermodynamic calculation
Part of deformation energy converted in heat
  90% of the total deformation energy
*,
Chip
Notes: In this analysis, the energy flows considered for the volume control are listed above. Then, with the temperature field of the Infrared camera frames, this analysis is able to calculate the heat flow through the tool and the chip and, consequently, the heat partition of the total power produced during the process. About 10% of the deformation energy is converted in heat and the heat flow through the workpiece is calculated by the total balance.

## Slide 9: Post processing of thermal pictures Heat carried away from the tool tip
The heat flow through the tool is calculated as a mean value between the heat flows calculated for the last two isothermals.
Method based on [BOOTHROYD].
  : heat conductivity
  : length of the isothermal
  : temperature gradient normal to line
  : effective tool width
Tool

## Slide 10: Post processing of thermal pictures Heat carried away by the chip
Tool
Chip
End of contact chip - tool
The heat flow is calculated on the end of contact between chip and tool interfaces
Method based on [BOOTHROYD].
  : heat capacity function
  : chip temperature
  : environment temperature
  : velocity of the chip
  : chip thickness
  : chip width

## Slide 11: Gliederung
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Influence of uncut chip thickness and cutting velocity
3.2
Time and spatial varying thermal properties
3.1
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 12: Time and spatial varying thermal properties Temperature at tool tip [°C] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 323.5206 | 271.9162 | 380.5434 | 341.2377 | 357.2232 | 368.2788 | 230.1309 | 364.6832 | 365.8805 | 343.2452 | 364.6607 | 379.6024 | 393.9241 | 390.0437 | 373.423 | 398.9011 | 411.4206 | 425.8531
VP42_1_H300_V100_C45_MF_425 | 442.907 | 491.0974 | 498.6279 | 450.6018 | 444.4791 | 340.6401 | 471.2703 | 433.7598 | 426.1506 | 282.3214 | 323.3509 | 255.7746 | 504.0463 | 485.6611 | 516.0332 | 517.7154 | 520.8733 | 525.9864
VP43_1_H400_V100_C45_MF_285 | 475.9792 | 406.8634 | 496.2303 | 444.492 | 421.7696 | 195.0595
VP45_2_H200_V150_C45_MF_425 | 363.7171 | 378.5227 | 387.0074 | 395.5219 | 410.6586 | 412.4561 | 402.5545 | 408.8741 | 411.6293 | 408.0815 | 415.8895 | 415.7033 | 420.948 | 444.6016 | 447.3969 | 461.0162 | 447.4671 | 441.2219
VP46_1_H300_V150_C45_MF_285 | 425.3031 | 385.6967 | 416.9808 | 388.6194 | 419.6816 | 428.1679 | 436.2967 | 452.2375 | 437.1667 | 384.2404 | 438.4321 | 320.4099 | 442.1594 | 492.6639 | 486.9684 | 492.3859 | 488.9218 | 505.5068
VP49_1_H400_V150_C45_MF_285 | 414.4026 | 414.7684 | 441.6356 | 253.9839 | 421.9092 | 485.0291 | 476.3299 | 470.3219 | 416.562 | 469.1423 | 474.6055 | 474.9649 | 493.8176 | 495.579 | 514.8465 | 506.6511 | 489.6865 | 469.3475
VP50_1_H500_V150_C45_MF_285 | 412.4521 | 377.9897 | 447.9103 | 416.5194 | 457.2466 | 439.4002 | 506.3999 | 468.2151 | 457.8948 | 424.7005 | 430.3532 | 477.8122 | 511.4966 | 514.4709 | 502.4442 | 486.0228 | 490.5698 | 473.5951

## Slide 13: Time and spatial varying thermal properties Internal energy in tool [Joule] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 6.5224 | 6.7965 | 7.0719 | 7.3539 | 7.8868 | 8.1574 | 7.964 | 8.4782 | 8.7992 | 9.1514 | 9.4147 | 9.5462 | 9.7156 | 9.9526 | 9.8572 | 10.3038 | 10.4344 | 10.4692
VP42_1_H300_V100_C45_MF_425 | 8.6795 | 8.9284 | 9.2325 | 9.6003 | 10.0522 | 10.2113 | 10.5446 | 10.7162 | 10.8376 | 10.3466 | 10.6856 | 11.1312 | 11.4614 | 11.5732 | 12.7034 | 12.9454 | 13.1586 | 13.3152
VP43_1_H400_V100_C45_MF_285 | 9.7584 | 9.8709 | 10.4491 | 10.8884 | 11.2608 | 10.6312
VP45_2_H200_V150_C45_MF_425 | 1.5376 | 1.7419 | 1.9444 | 2.1819 | 2.4671 | 2.7856 | 3.1359 | 3.5036 | 3.8728 | 4.1878 | 4.4347 | 4.6127 | 4.8247 | 5.0665 | 5.3337 | 5.7504 | 6.1824 | 6.4363
VP46_1_H300_V150_C45_MF_285 | 2.5631 | 2.8266 | 3.1545 | 3.4264 | 3.8378 | 4.3676 | 4.87 | 5.4523 | 5.947 | 6.3015 | 6.4102 | 6.6173 | 6.1817 | 7.25 | 7.6531 | 8.1454 | 8.6188 | 8.84
VP49_1_H400_V150_C45_MF_285 | 5.0798 | 5.5896 | 6.1222 | 6.2829 | 6.9385 | 7.5386 | 8.1279 | 8.7742 | 9.371 | 9.8999 | 10.1846 | 10.3374 | 10.5043 | 10.7092 | 11.0906 | 11.6349 | 12.2059 | 12.4869
VP50_1_H500_V150_C45_MF_285 | 6.23 | 6.8538 | 7.3979 | 7.8002 | 8.2048 | 8.7882 | 9.527 | 10.2283 | 11.0142 | 11.6462 | 12.0316 | 12.2152 | 12.3571 | 12.5159 | 12.8927 | 13.4692 | 14.2166 | 14.6323
Notes: The higher the chip thickness the higher the internal energy/heat rate
The lower the cutting speed the higher the internal energy in the tool  High Speed cutting

## Slide 14: Time and spatial varying thermal properties Heating rate of the tool [W] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 15.4407 | 15.4407 | 15.4407 | 15.4407 | 15.4407 | 15.4407 | 15.4407 | 15.4407 | 15.4407 | 15.4407 | 15.4407 | 15.4407 | 15.4407 | 15.4407 | 15.4407 | 15.4407 | 15.4407 | 15.4407
VP42_1_H300_V100_C45_MF_425 | 16.6173 | 16.6173 | 16.6173 | 16.6173 | 16.6173 | 16.6173 | 16.6173 | 16.6173 | 16.6173 | 16.6173 | 16.6173 | 16.6173 | 16.6173 | 16.6173 | 16.6173 | 16.6173 | 16.6173 | 16.6173
VP43_1_H400_V100_C45_MF_285 | 16.5484 | 16.5484 | 16.5484 | 16.5484 | 16.5484 | 16.5484
VP45_2_H200_V150_C45_MF_425 | 12.5324 | 12.5324 | 12.5324 | 12.5324 | 12.5324 | 12.5324 | 12.5324 | 12.5324 | 12.5324 | 12.5324 | 12.5324 | 12.5324 | 12.5324 | 12.5324 | 12.5324 | 12.5324 | 12.5324 | 12.5324
VP46_1_H300_V150_C45_MF_285 | 16.0028 | 16.0028 | 16.0028 | 16.0028 | 16.0028 | 16.0028 | 16.0028 | 16.0028 | 16.0028 | 16.0028 | 16.0028 | 16.0028 | 16.0028 | 16.0028 | 16.0028 | 16.0028 | 16.0028 | 16.0028
VP49_1_H400_V150_C45_MF_285 | 18.6621 | 18.6621 | 18.6621 | 18.6621 | 18.6621 | 18.6621 | 18.6621 | 18.6621 | 18.6621 | 18.6621 | 18.6621 | 18.6621 | 18.6621 | 18.6621 | 18.6621 | 18.6621 | 18.6621 | 18.6621
VP50_1_H500_V150_C45_MF_285 | 20.939 | 20.939 | 20.939 | 20.939 | 20.939 | 20.939 | 20.939 | 20.939 | 20.939 | 20.939 | 20.939 | 20.939 | 20.939 | 20.939 | 20.939 | 20.939 | 20.939 | 20.939
Notes: Heating rate rises with chip thickness
Heating rate decreases with cutting speed
H/v  Heating rate
1,33
2
4
2
3
2,66
3,333

## Slide 15: Time and spatial varying thermal properties Heat carried away by chip [W] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 1446.9037 | 1500.714 | 1451.366 | 1450.7175 | 1523.3013 | 1526.934 | 1392.793 | 1493.1362 | 1594.0554 | 1427.9538 | 1554.7901 | 1602.5165 | 1624.0372 | 1635.069 | 1589.2306 | 1724.2013 | 1825.9456 | 1704.9593
VP42_1_H300_V100_C45_MF_425 | 2227.4118 | 2165.4074 | 2208.0209 | 2199.885 | 2261.3844 | 2203.7899 | 2195.2405 | 2222.4003 | 2237.2376 | 2244.5721 | 2246.1977 | 2273.3784 | 2258.7944 | 2343.3527 | 2365.7067 | 2380.7834 | 2543.5444 | 2526.242
VP43_1_H400_V100_C45_MF_285 | 2660.3012 | 2674.8095 | 2734.291 | 2713.5039 | 2756.6819 | 2772.8196
VP45_2_H200_V150_C45_MF_425 | 2211.1666 | 2131.5983 | 2135.074 | 2141.749 | 2208.7243 | 2215.9191 | 2195.4285 | 2209.5729 | 2208.4354 | 2167.633 | 2166.4547 | 2117.3798 | 2194.5496 | 2264.3116 | 2267.3972 | 2317.1508 | 2414.638 | 2425.7515
VP46_1_H300_V150_C45_MF_285 | 3086.5735 | 3075.8261 | 3108.6092 | 3077.5016 | 3148.4235 | 3128.8205 | 3066.2035 | 3055.4101 | 3081.729 | 3082.416 | 3094.5335 | 3131.2069 | 3135.8375 | 3145.0925 | 3184.8716 | 3226.8478 | 3394.0747 | 3375.8082
VP49_1_H400_V150_C45_MF_285 | 3703.6478 | 3636.3396 | 3744.3018 | 3768.0535 | 3889.5999 | 4034.6229 | 3975.9522 | 4006.6247 | 3828.9325 | 3860.761 | 3944.7605 | 3892.4492 | 3953.3381 | 3900.7334 | 3935.8881 | 3961.3381 | 4063.606 | 4015.3245
VP50_1_H500_V150_C45_MF_285 | 4552.4075 | 4621.685 | 4751.0572 | 4866.2372 | 5104.8332 | 5095.3821 | 5000.6533 | 4892.1433 | 4847.5272 | 4814.495 | 4792.0381 | 4843.6789 | 4845.0776 | 4887.454 | 5004.1952 | 5045.1906 | 5110.3196 | 4981.0634
Notes: Heat carried away by chip rises with hsp*vc
Heat carried away by chip increases with cutting length for small chip thickness
Why?????
vc* hsp ~ chip ; lc ↑ → chip = const. (gilt nicht für Vp41 , VP42)
chip ↑ → Bchip ↑ (für Vp41 , VP42)
vc* hsp ~ ( 𝒒) ̇^´chip ; lc ↑ → ( 𝒒) ̇^´chip = const. (gilt nicht für Vp41 , VP42)
( 𝒒) ̇^´chip ↑ → Bchip ↑ (für Vp41 , VP42)

## Slide 16: Time and spatial varying thermal properties Heat partition to the chip for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 0.60694 | 0.62951 | 0.60676 | 0.60854 | 0.63899 | 0.63612 | 0.57706 | 0.62093 | 0.66525 | 0.59274 | 0.64887 | 0.66995 | 0.68124 | 0.68587 | 0.66664 | 0.72446 | 0.76721 | 0.71637
VP42_1_H300_V100_C45_MF_425 | 0.64915 | 0.63576 | 0.65008 | 0.64768 | 0.66579 | 0.64883 | 0.64075 | 0.65156 | 0.651 | 0.65515 | 0.6604 | 0.66746 | 0.6593 | 0.68398 | 0.69456 | 0.69385 | 0.74128 | 0.74377
VP43_1_H400_V100_C45_MF_285 | 0.64724 | 0.65635 | 0.66524 | 0.66103 | 0.67155 | 0.6804
VP45_2_H200_V150_C45_MF_425 | 0.67329 | 0.65163 | 0.6527 | 0.65474 | 0.67163 | 0.67741 | 0.6685 | 0.66906 | 0.66967 | 0.65823 | 0.65878 | 0.64473 | 0.66823 | 0.68563 | 0.68656 | 0.7006 | 0.7372 | 0.74156
VP46_1_H300_V150_C45_MF_285 | 0.68413 | 0.68175 | 0.68902 | 0.67814 | 0.69377 | 0.68774 | 0.67482 | 0.67723 | 0.67652 | 0.68321 | 0.68433 | 0.69244 | 0.69505 | 0.69551 | 0.70006 | 0.71522 | 0.7479 | 0.74824
VP49_1_H400_V150_C45_MF_285 | 0.61522 | 0.59901 | 0.61758 | 0.62149 | 0.64463 | 0.66867 | 0.65894 | 0.66084 | 0.63231 | 0.63757 | 0.64982 | 0.6428 | 0.65742 | 0.64795 | 0.65305 | 0.65652 | 0.67024 | 0.66469
VP50_1_H500_V150_C45_MF_285 | 0.6265 | 0.63812 | 0.65803 | 0.67398 | 0.70702 | 0.70043 | 0.68971 | 0.67757 | 0.67139 | 0.66681 | 0.65798 | 0.66806 | 0.66678 | 0.67553 | 0.69019 | 0.69354 | 0.70406 | 0.68549
Notes: No influence of level of heat partition inside the chip by chip thickness
Rising heat partition inside the chip, especially for lower chip thickness  Hypo: tool is heating up and is conducts less heat away
Hypo: The lower the chip thickness the lower the influence of friction at the rake face
1 = Bchip + Btool + BWP
Btool = konst. ; Bchip ↑ → BWP ↓

## Slide 17: Time and spatial varying thermal properties Heat flux into the tool [W] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 537.8213 | 551.0612 | 504.1976 | 489.8472 | 475.7109 | 462.2297 | 465.9544 | 436.4744 | 423.9621 | 436.2984 | 433.8529 | 432.3652 | 427.3557 | 416.7658 | 410.0894 | 411.1337 | 413.6419 | 425.8658
VP42_1_H300_V100_C45_MF_425 | 495.5091 | 499.1688 | 489.3581 | 487.6279 | 489.6444 | 477.1717 | 471.2803 | 459.3866 | 458.3732 | 498.0052 | 542.1343 | 477.3764 | 472.7017 | 421.8835 | 432.228 | 408.5606 | 406.485 | 376.3064
VP43_1_H400_V100_C45_MF_285 | 547.0138 | 336.4551 | 624.8956 | 551.3233 | 518.1474 | 687.9283
VP45_2_H200_V150_C45_MF_425 | 618.1984 | 640.028 | 641.7201 | 617.8658 | 647.1573 | 632.3828 | 633.7377 | 620.1267 | 610.2987 | 591.7276 | 568.9634 | 558.4665 | 539.3604 | 519.0394 | 506.3175 | 492.2143 | 482.4562 | 333.451
VP46_1_H300_V150_C45_MF_285 | 922.1491 | 933.1709 | 908.633 | 913.8529 | 861.6563 | 816.3021 | 784.7614 | 782.7941 | 759.174 | 728.4207 | 674.5768 | 641.4992 | 669.7591 | 644.0289 | 592.3355 | 625.4251 | 590.9196 | 520.9051
VP49_1_H400_V150_C45_MF_285 | 907.3091 | 895.5821 | 890.24 | 850.9987 | 783.3972 | 760.2121 | 737.769 | 734.4101 | 742.1041 | 736.211 | 707.8437 | 698.2731 | 704.5002 | 680.5663 | 659.2025 | 646.5626 | 628.3064 | 483.8331
VP50_1_H500_V150_C45_MF_285 | 1010.7407 | 958.6727 | 904.7866 | 873.8136 | 844.2917 | 823.7051 | 800.0742 | 777.6082 | 777.0326 | 780.2792 | 750.6885 | 728.8314 | 707.4754 | 682.0295 | 651.7829 | 633.2114 | 623.9451 | 414.1149

## Slide 18: Time and spatial varying thermal properties Heat flux into the tool [W] for different vc and hsp 2
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_1_H200_V100_C45_MF_425 | 553.4076 | 562.1962 | 536.3223 | 534.3013 | 541.3643 | 500.4892 | 484.2029 | 477.0592 | 481.5862 | 469.2852 | 464.1822 | 457.1269 | 451.0774 | 432.859 | 437.7509 | 421.9784 | 416.3514 | 452.6575
VP41_2_H200_V100_C45_MF_425 | 537.8213 | 551.0612 | 504.1976 | 489.8472 | 475.7109 | 462.2297 | 465.9544 | 436.4744 | 423.9621 | 436.2984 | 433.8529 | 432.3652 | 427.3557 | 416.7658 | 410.0894 | 411.1337 | 413.6419 | 425.8658
VP42_1_H300_V100_C45_MF_425 | 495.5091 | 499.1688 | 489.3581 | 487.6279 | 489.6444 | 477.1717 | 471.2803 | 459.3866 | 458.3732 | 498.0052 | 542.1343 | 477.3764 | 472.7017 | 421.8835 | 432.228 | 408.5606 | 406.485 | 376.3064
VP43_1_H400_V100_C45_MF_285 | 547.0138 | 336.4551 | 624.8956 | 551.3233 | 518.1474 | 687.9283
VP45_2_H200_V150_C45_MF_425 | 618.1984 | 640.028 | 641.7201 | 617.8658 | 647.1573 | 632.3828 | 633.7377 | 620.1267 | 610.2987 | 591.7276 | 568.9634 | 558.4665 | 539.3604 | 519.0394 | 506.3175 | 492.2143 | 482.4562 | 333.451
VP46_1_H300_V150_C45_MF_285 | 922.1491 | 933.1709 | 908.633 | 913.8529 | 861.6563 | 816.3021 | 784.7614 | 782.7941 | 759.174 | 728.4207 | 674.5768 | 641.4992 | 669.7591 | 644.0289 | 592.3355 | 625.4251 | 590.9196 | 520.9051
VP46_2_H300_V150_C45_MF_285 | 941.2428 | 933.4865 | 970.8659 | 949.7809 | 868.9845 | 846.8186 | 788.7198 | 769.9862 | 764.6344 | 750.5078 | 711.5717 | 682.1477 | 667.9614 | 648.656 | 624.2436 | 609.1016 | 615.5715 | 492.6965
VP49_1_H400_V150_C45_MF_285 | 907.3091 | 895.5821 | 890.24 | 850.9987 | 783.3972 | 760.2121 | 737.769 | 734.4101 | 742.1041 | 736.211 | 707.8437 | 698.2731 | 704.5002 | 680.5663 | 659.2025 | 646.5626 | 628.3064 | 483.8331
VP49_2_H400_V150_C45_MF_285 | 845.6697 | 906.1077 | 859.812 | 808.4793 | 773.5746 | 752.201 | 727.0429 | 725.5287 | 710.9076 | 684.2109 | 694.0327 | 683.8079 | 663.6366 | 650.1855 | 624.714 | 602.9008 | 626.7539 | 457.7981
VP50_1_H500_V150_C45_MF_285 | 1010.7407 | 958.6727 | 904.7866 | 873.8136 | 844.2917 | 823.7051 | 800.0742 | 777.6082 | 777.0326 | 780.2792 | 750.6885 | 728.8314 | 707.4754 | 682.0295 | 651.7829 | 633.2114 | 623.9451 | 414.1149
VP50_2_H500_V150_C45_MF_285 | 990.3566 | 973.2699 | 912.91 | 882.583 | 840.7158 | 814.4605 | 811.2716 | 786.7426 | 767.3583 | 798.2731 | 765.9853 | 737.0867 | 704.2792 | 679.0674 | 658.0564 | 651.6257 | 635.4241 | 404.3576
Notes: For small chip thickness no influence of cutting speed
Heat flux into the tool rises with chip thickness decreasingly,
Less rise for smaller cutting speeds
Decreases for higher chip thickness over time constant for small chip thickness hypo: tool gets to hot to carry heat away
Hypo: The higher the chip thickness the higher the frictional influence
Thermal number? Vc *hsp??

## Slide 19: Time and spatial varying thermal properties Heat partition into the tool for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 0.2256 | 0.23116 | 0.21078 | 0.20548 | 0.19955 | 0.19256 | 0.19306 | 0.18151 | 0.17693 | 0.1811 | 0.18106 | 0.18075 | 0.17927 | 0.17482 | 0.17202 | 0.17275 | 0.1738 | 0.17894
VP42_1_H300_V100_C45_MF_425 | 0.14441 | 0.14655 | 0.14408 | 0.14357 | 0.14416 | 0.14049 | 0.13756 | 0.13468 | 0.13338 | 0.14536 | 0.15939 | 0.14016 | 0.13797 | 0.12314 | 0.1269 | 0.11907 | 0.11846 | 0.11079
VP43_1_H400_V100_C45_MF_285 | 0.1394 | 0.088931 | 0.15835 | 0.14063 | 0.13255
VP45_2_H200_V150_C45_MF_425 | 0.18824 | 0.19566 | 0.19617 | 0.18888 | 0.19679 | 0.19332 | 0.19297 | 0.18777 | 0.18506 | 0.17968 | 0.17301 | 0.17005 | 0.16423 | 0.15716 | 0.15331 | 0.14882 | 0.1473 | 0.10194
VP46_1_H300_V150_C45_MF_285 | 0.20439 | 0.20684 | 0.2014 | 0.20137 | 0.18987 | 0.17943 | 0.17271 | 0.1735 | 0.16666 | 0.16145 | 0.14918 | 0.14186 | 0.14845 | 0.14242 | 0.1302 | 0.13862 | 0.13021 | 0.11546
VP49_1_H400_V150_C45_MF_285 | 0.15071 | 0.14753 | 0.14683 | 0.14036 | 0.12983 | 0.12599 | 0.12227 | 0.12113 | 0.12255 | 0.12158 | 0.1166 | 0.11531 | 0.11716 | 0.11305 | 0.10938 | 0.10716 | 0.10363 | 0.080093
VP50_1_H500_V150_C45_MF_285 | 0.1391 | 0.13236 | 0.12531 | 0.12102 | 0.11694 | 0.11323 | 0.11035 | 0.1077 | 0.10762 | 0.10807 | 0.10307 | 0.10052 | 0.097363 | 0.094268 | 0.089896 | 0.087044 | 0.085963 | 0.056991
Notes: Heat partition inside tool higher for low cutting speed  Puls
No influence of chip thickness  Puls
Remains constant over time

## Slide 20: Time and spatial varying thermal properties Heat flux into the workpiece [W] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 399.2048 | 332.1547 | 436.448 | 443.3651 | 384.9177 | 411.2226 | 554.8337 | 475.0844 | 378.1426 | 544.8393 | 407.5171 | 357.13 | 332.5369 | 332.0951 | 384.6099 | 244.6531 | 140.4006 | 249.163
VP42_1_H300_V100_C45_MF_425 | 708.3569 | 741.4585 | 699.1714 | 709.0375 | 645.5216 | 715.5888 | 759.5109 | 729.1106 | 741.0243 | 683.4545 | 612.9219 | 655.2798 | 694.5357 | 660.7956 | 608.0999 | 641.9338 | 481.2485 | 494.002
VP43_1_H400_V100_C45_MF_285 | 902.8935 | 1064.0178 | 751.0218 | 840.1052 | 830.1032 | 614.5346
VP45_2_H200_V150_C45_MF_425 | 454.7553 | 499.5369 | 494.369 | 511.5483 | 432.7092 | 422.8613 | 454.954 | 472.8265 | 479.0542 | 533.7844 | 553.1726 | 608.2739 | 550.2103 | 519.1751 | 528.8115 | 497.9993 | 378.3169 | 511.9606
VP46_1_H300_V150_C45_MF_285 | 502.9328 | 502.6583 | 494.4131 | 546.7735 | 528.0482 | 604.303 | 692.755 | 673.4511 | 714.3493 | 700.8186 | 752.8602 | 749.2644 | 706.0587 | 732.8491 | 772.2185 | 659.3823 | 553.1337 | 614.942
VP49_1_H400_V150_C45_MF_285 | 1409.1216 | 1538.6299 | 1428.3672 | 1443.8569 | 1360.8383 | 1239.0004 | 1320.1142 | 1321.8743 | 1484.3887 | 1458.4533 | 1417.9473 | 1464.703 | 1355.5302 | 1438.7787 | 1431.8077 | 1425.9347 | 1370.9967 | 1541.7394
VP50_1_H500_V150_C45_MF_285 | 1703.2288 | 1662.2937 | 1564.3162 | 1480.1091 | 1271.035 | 1355.5138 | 1449.6839 | 1550.4084 | 1595.6002 | 1625.3858 | 1740.2729 | 1677.9012 | 1713.824 | 1665.5447 | 1594.4334 | 1596.199 | 1524.0523 | 1871.1986
Notes: Heat flux inside work piece decreases with cutting speed and chip thickness
Heat flux into workpiece decreases over cutting length for small chip thickness
How over time?
How is this possible?

## Slide 21: Time and spatial varying thermal properties Heat partition into the workpiece for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 0.16746 | 0.13933 | 0.18246 | 0.18598 | 0.16146 | 0.17132 | 0.22988 | 0.19757 | 0.15781 | 0.22616 | 0.17007 | 0.1493 | 0.13949 | 0.13931 | 0.16133 | 0.1028 | 0.058992 | 0.10469
VP42_1_H300_V100_C45_MF_425 | 0.20644 | 0.21769 | 0.20585 | 0.20875 | 0.19005 | 0.21068 | 0.22169 | 0.21376 | 0.21562 | 0.19949 | 0.1802 | 0.19239 | 0.20272 | 0.19287 | 0.17854 | 0.18708 | 0.14025 | 0.14544
VP43_1_H400_V100_C45_MF_285 | 0.21967 | 0.26109 | 0.18272 | 0.20466 | 0.20222 | 0.1508
VP45_2_H200_V150_C45_MF_425 | 0.13847 | 0.15271 | 0.15113 | 0.15638 | 0.13158 | 0.12927 | 0.13853 | 0.14317 | 0.14527 | 0.16209 | 0.16821 | 0.18522 | 0.16754 | 0.15721 | 0.16012 | 0.15057 | 0.1155 | 0.15651
VP46_1_H300_V150_C45_MF_285 | 0.11147 | 0.11141 | 0.10959 | 0.12048 | 0.11636 | 0.13283 | 0.15246 | 0.14927 | 0.15682 | 0.15534 | 0.16649 | 0.16569 | 0.1565 | 0.16206 | 0.16974 | 0.14615 | 0.12189 | 0.1363
VP49_1_H400_V150_C45_MF_285 | 0.23407 | 0.25346 | 0.23559 | 0.23815 | 0.22553 | 0.20534 | 0.21879 | 0.21803 | 0.24513 | 0.24085 | 0.23358 | 0.24188 | 0.22542 | 0.239 | 0.23757 | 0.23632 | 0.22613 | 0.25522
VP50_1_H500_V150_C45_MF_285 | 0.2344 | 0.22951 | 0.21666 | 0.205 | 0.17604 | 0.18634 | 0.19995 | 0.21473 | 0.22099 | 0.22512 | 0.23895 | 0.23142 | 0.23586 | 0.23021 | 0.21991 | 0.21942 | 0.20997 | 0.25751
Notes: Heat partition into workpiece independent from vc and hsp does not fit to K&H
Decreases for small chip thickness

## Slide 22: Time and spatial varying thermal properties Friction coefficient µ for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136
VP42_1_H300_V100_C45_MF_425 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572
VP43_1_H400_V100_C45_MF_285 | 0.54011 | 0.54011 | 0.54011 | 0.54011 | 0.54011 | 0.54011
VP45_2_H200_V150_C45_MF_425 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074
VP46_1_H300_V150_C45_MF_285 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265
VP49_1_H400_V150_C45_MF_285 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174
VP50_1_H500_V150_C45_MF_285 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012

## Slide 23: Time and spatial varying thermal properties Heat partition ratios for hsp = 200 µm, vc = 100 m/min
Chart: Workpiece position [mm]
| 113,62 | 118,70 | 123,78 | 128,86 | 133,94 | 139,02 | 144,11 | 149,19 | 154,27 | 159,35 | 164,43 | 169,51 | 174,59 | 179,67 | 184,76 | 189,84 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 - Summe von Percent - Heat inside tool/Total heat | 0.21913 | 0.22468 | 0.20433 | 0.199 | 0.19307 | 0.18613 | 0.18666 | 0.17509 | 0.17049 | 0.1747 | 0.17462 | 0.1743 | 0.17279 | 0.16835 | 0.16555 | 0.16626 | 0.16731 | 0.17245
VP41_2_H200_V100_C45_MF_425 - Summe von Percent - Heat through chip/Total heat | 0.60694 | 0.62951 | 0.60676 | 0.60854 | 0.63899 | 0.63612 | 0.57706 | 0.62093 | 0.66525 | 0.59274 | 0.64887 | 0.66995 | 0.68124 | 0.68587 | 0.66664 | 0.72446 | 0.76721 | 0.71637
VP41_2_H200_V100_C45_MF_425 - Summe von Percent - Heat through workpiece/Total heat | 0.16746 | 0.13933 | 0.18246 | 0.18598 | 0.16146 | 0.17132 | 0.22988 | 0.19757 | 0.15781 | 0.22616 | 0.17007 | 0.1493 | 0.13949 | 0.13931 | 0.16133 | 0.1028 | 0.058992 | 0.10469
Work piece
Tool
Chip

## Slide 24: Temperature distribution for orthogonal cutting Temperature distribution for hsp = 200 µm, vc = 100 m/min
Workpiece position : 124 mm
Workpiece position : 200 mm
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
[°C]
[W]
Chart: 
| 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 9.1003 | 139.5096 | 217.2265 | 342.4747 | 220.7361 | 385.738 | 453.9045 | 581.5819
Chart: 
| 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 20.1655 | 233.9058 | 323.6939 | 226.8855 | 302.6419 | 295.3236 | 312.5295 | 395.5563 | 472.6004

## Slide 25: Time and spatial varying thermal properties Heat partition ratios for hsp = 200 µm, vc = 150 m/min
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 116,16 | 123,78 | 131,40 | 139,02 | 146,65 | 154,27 | 161,89 | 169,51 | 177,13 | 184,76 | 192,38 | 200,00
VP45_2_H200_V150_C45_MF_425 - Summe von Percent - Heat inside tool/Total heat | 0.18442 | 0.19183 | 0.19234 | 0.18505 | 0.19298 | 0.18949 | 0.18915 | 0.18398 | 0.18126 | 0.17588 | 0.1692 | 0.16623 | 0.16042 | 0.15337 | 0.14952 | 0.14503 | 0.14347 | 0.098105
VP45_2_H200_V150_C45_MF_425 - Summe von Percent - Heat through chip/Total heat | 0.67329 | 0.65163 | 0.6527 | 0.65474 | 0.67163 | 0.67741 | 0.6685 | 0.66906 | 0.66967 | 0.65823 | 0.65878 | 0.64473 | 0.66823 | 0.68563 | 0.68656 | 0.7006 | 0.7372 | 0.74156
VP45_2_H200_V150_C45_MF_425 - Summe von Percent - Heat through workpiece/Total heat | 0.13847 | 0.15271 | 0.15113 | 0.15638 | 0.13158 | 0.12927 | 0.13853 | 0.14317 | 0.14527 | 0.16209 | 0.16821 | 0.18522 | 0.16754 | 0.15721 | 0.16012 | 0.15057 | 0.1155 | 0.15651
Work piece
Tool
Chip

## Slide 26
Time and spatial varying thermal properties Temperature distribution for hsp = 200 µm, vc = 150 m/min
Workpiece position : 124 mm
Workpiece position : 200 mm
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
[°C]
[W]
Chart: 
| 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 203.3038 | 323.357 | 360.8375 | 407.538 | 511.4623 | 703.7264
Chart: 
| 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 208.0108 | 282.9195 | 182.1045 | 160.2704 | 184.049 | 263.4118 | 378.4255
Notes: With higher cutting speed and lower chip thickness more heat is transferred over tip

## Slide 27: Time and spatial varying thermal properties Heat partition ratios for hsp = 300 µm, vc = 100 m/min
Chart: Workpiece position [mm]
| 113,62 | 118,70 | 123,78 | 128,86 | 133,94 | 139,02 | 144,11 | 149,19 | 154,27 | 159,35 | 164,43 | 169,51 | 174,59 | 179,67 | 184,76 | 189,84 | 194,92 | 200,00
VP42_1_H300_V100_C45_MF_425 - Summe von Percent - Heat inside tool/Total heat | 0.13957 | 0.14168 | 0.13918 | 0.13867 | 0.13927 | 0.13559 | 0.13271 | 0.12981 | 0.12854 | 0.14051 | 0.15451 | 0.13528 | 0.13312 | 0.11829 | 0.12202 | 0.11423 | 0.11362 | 0.1059
VP42_1_H300_V100_C45_MF_425 - Summe von Percent - Heat through chip/Total heat | 0.64915 | 0.63576 | 0.65008 | 0.64768 | 0.66579 | 0.64883 | 0.64075 | 0.65156 | 0.651 | 0.65515 | 0.6604 | 0.66746 | 0.6593 | 0.68398 | 0.69456 | 0.69385 | 0.74128 | 0.74377
VP42_1_H300_V100_C45_MF_425 - Summe von Percent - Heat through workpiece/Total heat | 0.20644 | 0.21769 | 0.20585 | 0.20875 | 0.19005 | 0.21068 | 0.22169 | 0.21376 | 0.21562 | 0.19949 | 0.1802 | 0.19239 | 0.20272 | 0.19287 | 0.17854 | 0.18708 | 0.14025 | 0.14544
Tool
Work piece
Chip

## Slide 28
Time and spatial varying thermal properties Temperature distribution for hsp = 300 µm, vc = 100 m/min
Workpiece position : 124 mm
Workpiece position : 200 mm
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
[°C]
[W]
Chart: 
| 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 76.8222 | 100.5985 | 97.966 | 177.9767 | 275.9327 | 295.056 | 338.89 | 408.5537 | 536.928
Chart: 
| 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 61.0974 | 88.2377 | 126.5558 | 197.9065 | 238.4206 | 238.8037 | 309.4507 | 352.8802 | 366.4979

## Slide 29: Time and spatial varying thermal properties Heat partition ratios for hsp = 300 µm, vc = 150 m/min
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 116,16 | 123,78 | 131,40 | 139,02 | 146,65 | 154,27 | 161,89 | 169,51 | 177,13 | 184,76 | 192,38 | 200,00
VP46_1_H300_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.20085 | 0.20329 | 0.19785 | 0.19785 | 0.18634 | 0.17591 | 0.16919 | 0.16996 | 0.16315 | 0.15791 | 0.14564 | 0.13832 | 0.1449 | 0.13888 | 0.12668 | 0.13508 | 0.12669 | 0.11191
VP46_1_H300_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.68413 | 0.68175 | 0.68902 | 0.67814 | 0.69377 | 0.68774 | 0.67482 | 0.67723 | 0.67652 | 0.68321 | 0.68433 | 0.69244 | 0.69505 | 0.69551 | 0.70006 | 0.71522 | 0.7479 | 0.74824
VP46_1_H300_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.11147 | 0.11141 | 0.10959 | 0.12048 | 0.11636 | 0.13283 | 0.15246 | 0.14927 | 0.15682 | 0.15534 | 0.16649 | 0.16569 | 0.1565 | 0.16206 | 0.16974 | 0.14615 | 0.12189 | 0.1363
VP46_2_H300_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.20476 | 0.20304 | 0.20915 | 0.20481 | 0.18876 | 0.18222 | 0.17014 | 0.1658 | 0.16505 | 0.16152 | 0.15391 | 0.14722 | 0.14278 | 0.13874 | 0.13458 | 0.13107 | 0.13266 | 0.10452
VP46_2_H300_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.69408 | 0.6853 | 0.67724 | 0.68756 | 0.69731 | 0.68802 | 0.6971 | 0.6837 | 0.68455 | 0.69855 | 0.68372 | 0.69243 | 0.69087 | 0.69032 | 0.70817 | 0.70888 | 0.74403 | 0.76151
VP46_2_H300_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.097548 | 0.10804 | 0.11003 | 0.10404 | 0.11032 | 0.12617 | 0.12916 | 0.1469 | 0.14679 | 0.13634 | 0.15875 | 0.15674 | 0.16277 | 0.16735 | 0.15363 | 0.15643 | 0.11969 | 0.13039
Work piece
Tool
Chip

## Slide 30
Time and spatial varying thermal properties Temperature distribution for hsp = 300 µm, vc = 150 m/min
Workpiece position : 124 mm
Workpiece position : 200 mm
Chart: 
| 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 31.9529 | 186.5284 | 236.7895 | 325.124 | 417.3095 | 509.687 | 657.2823 | 876.3003
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
[°C]
[W]
Chart: 
| 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 19.7059 | 178.4143 | 169.0574 | 179.0231 | 263.8184 | 339.1859 | 352.3603 | 446.9513 | 562.8532

## Slide 31: Time and spatial varying thermal properties Heat partition ratios for hsp = 400 µm, vc = 100 m/min
Chart: Workpiece position [mm]
| 113,62 | 118,70 | 123,78 | 128,86 | 133,94
Summe von Percent - Heat inside tool/Total heat | 0.1394 | 0.088931 | 0.15835 | 0.14063 | 0.13255
Summe von Percent - Heat through chip/Total heat | 0.64724 | 0.65635 | 0.66524 | 0.66103 | 0.67155
Summe von Percent - Heat through workpiece/Total heat | 0.21335 | 0.25472 | 0.1764 | 0.19833 | 0.1959
Tool
Work piece
Chip

## Slide 32: Time and spatial varying thermal properties Heat partition ratios for hsp = 400 µm, vc = 150 m/min
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 116,16 | 123,78 | 131,40 | 139,02 | 146,65 | 154,27 | 161,89 | 169,51 | 177,13 | 184,76 | 192,38 | 200,00
VP49_1_H400_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.14761 | 0.14445 | 0.14376 | 0.13728 | 0.12674 | 0.1229 | 0.11918 | 0.11805 | 0.11947 | 0.1185 | 0.11353 | 0.11223 | 0.11405 | 0.10995 | 0.10628 | 0.10406 | 0.10055 | 0.077004
VP49_1_H400_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.61522 | 0.59901 | 0.61758 | 0.62149 | 0.64463 | 0.66867 | 0.65894 | 0.66084 | 0.63231 | 0.63757 | 0.64982 | 0.6428 | 0.65742 | 0.64795 | 0.65305 | 0.65652 | 0.67024 | 0.66469
VP49_1_H400_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.23407 | 0.25346 | 0.23559 | 0.23815 | 0.22553 | 0.20534 | 0.21879 | 0.21803 | 0.24513 | 0.24085 | 0.23358 | 0.24188 | 0.22542 | 0.239 | 0.23757 | 0.23632 | 0.22613 | 0.25522
VP49_2_H400_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.14086 | 0.15223 | 0.14327 | 0.13501 | 0.12858 | 0.12509 | 0.1215 | 0.12024 | 0.11886 | 0.11363 | 0.11502 | 0.11408 | 0.11074 | 0.10742 | 0.10334 | 0.099616 | 0.10429 | 0.075123
VP49_2_H400_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.60865 | 0.63929 | 0.63015 | 0.67285 | 0.68218 | 0.6776 | 0.69015 | 0.66985 | 0.68514 | 0.68118 | 0.66279 | 0.67321 | 0.68914 | 0.70214 | 0.68701 | 0.71862 | 0.69867 | 0.66834
VP49_2_H400_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.24724 | 0.20521 | 0.22332 | 0.18888 | 0.18599 | 0.19406 | 0.18508 | 0.20667 | 0.19272 | 0.20194 | 0.21893 | 0.20944 | 0.19684 | 0.1872 | 0.2064 | 0.17851 | 0.19377 | 0.25328
Tool
Work piece
Chip

## Slide 33
Chart: 
| 560.0 | 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 80.7151 | 320.6505 | 164.6276 | 258.5114 | 292.081 | 307.2485 | 295.4871 | 320.948 | 442.4843 | 487.8577
Time and spatial varying thermal properties Temperature distribution for hsp = 400 µm, vc = 150 m/min [1/2]
Workpiece position : 124 mm
Workpiece position : 200 mm
Chart: 
| 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 68.689 | 268.2742 | 250.5316 | 437.5165 | 522.3134 | 526.7539 | 484.8667 | 611.3435 | 820.1525
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines
[°C]
[W]

## Slide 34
Chart: 
| 560.0 | 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 192.8838 | 257.8368 | 210.0623 | 233.8197 | 235.1887 | 246.4138 | 260.4695 | 317.5629 | 415.2001 | 462.272
Time and spatial varying thermal properties Temperature distribution for hsp = 400 µm, vc = 150 m/min [2/2]
Workpiece position : 124 mm
Workpiece position : 200 mm
Chart: 
| 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 237.8927 | 166.411 | 165.4571 | 350.3633 | 437.1715 | 468.495 | 479.0329 | 604.9173 | 808.0161
[°C]
[W]
[°C]
[W]
Heat flow through the isothermal lines
Heat flow through the isothermal lines

## Slide 35: Time and spatial varying thermal properties Heat partition ratios for hsp = 500 µm, vc = 150 m/min
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 116,16 | 123,78 | 131,40 | 139,02 | 146,65 | 154,27 | 161,89 | 169,51 | 177,13 | 184,76 | 192,38 | 200,00
VP50_1_H500_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.13622 | 0.12947 | 0.12241 | 0.11812 | 0.11404 | 0.11035 | 0.10746 | 0.1048 | 0.10472 | 0.10517 | 0.1002 | 0.097635 | 0.094481 | 0.091374 | 0.087008 | 0.084166 | 0.083078 | 0.054109
VP50_1_H500_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.6265 | 0.63812 | 0.65803 | 0.67398 | 0.70702 | 0.70043 | 0.68971 | 0.67757 | 0.67139 | 0.66681 | 0.65798 | 0.66806 | 0.66678 | 0.67553 | 0.69019 | 0.69354 | 0.70406 | 0.68549
VP50_1_H500_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.2344 | 0.22951 | 0.21666 | 0.205 | 0.17604 | 0.18634 | 0.19995 | 0.21473 | 0.22099 | 0.22512 | 0.23895 | 0.23142 | 0.23586 | 0.23021 | 0.21991 | 0.21942 | 0.20997 | 0.25751
VP50_2_H500_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.13555 | 0.13286 | 0.12401 | 0.12047 | 0.11436 | 0.11106 | 0.11061 | 0.10729 | 0.10389 | 0.10806 | 0.10416 | 0.099669 | 0.095733 | 0.091482 | 0.088766 | 0.087869 | 0.085412 | 0.053271
VP50_2_H500_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.6415 | 0.65939 | 0.65955 | 0.69394 | 0.73029 | 0.71535 | 0.71119 | 0.69405 | 0.69127 | 0.67765 | 0.68556 | 0.67657 | 0.68968 | 0.68217 | 0.69574 | 0.69898 | 0.70165 | 0.67331
VP50_2_H500_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.21996 | 0.20476 | 0.21346 | 0.1826 | 0.15237 | 0.1706 | 0.1752 | 0.19566 | 0.20186 | 0.21132 | 0.20729 | 0.22078 | 0.21159 | 0.22337 | 0.21252 | 0.21017 | 0.20997 | 0.27045
Tool
Work piece
Chip

## Slide 36
Chart: 
| 600.0 | 560.0 | 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 63.8527 | 560.2505 | 251.2757 | 252.2608 | 230.2662 | 211.3697 | 220.3811 | 278.852 | 347.0043 | 400.8129 | 385.539
Chart: 
| 520.0 | 480.0 | 440.0 | 400.0 | 360.0 | 320.0 | 280.0 | 240.0 | 200.0
Heat flow through the isothermal lines | 279.47 | 190.28 | 318.99 | 368.67 | 455.56 | 463.8 | 546.98 | 679.2 | 834.14
Time and spatial varying thermal properties Temperature distribution for hsp = 500 µm, vc = 150 m/min
Workpiece position : 200 mm
[°C]
[W]
[°C]
[W]
Workpiece position : 124 mm
Heat flow through the isothermal lines
Heat flow through the isothermal lines

## Slide 37: Time and spatial varying thermal properties Conclusion
XYZ

## Slide 38: Time and spatial varying thermal properties Means to enhance quality of measurement
Determine emissivity of chip/tool/workpiece
  Collect chips
  Heating + Pyrometer + Camera
  e (DL)
  Regression of Tcam (DL, ecam) for IT
Enhance quantity of valid pixels
  Expand field of measurement
  Measurement with multiple integration times
  Overlap pictures via algorithm
Determine workpiece directly
  Separate measurements for the work piece
  Compare Heat flows with Ptotal

## Slide 39: Gliederung
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Influence of uncut chip thickness and cutting velocity
3.2
Time and spatial varying thermal properties
3.1
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 40: Influence of uncut chip thickness and cutting velocity Workpiece position 124 mm
ap = 3,5 mm, = 6°, = 3°, = 0, uncoated, workpiece position: 124 mm
Chart: Heat partition (chip)
| 100,00 | 150,00
200,00 | 0.60676 | 0.66906
300,00 | 0.65008 | 0.67723
400,00 | 0.66524 | 0.66084
500,00 | 0.67757
Chart: Heat partition (tool)
| 100.0 | 150.0
200,00 | 0.21078 | 0.18777
300,00 | 0.14408 | 0.1735
400,00 | 0.1326 | 0.12113
500,00 | 0.1077
Chart: Heat flow (chip) [W]
| 100,00 | 150,00
200,00 | 1451.366 | 2209.5729
300,00 | 2208.0209 | 3055.4101
400,00 | 2734.291 | 4006.6247
500,00 | 4892.1433
Chart: Heat flow (workpiece) [W]
| 100.0 | 150.0
200,00 | 436.448 | 472.8265
300,00 | 699.1714 | 673.4511
400,00 | 837.71 | 1321.8743
500,00 | 1550.4084
Chart: Heat partition (workpiece)
| 100.0 | 150.0
200,00 | 0.18246 | 0.14317
300,00 | 0.20585 | 0.14927
400,00 | 0.20381 | 0.21803
500,00 | 0.21473
hsp [µm]
Cutting velocity [m/min]
Chart: Heat flow (tool) [W]
| 100.0 | 150.0
200,00 | 504.1976 | 620.1267
300,00 | 489.3581 | 782.7941
400,00 | 554.7424 | 734.4101
500,00 | 777.6082

## Slide 41: Influence of uncut chip thickness and cutting velocity Workpiece position 200 mm
ap = 3,5 mm, = 6°, = 3°, = 0, uncoated, workpiece position: 200 mm
Chart: Heat flow (chip) [W]
| 100,00 | 150,00
200,00 | 1704.9593 | 2425.7515
300,00 | 2526.242 | 3375.8082
400,00 | 4015.3245
500,00 | 4981.0634
Chart: Heat partition (chip)
| 100,00 | 150,00
200,00 | 0.71637 | 0.74156
300,00 | 0.74377 | 0.74824
400,00 | 0.66469
500,00 | 0.68549
Chart: Heat partition (tool)
| 100,00 | 150,00
200,00 | 0.17245 | 0.098105
300,00 | 0.1059 | 0.11191
400,00 | 0.077004
500,00 | 0.054109
Chart: Heat flow (workpiece) [W]
| 100,00 | 150,00
200,00 | 249.163 | 511.9606
300,00 | 494.002 | 614.942
400,00 | 1541.7394
500,00 | 1871.1986
Chart: Heat partition (workpiece)
| 100,00 | 150,00
200,00 | 0.10469 | 0.15651
300,00 | 0.14544 | 0.1363
400,00 | 0.25522
500,00 | 0.25751
Chart: Heat flow (tool) [W]
| 100,00 | 150,00
200,00 | 425.8658 | 333.451
300,00 | 376.3064 | 520.9051
400,00 | 483.8331
500,00 | 414.1149
hsp [µm]
Cutting velocity [m/min]

## Slide 42: Gliederung
Influence of uncut chip thickness and cutting velocity
4.2
Time and spatial varying thermal properties
4.1
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 43: Gliederung
Influence of uncut chip thickness and cutting velocity
4.2
Time and spatial varying thermal properties
4.1
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 44
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 321.3902 | 367.561 | 410.1505 | 395.1678 | 432.9221 | 449.1885 | 454.0863 | 469.7017
VP33_1_H300_V150_ACF_MF_285 | 371.9721 | 332.6266 | 411.2879 | 422.8724 | 455.4693 | 418.2797 | 417.113 | 500.5418
VP36_1_H200_V100_ABA_MF_285 | 349.5812 | 360.4937 | 357.1486 | 361.008 | 370.1721 | 380.1351 | 386.0042 | 387.3429 | 387.6348 | 392.4169 | 399.6261
VP37_1_H200_V150_ABA_MF_425 | 318.1848 | 337.8549 | 348.1765 | 363.7722 | 372.187 | 370.5649 | 383.7259 | 397.4685
VP38_1_H300_V100_ABA_MF_425 | 382.1139 | 402.2912 | 402.8205 | 408.1818 | 413.1409 | 431.4014 | 434.8009 | 443.6369 | 445.5173 | 447.2252 | 455.9241
VP39_1_H300_V150_ABA_MF_425 | 373.6612 | 358.1595 | 413.5302 | 409.9127 | 435.0396 | 446.674 | 454.036 | 464.5749
VP4_1_H300_V100_ACF_MF_285 | 285.7404 | 297.4284 | 320.7272 | 308.9522 | 331.8331 | 355.2696 | 318.6728 | 354.2421 | 284.6421 | 194.974 | 506.3026
VP40_1_H400_V150_ABA_MF_425 | 385.2255 | 426.9951 | 428.2603 | 427.7184 | 436.8727 | 422.9702 | 449.8983 | 428.6826
VP5_2_H200_V100_ACF_MF_285 | 272.4543 | 252.3369 | 279.3771 | 257.7996 | 284.924 | 287.6386 | 285.9041 | 307.4738 | 485.4433 | 403.6575 | 488.5987
VP6_1_H100_V100_ACF_MF_285 | 245.3085 | 104.1934 | 251.8863 | 269.8535 | 216.212 | 243.917 | 262.8675 | 372.8918 | 263.803 | 407.4966 | 428.8904

## Slide 45
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 0.31408 | 0.56535 | 0.83945 | 1.0449 | 1.3901 | 1.7175 | 2.0659 | 2.3568
VP33_1_H300_V150_ACF_MF_285 | 0.59116 | 0.84752 | 1.1029 | 0.67127 | 0.9798 | 1.4797 | 1.9825 | 2.361
VP36_1_H200_V100_ABA_MF_285 | 0.61608 | 0.82106 | 1.084 | 1.2591 | 1.3743 | 1.4835 | 1.5734 | 1.6395 | 1.7275 | 1.8411 | 1.979
VP37_1_H200_V150_ABA_MF_425 | 0.32515 | 0.44336 | 0.58506 | 0.7498 | 0.92807 | 1.1313 | 1.3282 | 1.4519
VP38_1_H300_V100_ABA_MF_425 | 0.8236 | 1.0697 | 1.338 | 1.6743 | 1.925 | 2.1278 | 2.3352 | 2.4781 | 2.6058 | 2.7855 | 2.9973
VP39_1_H300_V150_ABA_MF_425 | 0.53181 | 0.66833 | 0.98678 | 1.2182 | 1.4779 | 1.9045 | 2.2954 | 2.5762
VP4_1_H300_V100_ACF_MF_285 | 0.79698 | 1.076 | 1.4035 | 1.9091 | 2.1115 | 2.5019 | 2.695 | 2.9157 | 3.1033 | 3.568 | 4.2008
VP40_1_H400_V150_ABA_MF_425 | 0.6531 | 0.82723 | 1.0792 | 1.3428 | 1.6944 | 1.969 | 2.2499 | 2.4618
VP5_2_H200_V100_ACF_MF_285 | 0.40798 | 0.61554 | 0.81328 | 1.2086 | 1.2974 | 1.8634 | 2.0269 | 2.1183 | 2.8823 | 3.0771 | 3.3187
VP6_1_H100_V100_ACF_MF_285 | 0.23428 | 0.10862 | 0.087523 | 0.26349 | 0.55101 | 0.68685 | 0.77571 | 1.0349 | 0.91902 | 1.2178 | 1.3081

## Slide 46
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 12.6955 | 12.6955 | 12.6955 | 12.6955 | 12.6955 | 12.6955 | 12.6955 | 12.6955
VP33_1_H300_V150_ACF_MF_285 | 9.9915 | 9.9915 | 9.9915 | 9.9915 | 9.9915 | 9.9915 | 9.9915 | 9.9915
VP36_1_H200_V100_ABA_MF_285 | 8.0893 | 8.0893 | 8.0893 | 8.0893 | 8.0893 | 8.0893 | 8.0893 | 8.0893 | 8.0893 | 8.0893 | 8.0893
VP37_1_H200_V150_ABA_MF_425 | 7.2382 | 7.2382 | 7.2382 | 7.2382 | 7.2382 | 7.2382 | 7.2382 | 7.2382
VP38_1_H300_V100_ABA_MF_425 | 13.8213 | 13.8213 | 13.8213 | 13.8213 | 13.8213 | 13.8213 | 13.8213 | 13.8213 | 13.8213 | 13.8213 | 13.8213
VP39_1_H300_V150_ABA_MF_425 | 13.0426 | 13.0426 | 13.0426 | 13.0426 | 13.0426 | 13.0426 | 13.0426 | 13.0426
VP4_1_H300_V100_ACF_MF_285 | 20.353 | 20.353 | 20.353 | 20.353 | 20.353 | 20.353 | 20.353 | 20.353 | 20.353 | 20.353 | 20.353
VP40_1_H400_V150_ABA_MF_425 | 11.6779 | 11.6779 | 11.6779 | 11.6779 | 11.6779 | 11.6779 | 11.6779 | 11.6779
VP5_2_H200_V100_ACF_MF_285 | 19.4565 | 19.4565 | 19.4565 | 19.4565 | 19.4565 | 19.4565 | 19.4565 | 19.4565 | 19.4565 | 19.4565 | 19.4565
VP6_1_H100_V100_ACF_MF_285 | 8.2555 | 8.2555 | 8.2555 | 8.2555 | 8.2555 | 8.2555 | 8.2555 | 8.2555 | 8.2555 | 8.2555 | 8.2555

## Slide 47
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 1594.6527 | 1758.2159 | 1982.0562 | 1850.8901 | 1825.6445 | 1876.9059 | 2036.7403 | 2179.0138
VP33_1_H300_V150_ACF_MF_285 | 2770.8108 | 2609.1584 | 2569.644 | 2617.3778 | 2630.5351 | 2608.5191 | 2681.1743 | 2995.518
VP36_1_H200_V100_ABA_MF_285 | 1202.8587 | 1216.6629 | 1235.8852 | 1262.0608 | 1257.6486 | 1305.7559 | 1277.4352 | 1279.4278 | 1291.7793 | 1320.4503 | 1287.87
VP37_1_H200_V150_ABA_MF_425 | 1869.7601 | 1808.0195 | 1889.4131 | 1873.4656 | 1855.9529 | 1931.4035 | 1958.6705 | 2069.6085
VP38_1_H300_V100_ABA_MF_425 | 1902.1348 | 1937.641 | 1862.1379 | 1784.5578 | 1928.0247 | 1832.2297 | 1992.2857 | 1876.1866 | 1933.1588 | 2110.3964 | 2096.4155
VP39_1_H300_V150_ABA_MF_425 | 2887.2698 | 2791.4786 | 2677.1419 | 3211.2793 | 3305.0238 | 3368.6602 | 3301.8236 | 3317.1531
VP4_1_H300_V100_ACF_MF_285 | 1640.1197 | 1635.65 | 1639.1284 | 1711.7443 | 1749.655 | 1747.4185 | 1788.1253 | 1783.8362 | 1822.0647 | 2077.8457 | 2061.9343
VP40_1_H400_V150_ABA_MF_425 | 3235.3085 | 2910.8211 | 3632.1106 | 3815.6384 | 3514.3823 | 3706.9548 | 3777.1449 | 3718.2853
VP5_2_H200_V100_ACF_MF_285 | 1122.4392 | 1129.2216 | 1150.0824 | 1214.0439 | 1200.1641 | 1261.9271 | 1271.2989 | 1302.2193 | 1346.7622 | 1500.0549 | 1446.6439
VP6_1_H100_V100_ACF_MF_285 | 566.3211 | 539.7141 | 580.2875 | 581.9489 | 575.6727 | 586.1007 | 613.8167 | 577.766 | 612.0218 | 643.2098 | 641.1979

## Slide 48
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 0.62364 | 0.68761 | 0.77012 | 0.72385 | 0.70838 | 0.7331 | 0.79654 | 0.85218
VP33_1_H300_V150_ACF_MF_285 | 0.82244 | 0.77615 | 0.75923 | 0.77515 | 0.77722 | 0.77163 | 0.79218 | 0.89012
VP36_1_H200_V100_ABA_MF_285 | 0.6195 | 0.62661 | 0.63651 | 0.64815 | 0.64461 | 0.67059 | 0.65605 | 0.65894 | 0.6653 | 0.68007 | 0.66141
VP37_1_H200_V150_ABA_MF_425 | 0.67851 | 0.65474 | 0.68564 | 0.68187 | 0.67741 | 0.69943 | 0.7149 | 0.75469
VP38_1_H300_V100_ABA_MF_425 | 0.66941 | 0.6819 | 0.65533 | 0.617 | 0.6771 | 0.63498 | 0.68882 | 0.65021 | 0.66838 | 0.73473 | 0.72653
VP39_1_H300_V150_ABA_MF_425 | 0.65894 | 0.63016 | 0.60839 | 0.72977 | 0.74437 | 0.76554 | 0.75035 | 0.74882
VP4_1_H300_V100_ACF_MF_285 | 0.71074 | 0.71536 | 0.71599 | 0.74381 | 0.76231 | 0.75932 | 0.78205 | 0.7772 | 0.78958 | 0.90647 | 0.89353
VP40_1_H400_V150_ABA_MF_425 | 0.67518 | 0.60353 | 0.75309 | 0.79463 | 0.72868 | 0.77281 | 0.78661 | 0.77517
VP5_2_H200_V100_ACF_MF_285 | 0.66631 | 0.6655 | 0.67981 | 0.72068 | 0.70731 | 0.74806 | 0.75673 | 0.76746 | 0.79371 | 0.89047 | 0.85635
VP6_1_H100_V100_ACF_MF_285 | 0.59892 | 0.5753 | 0.61059 | 0.61545 | 0.6098 | 0.62185 | 0.65125 | 0.61492 | 0.65138 | 0.68562 | 0.6803

## Slide 53: Gliederung
Influence of uncut chip thickness and cutting velocity
4.2
Time and spatial varying thermal properties
4.1
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1