## Slide 1: Results – Method 1
Experimental investigation of temperatures and heat flows for orthogonal cutting 1045/4140 steel by thermal imaging

## Slide 2: Gliederung
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 3: Gliederung
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 4: Experimental Setup Design of Experiment
Thermal camera
Workpiece
Tool
Cutting process
Area covered by the thermal camera

## Slide 5: Experimental Setup Design of Experiment for AISI 1045
Experiments | Cutting Velocity [m/min] | Uncut chip thickness [µm] | Integration time [µs] | Cutting Force [N] | Passive Force [N] | Heat treatment
VP41_1_H200_V100_C45_MF_425 | 100 | 200 | 425 | 1500 | 1000 | Normalized
VP41_2_H200_V100_C45_MF_425 | 100 | 200 | 425 | 1565 | 1005 | Normalized
VP42_1_H300_V100_C45_MF_425 | 100 | 300 | 425 | 2250 | 1159 | Normalized
VP42_2_H300_V100_C45_MF_285 | 100 | 300 | 285 | 2136 | 1079 | Normalized
VP43_1_H400_V100_C45_MF_285 | 100 | 400 | 285 | 2716 | 1118 | Normalized
VP45_2_H200_V150_C45_MF_425 | 150 | 200 | 425 | 1448 | 688 | Normalized
VP46_1_H300_V150_C45_MF_285 | 150 | 300 | 285 | 2006 | 801 | Normalized
VP46_2_H300_V150_C45_MF_285 | 150 | 300 | 285 | 2004 | 875 | Normalized
VP49_1_H400_V150_C45_MF_285 | 150 | 400 | 285 | 2675 | 1046 | Normalized
VP49_2_H400_V150_C45_MF_285 | 150 | 400 | 285 | 2590 | 1000 | Normalized
VP50_1_H500_V150_C45_MF_285 | 150 | 500 | 285 | 3220 | 1120 | Normalized
VP50_2_H500_V150_C45_MF_285 | 150 | 500 | 285 | 3178 | 1162 | Normalized

## Slide 6: Experimental Setup Design of Experiment for AISI 4140 [1/2]
Experiments | Cutting Velocity [m/min] | Uncut chip thickness [µm] | Integration time [µs] | Cutting Force [N] | Passive Force [N] | Heat treatment
VP4_1_H300_V100_ACF_MF_285 | 100 | 300 | 285 | 1520 | 691 | Normalized
VP4_2_H300_V100_ACF_MF_285 | 100 | 300 | 285 | 1560 | 734 | Normalized
VP5_1_H200_V100_ACF_MF_285 | 100 | 200 | 285 | 1105 | 556 | Normalized
VP5_2_H200_V100_ACF_MF_285 | 100 | 200 | 285 | 1113 | 546 | Normalized
VP6_1_H100_V100_ACF_MF_285 | 100 | 100 | 285 | 619 | 361 | Normalized
VP32_1_H200_V150_ACF_MF_285 | 150 | 200 | 285 | 1133 | 519 | Normalized
VP32_2_H200_V150_ACF_MF_285 | 150 | 200 | 285 | 1054 | 496 | Normalized
VP33_1_H300_V150_ACF_MF_285 | 150 | 300 | 285 | 1495 | 538 | Normalized
VP36_1_H200_V100_ABA_MF_285 | 100 | 200 | 285 | 1302 | 400 | Tempered
VP36_2_H200_V100_ABA_MF_425 | 100 | 200 | 425 | 1242 | 436 | Tempered
VP36_3_H200_V100_ABA_MF_425 | 100 | 200 | 425 | 1295 | 410 | Tempered
VP37_1_H200_V150_ABA_MF_425 | 150 | 200 | 425 | 1225 | 373 | Tempered

## Slide 7: Experimental Setup Design of Experiment for AISI 4140 [2/2]
Experiments | Cutting Velocity [m/min] | Uncut chip thickness [µm] | Integration time [µs] | Cutting Force [N] | Passive Force [N] | Heat treatment
VP37_2_H200_V150_ABA_MF_425 | 150 | 200 | 425 | 1260 | 362 | Tempered
VP38_1_H300_V100_ABA_MF_425 | 100 | 300 | 425 | 1846 | 1574 | Tempered
VP38_2_H300_V100_ABA_MF_425 | 100 | 300 | 425 | 2028 | 1633 | Tempered
VP39_1_H300_V150_ABA_MF_425 | 150 | 300 | 425 | 1892 | 1576 | Tempered
VP39_2_H300_V150_ABA_MF_425 | 150 | 300 | 425 | 1936 | 1820 | Tempered

## Slide 8: Experimental Setup Boundary Conditions for AISI 1045
Boundary Conditions |  |  |  |  | 
Tool |  | Camera |  | Workpiece | 
Heat Conductivity [W/(mK)] | 75,4 | Pixel pitch (Infrared Camera) [mm/pixel] | 0,015 | Length of the workpiece [mm] | 200
Heat Capacity [J/(cm^3K)] | Interpolation* | Maximum digit level valid (FLIR X) | 8192 | Heat Capacity [J/(kgK)] | Interpolation**
Rake Angle [°] | 6 | Maximum digit level valid (FLIR SC7600) | 16000 | Workpiece Material | AISI 1045 (normalized)
Clearance Angle [°] | 3 | Frame Rate (Infrared Camera) [Hz] | 328 | Depth of Cut ap [mm] | 3,5
Assumed percentage of heat conducted away by convection and radiation | 0,03 | Minimum valid temperature for the frames [°C] | 200 | Maximum error of the workpiece position for = 100 [mm/mm] | 0,0255
Cutting edge radius [µm] | < 5 | Emissivity (Experimentally determined - tool and workpiece coated) | 0,85 | Maximum error of the workpiece position for = 150 [mm/mm] | 0,038
 |  |  |  | Percentage of the deformation energy converted into heat | 0,9
 |  |  |  | Density (based on steel) [kg/m^3] | 7874
Boundary Conditions |  |  |  |  | 
Tool |  | Camera |  | Workpiece | 
Heat Conductivity [W/(mK)] | 75,4 | Pixel pitch (Infrared Camera) [mm/pixel] | 0,015 | Length of the workpiece [mm] | 200
Heat Capacity [J/(cm^3K)] | Interpolation* | Maximum digit level valid (FLIR X) | 8192 | Heat Capacity [J/(kgK)] | Interpolation**
Rake Angle [°] | 6 | Maximum digit level valid (FLIR SC7600) | 16000 | Workpiece Material | AISI 1045 (normalized)
Clearance Angle [°] | 3 | Frame Rate (Infrared Camera) [Hz] | 328 | Depth of Cut ap [mm] | 3,5
Assumed percentage of heat conducted away by convection and radiation | 0,03 | Minimum valid temperature for the frames [°C] | 200 |  | 0,0255
Cutting edge radius [µm] | < 5 | Emissivity (Experimentally determined - tool and workpiece coated) | 0,85 |  | 0,038
 |  |  |  | Percentage of the deformation energy converted into heat | 0,9
 |  |  |  | Density (based on steel) [kg/m^3] | 7874
*Tool [J/(cm^3K)] |  | 
**Workpiece [J/(kgK)] |  | 
Interpolation

## Slide 9: Experimental Setup Boundary Conditions for AISI 4140
Boundary Conditions |  |  |  |  | 
Tool |  | Camera |  | Workpiece | 
Heat Conductivity [W/(mK)] | 75,4 | Pixel pitch (Infrared Camera) [mm/pixel] | 0,015 | Length of the workpiece [mm] | 80
Heat Capacity [J/(cm^3K)] | Interpolation* | Maximum digit level valid (FLIR X) | 8192 | Heat Capacity [J/(kgK)] | Interpolation**
Rake Angle [°] | 6 | Maximum digit level valid (FLIR SC7600) | 16000 | Workpiece Material | AISI 4140 (normalized / tempered)
Clearance Angle [°] | 3 | Frame Rate (Infrared Camera) [Hz] | 328 | Depth of Cut ap [mm] | 2,8
Assumed percentage of heat conducted away by convection and radiation | 0,03 | Minimum valid temperature for the frames [°C] | 200 | Maximum error of the workpiece position for = 100 [mm/mm] | 0,064
Cutting edge radius [µm] | 66 | Emissivity (Experimentally determined - tool and workpiece coated) | 0,85 | Maximum error of the workpiece position for = 150 [mm/mm] | 0,095
 |  |  |  | Percentage of the deformation energy converted into heat | 0,9
 |  |  |  | Density (based on steel) [kg/m^3] | 7874
Boundary Conditions |  |  |  |  | 
Tool |  | Camera |  | Workpiece | 
Heat Conductivity [W/(mK)] | 75,4 | Pixel pitch (Infrared Camera) [mm/pixel] | 0,015 | Length of the workpiece [mm] | 80
Heat Capacity [J/(cm^3K)] | Interpolation* | Maximum digit level valid (FLIR X) | 8192 | Heat Capacity [J/(kgK)] | Interpolation**
Rake Angle [°] | 6 | Maximum digit level valid (FLIR SC7600) | 16000 | Workpiece Material | AISI 4140 (normalized / tempered)
Clearance Angle [°] | 3 | Frame Rate (Infrared Camera) [Hz] | 328 | Depth of Cut ap [mm] | 2,8
Assumed percentage of heat conducted away by convection and radiation | 0,03 | Minimum valid temperature for the frames [°C] | 200 |  | 0,064
Cutting edge radius [µm] | 66 | Emissivity (Experimentally determined - tool and workpiece coated) | 0,85 |  | 0,095
 |  |  |  | Percentage of the deformation energy converted into heat | 0,9
 |  |  |  | Density (based on steel) [kg/m^3] | 7874
*Tool [J/(cm^3K)] |  | 
**Workpiece [J/(kgK)] |  | 
Interpolation

## Slide 10: Gliederung
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 11: Post processing of thermal pictures Energy balance in the volume control
Tool
Workpiece
Control volume
Inside Energy
Total power produced
  Direct force measurement
Energy from material going inside the control volume
  Always zero ()
Outside Energy
Heat flow into the tool
  Calculation by gradient
Heat flow into the workpiece
  Calculation by heat balance
Energy from the chip going outside
  thermodynamic calculation
Part of deformation energy converted in heat
  90% of the total deformation energy ()
*,
Chip
Notes: In this analysis, the energy flows considered for the volume control are listed above. Then, with the temperature field of the Infrared camera frames, this analysis is able to calculate the heat flow through the tool and the chip and, consequently, the heat partition of the total power produced during the process. About 90% of the deformation energy is converted in heat and the heat flow through the workpiece is calculated by the total balance.

## Slide 12: Post processing of thermal pictures Heat carried away from the tool tip
The heat flow through the tool is calculated as a mean value between the heat flows calculated for the last two lines.
Method based on [BOOTHROYD].
  : heat conductivity
  : length of the line
  : temperature gradient normal to line
  : effective tool width
Tool

## Slide 13: Post processing of thermal pictures Lines along the tool – obtaining process
The drawn lines are normal to the vector
Bigger valid areas (Temperature ≥ 200°C) are obtained due to the resultant direction of .
The lines are equally spaced in 4 pixels (60µm) from each other, and the last one is the tool tip farthest which still has only valid pixels.
: unitary vector on the rake face direction
: unitary vector on the clearance face direction

## Slide 14: Post processing of thermal pictures Temperature gradient – calculation method
Each line along the tool is consisted of pixels, and each pixel has a corresponding temperature ().
Gradients for the red pixel on the x () and y () directions:
So, as is the vector normal to the lines, then the module of the normal component to these lines of the gradient is calculated as:
Tool

## Slide 15: Post processing of thermal pictures Heat carried away by the chip
The heat flow is calculated on the end of contact between chip and tool interfaces
Method based on [BOOTHROYD].
  : heat capacity function
  : chip temperature
  : environment temperature
  : velocity of the chip
  : chip thickness
  : chip width
Tool
Chip
End of contact chip - tool

## Slide 16: Gliederung
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Influence of uncut chip thickness and cutting velocity
3.2
Time and spatial varying thermal properties
3.1
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 17: Time and spatial varying thermal properties Temperature at tool tip [°C] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 323.5206 | 271.9162 | 380.5434 | 341.2377 | 357.2232 | 368.2788 | 230.1309 | 364.6832 | 365.8805 | 343.2452 | 364.6607 | 379.6024 | 393.9241 | 390.0437 | 373.423 | 398.9011 | 411.4206 | 425.8531
VP42_1_H300_V100_C45_MF_425 | 442.907 | 491.0974 | 498.6279 | 450.6018 | 444.4791 | 340.6401 | 471.2703 | 433.7598 | 426.1506 | 282.3214 | 323.3509 | 255.7746 | 504.0463 | 485.6611 | 516.0332 | 517.7154 | 520.8733 | 525.9864
VP43_1_H400_V100_C45_MF_285 | 475.9792 | 406.8634 | 496.2303 | 444.492 | 421.7696 | 195.0595
VP45_2_H200_V150_C45_MF_425 | 363.7171 | 378.5227 | 387.0074 | 395.5219 | 410.6586 | 412.4561 | 402.5545 | 408.8741 | 411.6293 | 408.0815 | 415.8895 | 415.7033 | 420.948 | 444.6016 | 447.3969 | 461.0162 | 447.4671 | 441.2219
VP46_1_H300_V150_C45_MF_285 | 425.3031 | 385.6967 | 416.9808 | 388.6194 | 419.6816 | 428.1679 | 436.2967 | 452.2375 | 437.1667 | 384.2404 | 438.4321 | 320.4099 | 442.1594 | 492.6639 | 486.9684 | 492.3859 | 488.9218 | 505.5068
VP49_1_H400_V150_C45_MF_285 | 414.4026 | 414.7684 | 441.6356 | 253.9839 | 421.9092 | 485.0291 | 476.3299 | 470.3219 | 416.562 | 469.1423 | 474.6055 | 474.9649 | 493.8176 | 495.579 | 514.8465 | 506.6511 | 489.6865 | 469.3475
VP50_1_H500_V150_C45_MF_285 | 412.4521 | 377.9897 | 447.9103 | 416.5194 | 457.2466 | 439.4002 | 506.3999 | 468.2151 | 457.8948 | 424.7005 | 430.3532 | 477.8122 | 511.4966 | 514.4709 | 502.4442 | 486.0228 | 490.5698 | 473.5951

## Slide 18: Time and spatial varying thermal properties Internal energy in tool [Joule] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 6.5224 | 6.7965 | 7.0719 | 7.3539 | 7.8868 | 8.1574 | 7.964 | 8.4782 | 8.7992 | 9.1514 | 9.4147 | 9.5462 | 9.7156 | 9.9526 | 9.8572 | 10.3038 | 10.4344 | 10.4692
VP42_1_H300_V100_C45_MF_425 | 8.6795 | 8.9284 | 9.2325 | 9.6003 | 10.0522 | 10.2113 | 10.5446 | 10.7162 | 10.8376 | 10.3466 | 10.6856 | 11.1312 | 11.4614 | 11.5732 | 12.7034 | 12.9454 | 13.1586 | 13.3152
VP43_1_H400_V100_C45_MF_285 | 9.7584 | 9.8709 | 10.4491 | 10.8884 | 11.2608 | 10.6312
VP45_2_H200_V150_C45_MF_425 | 1.5376 | 1.7419 | 1.9444 | 2.1819 | 2.4671 | 2.7856 | 3.1359 | 3.5036 | 3.8728 | 4.1878 | 4.4347 | 4.6127 | 4.8247 | 5.0665 | 5.3337 | 5.7504 | 6.1824 | 6.4363
VP46_1_H300_V150_C45_MF_285 | 2.5631 | 2.8266 | 3.1545 | 3.4264 | 3.8378 | 4.3676 | 4.87 | 5.4523 | 5.947 | 6.3015 | 6.4102 | 6.6173 | 6.1817 | 7.25 | 7.6531 | 8.1454 | 8.6188 | 8.84
VP49_1_H400_V150_C45_MF_285 | 5.0798 | 5.5896 | 6.1222 | 6.2829 | 6.9385 | 7.5386 | 8.1279 | 8.7742 | 9.371 | 9.8999 | 10.1846 | 10.3374 | 10.5043 | 10.7092 | 11.0906 | 11.6349 | 12.2059 | 12.4869
VP50_1_H500_V150_C45_MF_285 | 6.23 | 6.8538 | 7.3979 | 7.8002 | 8.2048 | 8.7882 | 9.527 | 10.2283 | 11.0142 | 11.6462 | 12.0316 | 12.2152 | 12.3571 | 12.5159 | 12.8927 | 13.4692 | 14.2166 | 14.6323
Notes: The higher the chip thickness the higher the internal energy/heat rate
The lower the cutting speed the higher the internal energy in the tool  High Speed cutting

## Slide 19: Time and spatial varying thermal properties Internal energy rate of the tool [W] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214 | 79.7214
VP42_1_H300_V100_C45_MF_425 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583 | 85.8583
VP43_1_H400_V100_C45_MF_285 | 134 | 134 | 134 | 134 | 134
VP45_2_H200_V150_C45_MF_425 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588 | 97.0588
VP46_1_H300_V150_C45_MF_285 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663 | 123.9663
VP49_1_H400_V150_C45_MF_285 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717 | 144.5717
VP50_1_H500_V150_C45_MF_285 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325 | 162.2325
Notes: Heating rate rises with chip thickness
Heating rate decreases with cutting speed
H/v  Heating rate
1,33
2
4
2
3
2,66
3,333

## Slide 20: Time and spatial varying thermal properties Internal energy carried away by chip [W] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 1446.9037 | 1500.714 | 1451.366 | 1450.7175 | 1523.3013 | 1526.934 | 1392.793 | 1493.1362 | 1594.0554 | 1427.9538 | 1554.7901 | 1602.5165 | 1624.0372 | 1635.069 | 1589.2306 | 1724.2013 | 1825.9456 | 1704.9593
VP42_1_H300_V100_C45_MF_425 | 2227.4118 | 2165.4074 | 2208.0209 | 2199.885 | 2261.3844 | 2203.7899 | 2195.2405 | 2222.4003 | 2237.2376 | 2244.5721 | 2246.1977 | 2273.3784 | 2258.7944 | 2343.3527 | 2365.7067 | 2380.7834 | 2543.5444 | 2526.242
VP43_1_H400_V100_C45_MF_285 | 2660.3012 | 2674.8095 | 2734.291 | 2713.5039 | 2756.6819 | 2772.8196
VP45_2_H200_V150_C45_MF_425 | 2211.1666 | 2131.5983 | 2135.074 | 2141.749 | 2208.7243 | 2215.9191 | 2195.4285 | 2209.5729 | 2208.4354 | 2167.633 | 2166.4547 | 2117.3798 | 2194.5496 | 2264.3116 | 2267.3972 | 2317.1508 | 2414.638 | 2425.7515
VP46_1_H300_V150_C45_MF_285 | 3086.5735 | 3075.8261 | 3108.6092 | 3077.5016 | 3148.4235 | 3128.8205 | 3066.2035 | 3055.4101 | 3081.729 | 3082.416 | 3094.5335 | 3131.2069 | 3135.8375 | 3145.0925 | 3184.8716 | 3226.8478 | 3394.0747 | 3375.8082
VP49_1_H400_V150_C45_MF_285 | 3703.6478 | 3636.3396 | 3744.3018 | 3768.0535 | 3889.5999 | 4034.6229 | 3975.9522 | 4006.6247 | 3828.9325 | 3860.761 | 3944.7605 | 3892.4492 | 3953.3381 | 3900.7334 | 3935.8881 | 3961.3381 | 4063.606 | 4015.3245
VP50_1_H500_V150_C45_MF_285 | 4552.4075 | 4621.685 | 4751.0572 | 4866.2372 | 5104.8332 | 5095.3821 | 5000.6533 | 4892.1433 | 4847.5272 | 4814.495 | 4792.0381 | 4843.6789 | 4845.0776 | 4887.454 | 5004.1952 | 5045.1906 | 5110.3196 | 4981.0634
Notes: Heat carried away by chip rises with hsp*vc
Heat carried away by chip increases with cutting length for small chip thickness
Why?????
vc* hsp ~ chip ; lc ↑ → chip = const. (gilt nicht für Vp41 , VP42)
chip ↑ → Bchip ↑ (für Vp41 , VP42)
vc* hsp ~ ( 𝒒) ̇^´chip ; lc ↑ → ( 𝒒) ̇^´chip = const. (gilt nicht für Vp41 , VP42)
( 𝒒) ̇^´chip ↑ → Bchip ↑ (für Vp41 , VP42)

## Slide 21: Time and spatial varying thermal properties Heat partition to the chip for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 0.60694 | 0.62951 | 0.60676 | 0.60854 | 0.63899 | 0.63612 | 0.57706 | 0.62093 | 0.66525 | 0.59274 | 0.64887 | 0.66995 | 0.68124 | 0.68587 | 0.66664 | 0.72446 | 0.76721 | 0.71637
VP42_1_H300_V100_C45_MF_425 | 0.64915 | 0.63576 | 0.65008 | 0.64768 | 0.66579 | 0.64883 | 0.64075 | 0.65156 | 0.651 | 0.65515 | 0.6604 | 0.66746 | 0.6593 | 0.68398 | 0.69456 | 0.69385 | 0.74128 | 0.74377
VP43_1_H400_V100_C45_MF_285 | 0.64724 | 0.65635 | 0.66524 | 0.66103 | 0.67155 | 0.6804
VP45_2_H200_V150_C45_MF_425 | 0.67329 | 0.65163 | 0.6527 | 0.65474 | 0.67163 | 0.67741 | 0.6685 | 0.66906 | 0.66967 | 0.65823 | 0.65878 | 0.64473 | 0.66823 | 0.68563 | 0.68656 | 0.7006 | 0.7372 | 0.74156
VP46_1_H300_V150_C45_MF_285 | 0.68413 | 0.68175 | 0.68902 | 0.67814 | 0.69377 | 0.68774 | 0.67482 | 0.67723 | 0.67652 | 0.68321 | 0.68433 | 0.69244 | 0.69505 | 0.69551 | 0.70006 | 0.71522 | 0.7479 | 0.74824
VP49_1_H400_V150_C45_MF_285 | 0.61522 | 0.59901 | 0.61758 | 0.62149 | 0.64463 | 0.66867 | 0.65894 | 0.66084 | 0.63231 | 0.63757 | 0.64982 | 0.6428 | 0.65742 | 0.64795 | 0.65305 | 0.65652 | 0.67024 | 0.66469
VP50_1_H500_V150_C45_MF_285 | 0.6265 | 0.63812 | 0.65803 | 0.67398 | 0.70702 | 0.70043 | 0.68971 | 0.67757 | 0.67139 | 0.66681 | 0.65798 | 0.66806 | 0.66678 | 0.67553 | 0.69019 | 0.69354 | 0.70406 | 0.68549
Notes: No influence of level of heat partition inside the chip by chip thickness
Rising heat partition inside the chip, especially for lower chip thickness  Hypo: tool is heating up and is conducts less heat away
Hypo: The lower the chip thickness the lower the influence of friction at the rake face
1 = Bchip + Btool + BWP
Btool = konst. ; Bchip ↑ → BWP ↓

## Slide 22: Time and spatial varying thermal properties Heat flow into the tool [W] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 174.9898 | 185.427 | 183.5584 | 174.6628 | 187.6676 | 181.1487 | 177.8051 | 175.1224 | 183.3825 | 174.4536 | 174.6958 | 174.0088 | 168.8091 | 171.3085 | 165.1698 | 170.171 | 168.0591 | 177.2033
VP42_1_H300_V100_C45_MF_425 | 207.3749 | 203.3318 | 200.1116 | 198.8233 | 198.4968 | 192.4023 | 196.2649 | 191.7946 | 189.6378 | 176.4483 | 181.5601 | 186.4606 | 205.3708 | 206.0945 | 186.1899 | 186.057 | 185.03 | 182.177
VP43_1_H400_V100_C45_MF_285 | 209.6865 | 250.5447 | 273.5606 | 232.7488 | 251.4691
VP45_2_H200_V150_C45_MF_425 | 169.0834 | 164.669 | 167.1594 | 175.3947 | 172.3657 | 184.8235 | 179.7375 | 192.8026 | 192.0576 | 189.8144 | 184.7656 | 184.9765 | 178.4484 | 179.238 | 176.3686 | 183.2584 | 187.2633 | 179.9538
VP46_1_H300_V150_C45_MF_285 | 215.5119 | 232.6677 | 222.8332 | 212.4771 | 221.4205 | 223.6145 | 228.6645 | 233.1993 | 238.6011 | 237.3116 | 246.7924 | 233.8908 | 237.5663 | 224.9591 | 222.3205 | 227.8837 | 228.6524 | 231.1235
VP49_1_H400_V150_C45_MF_285 | 301.8132 | 301.8448 | 296.7119 | 292.0198 | 310.3083 | 306.8231 | 316.8316 | 317.7345 | 320.1902 | 314.0135 | 310.2212 | 300.2932 | 290.0056 | 281.4552 | 277.6309 | 278.1966 | 283.8684 | 268.5243
VP50_1_H500_V150_C45_MF_285 | 336.9117 | 333.219 | 352.8455 | 338.4114 | 331.2958 | 325.1081 | 326.1268 | 322.8553 | 326.4338 | 328.9614 | 324.2766 | 311.2354 | 311.352 | 305.6342 | 302.461 | 308.2702 | 309.1887 | 287.4556

## Slide 23: Time and spatial varying thermal properties Heat flow into the tool [W] for different vc and hsp 2
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_1_H200_V100_C45_MF_425 | 176.7823 | 194.6592 | 179.3091 | 200.2326 | 191.7564 | 197.1866 | 200.8998 | 190.3598 | 192.3539 | 195.6777 | 195.6315 | 191.5615 | 190.312 | 188.9694 | 183.0086 | 184.0585 | 179.9344 | 187.7229
VP41_2_H200_V100_C45_MF_425 | 174.9898 | 185.427 | 183.5584 | 174.6628 | 187.6676 | 181.1487 | 177.8051 | 175.1224 | 183.3825 | 174.4536 | 174.6958 | 174.0088 | 168.8091 | 171.3085 | 165.1698 | 170.171 | 168.0591 | 177.2033
VP42_1_H300_V100_C45_MF_425 | 207.3749 | 203.3318 | 200.1116 | 198.8233 | 198.4968 | 192.4023 | 196.2649 | 191.7946 | 189.6378 | 176.4483 | 181.5601 | 186.4606 | 205.3708 | 206.0945 | 186.1899 | 186.057 | 185.03 | 182.177
VP43_1_H400_V100_C45_MF_285 | 209.6865 | 250.5447 | 273.5606 | 232.7488 | 251.4691
VP45_2_H200_V150_C45_MF_425 | 169.0834 | 164.669 | 167.1594 | 175.3947 | 172.3657 | 184.8235 | 179.7375 | 192.8026 | 192.0576 | 189.8144 | 184.7656 | 184.9765 | 178.4484 | 179.238 | 176.3686 | 183.2584 | 187.2633 | 179.9538
VP46_1_H300_V150_C45_MF_285 | 215.5119 | 232.6677 | 222.8332 | 212.4771 | 221.4205 | 223.6145 | 228.6645 | 233.1993 | 238.6011 | 237.3116 | 246.7924 | 233.8908 | 237.5663 | 224.9591 | 222.3205 | 227.8837 | 228.6524 | 231.1235
VP46_2_H300_V150_C45_MF_285 | 224.568 | 216.6443 | 225.0766 | 217.0972 | 230.4497 | 221.3453 | 231.5537 | 233.1625 | 243.0643 | 240.6486 | 235.5006 | 237.4287 | 229.0994 | 223.68 | 223.5469 | 226.4214 | 226.8217 | 226.0299
VP49_1_H400_V150_C45_MF_285 | 301.8132 | 301.8448 | 296.7119 | 292.0198 | 310.3083 | 306.8231 | 316.8316 | 317.7345 | 320.1902 | 314.0135 | 310.2212 | 300.2932 | 290.0056 | 281.4552 | 277.6309 | 278.1966 | 283.8684 | 268.5243
VP49_2_H400_V150_C45_MF_285 | 291.7248 | 303.0838 | 299.2662 | 296.0187 | 291.4125 | 300.7905 | 308.7929 | 308.1423 | 313.5861 | 308.0027 | 300.3639 | 290.4385 | 281.0854 | 274.5046 | 272.083 | 275.3597 | 282.9138 | 266.1894
VP50_1_H500_V150_C45_MF_285 | 336.9117 | 333.219 | 352.8455 | 338.4114 | 331.2958 | 325.1081 | 326.1268 | 322.8553 | 326.4338 | 328.9614 | 324.2766 | 311.2354 | 311.352 | 305.6342 | 302.461 | 308.2702 | 309.1887 | 287.4556
VP50_2_H500_V150_C45_MF_285 | 344.7064 | 337.7815 | 351.316 | 338.5551 | 332.1894 | 326.1144 | 327.1685 | 324.4865 | 327.6872 | 330.3101 | 327.1721 | 313.6844 | 304.7504 | 308.1786 | 305.2796 | 312.2711 | 312.3095 | 289.7248
Notes: For small chip thickness no influence of cutting speed
Heat flux into the tool rises with chip thickness decreasingly,
Less rise for smaller cutting speeds
Decreases for higher chip thickness over time constant for small chip thickness hypo: tool gets to hot to carry heat away
Hypo: The higher the chip thickness the higher the frictional influence
Thermal number? Vc *hsp??

## Slide 24: Time and spatial varying thermal properties Heat partition into the tool for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 0.073404 | 0.077782 | 0.076738 | 0.073267 | 0.078722 | 0.075466 | 0.073669 | 0.072825 | 0.076532 | 0.072415 | 0.072907 | 0.072746 | 0.070811 | 0.07186 | 0.069285 | 0.071501 | 0.070613 | 0.074456
VP42_1_H300_V100_C45_MF_425 | 0.060437 | 0.059698 | 0.058916 | 0.058537 | 0.058441 | 0.056646 | 0.057286 | 0.05623 | 0.055181 | 0.051502 | 0.05338 | 0.054744 | 0.059944 | 0.060155 | 0.054665 | 0.054224 | 0.053925 | 0.053636
VP43_1_H400_V100_C45_MF_285 | 0.051209 | 0.061336 | 0.066809 | 0.057046 | 0.061182
VP45_2_H200_V150_C45_MF_425 | 0.051485 | 0.05034 | 0.051101 | 0.053618 | 0.052413 | 0.056501 | 0.054729 | 0.05838 | 0.058238 | 0.057639 | 0.056184 | 0.056325 | 0.054337 | 0.054273 | 0.053404 | 0.055409 | 0.057172 | 0.055012
VP46_1_H300_V150_C45_MF_285 | 0.047768 | 0.051453 | 0.049335 | 0.04682 | 0.048731 | 0.049393 | 0.050198 | 0.051688 | 0.052379 | 0.0526 | 0.054315 | 0.051723 | 0.052656 | 0.049862 | 0.049049 | 0.050027 | 0.050446 | 0.050867
VP49_1_H400_V150_C45_MF_285 | 0.04978 | 0.049907 | 0.048939 | 0.048224 | 0.051546 | 0.051024 | 0.052257 | 0.052471 | 0.052877 | 0.052042 | 0.051354 | 0.049768 | 0.048007 | 0.0467 | 0.046065 | 0.045885 | 0.046991 | 0.044451
VP50_1_H500_V150_C45_MF_285 | 0.046468 | 0.046151 | 0.048869 | 0.04687 | 0.045593 | 0.044791 | 0.04498 | 0.044716 | 0.045071 | 0.045562 | 0.044913 | 0.042735 | 0.042848 | 0.042014 | 0.041578 | 0.042608 | 0.042453 | 0.03956
Notes: Heat partition inside tool higher for low cutting speed  Puls
No influence of chip thickness  Puls
Remains constant over time

## Slide 25: Time and spatial varying thermal properties Heat flow into the workpiece [W] for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 762.0363 | 697.7889 | 757.0873 | 758.5495 | 672.961 | 692.3036 | 842.9831 | 736.4364 | 618.7222 | 806.6841 | 666.6742 | 615.4864 | 591.0835 | 577.5524 | 629.5295 | 485.6158 | 385.9833 | 497.8255
VP42_1_H300_V100_C45_MF_425 | 996.4911 | 1037.2955 | 988.4179 | 997.8421 | 936.6692 | 1000.3582 | 1034.5263 | 996.7026 | 1009.7598 | 1005.0114 | 973.4961 | 946.1956 | 961.8666 | 876.5846 | 854.138 | 864.4374 | 702.7035 | 688.1314
VP43_1_H400_V100_C45_MF_285 | 1204.5997 | 1142.578 | 1064.3315 | 1112.9472 | 1079.6535
VP45_2_H200_V150_C45_MF_425 | 903.8703 | 974.8959 | 968.9297 | 954.0195 | 907.5008 | 870.4206 | 908.9542 | 900.1506 | 897.2953 | 935.6976 | 937.3705 | 981.764 | 911.1223 | 858.9766 | 858.7603 | 806.9552 | 673.5097 | 665.4578
VP46_1_H300_V150_C45_MF_285 | 1273.4139 | 1273.8125 | 1215.2539 | 1305.2106 | 1262.0426 | 1234.8873 | 1346.8062 | 1277.6225 | 1320.6844 | 1249.3848 | 1289.3172 | 1241.2232 | 1192.4843 | 1193.4313 | 1204.8848 | 1156.367 | 972.9392 | 1070.5882
VP49_1_H400_V150_C45_MF_285 | 2057.4481 | 2109.9065 | 1991.8796 | 1965.2194 | 1789.51 | 1639.8245 | 1770.1253 | 1731.0661 | 1879.4499 | 1831.153 | 1758.0323 | 1814.1679 | 1769.7836 | 1818.597 | 1786.1665 | 1796.3355 | 1664.3711 | 1731.242
VP50_1_H500_V150_C45_MF_285 | 2361.0923 | 2235.464 | 2087.8005 | 1984.6684 | 1798.4486 | 1806.7479 | 1923.6313 | 1976.532 | 2039.8328 | 2049.1616 | 2078.4852 | 2103.4773 | 2084.213 | 2057.2102 | 1943.1505 | 1853.9537 | 1834.7515 | 1822.4747
Notes: Heat flux inside work piece decreases with cutting speed and chip thickness
Heat flux into workpiece decreases over cutting length for small chip thickness
How over time?
How is this possible?

## Slide 26: Time and spatial varying thermal properties Heat partition into the workpiece for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 0.31966 | 0.29271 | 0.31651 | 0.31819 | 0.28229 | 0.28841 | 0.34927 | 0.30625 | 0.25821 | 0.33485 | 0.27823 | 0.25731 | 0.24795 | 0.24227 | 0.26407 | 0.20404 | 0.16218 | 0.20917
VP42_1_H300_V100_C45_MF_425 | 0.29041 | 0.30455 | 0.29101 | 0.29378 | 0.27577 | 0.29452 | 0.30196 | 0.29221 | 0.29382 | 0.29335 | 0.28622 | 0.2778 | 0.28075 | 0.25586 | 0.25077 | 0.25193 | 0.20479 | 0.2026
VP43_1_H400_V100_C45_MF_285 | 0.29419 | 0.27971 | 0.25993 | 0.27278 | 0.26268
VP45_2_H200_V150_C45_MF_425 | 0.27522 | 0.29803 | 0.2962 | 0.29165 | 0.27595 | 0.26609 | 0.27677 | 0.27256 | 0.27209 | 0.28413 | 0.28504 | 0.29894 | 0.27743 | 0.2601 | 0.26003 | 0.24399 | 0.20563 | 0.20343
VP46_1_H300_V150_C45_MF_285 | 0.28225 | 0.28169 | 0.26905 | 0.28761 | 0.27776 | 0.27277 | 0.29566 | 0.28318 | 0.28993 | 0.27692 | 0.28376 | 0.27449 | 0.26431 | 0.26452 | 0.26582 | 0.25385 | 0.21465 | 0.23562
VP49_1_H400_V150_C45_MF_285 | 0.33935 | 0.34885 | 0.32854 | 0.32454 | 0.29726 | 0.2727 | 0.29196 | 0.28587 | 0.31037 | 0.30348 | 0.29102 | 0.30067 | 0.29297 | 0.30175 | 0.29637 | 0.29628 | 0.27552 | 0.28659
VP50_1_H500_V150_C45_MF_285 | 0.32565 | 0.30961 | 0.28916 | 0.27488 | 0.2475 | 0.24892 | 0.26531 | 0.27375 | 0.28164 | 0.28381 | 0.28787 | 0.28882 | 0.28683 | 0.28279 | 0.26711 | 0.25625 | 0.25192 | 0.25081
Notes: Heat partition into workpiece independent from vc and hsp does not fit to K&H
Decreases for small chip thickness

## Slide 27: Time and spatial varying thermal properties Friction coefficient µ for different vc and hsp
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 113,62 | 116,16 | 118,70 | 123,78 | 128,86 | 131,40 | 133,94 | 139,02 | 144,11 | 146,65 | 149,19 | 154,27 | 159,35 | 161,89 | 164,43 | 169,51 | 174,59 | 177,13 | 179,67 | 184,76 | 189,84 | 192,38 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136 | 0.80136
VP42_1_H300_V100_C45_MF_425 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572 | 0.65572
VP43_1_H400_V100_C45_MF_285 | 0.54011 | 0.54011 | 0.54011 | 0.54011 | 0.54011 | 0.54011
VP45_2_H200_V150_C45_MF_425 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074 | 0.61074
VP46_1_H300_V150_C45_MF_285 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265 | 0.5265
VP49_1_H400_V150_C45_MF_285 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174 | 0.5174
VP50_1_H500_V150_C45_MF_285 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012 | 0.47012

## Slide 28: Time and spatial varying thermal properties Heat partition ratios for hsp = 200 µm, vc = 100 m/min
Chart: Workpiece position [mm]
| 113,62 | 118,70 | 123,78 | 128,86 | 133,94 | 139,02 | 144,11 | 149,19 | 154,27 | 159,35 | 164,43 | 169,51 | 174,59 | 179,67 | 184,76 | 189,84 | 194,92 | 200,00
VP41_2_H200_V100_C45_MF_425 - Summe von Percent - Heat through workpiece/Total heat | 0.31966 | 0.29271 | 0.31651 | 0.31819 | 0.28229 | 0.28841 | 0.34927 | 0.30625 | 0.25821 | 0.33485 | 0.27823 | 0.25731 | 0.24795 | 0.24227 | 0.26407 | 0.20404 | 0.16218 | 0.20917
VP41_2_H200_V100_C45_MF_425 - Summe von Percent - Heat through chip/Total heat | 0.60694 | 0.62951 | 0.60676 | 0.60854 | 0.63899 | 0.63612 | 0.57706 | 0.62093 | 0.66525 | 0.59274 | 0.64887 | 0.66995 | 0.68124 | 0.68587 | 0.66664 | 0.72446 | 0.76721 | 0.71637
VP41_2_H200_V100_C45_MF_425 - Summe von Percent - Heat inside tool/Total heat | 0.073404 | 0.077782 | 0.076738 | 0.073267 | 0.078722 | 0.075466 | 0.073669 | 0.072825 | 0.076532 | 0.072415 | 0.072907 | 0.072746 | 0.070811 | 0.07186 | 0.069285 | 0.071501 | 0.070613 | 0.074456
Tool
Workpiece
Chip

## Slide 29: Temperature distribution for orthogonal cutting Temperature distribution for hsp = 200 µm, vc = 100 m/min
Workpiece position : 124 mm
Workpiece position : 200 mm
[°C]

## Slide 30: Time and spatial varying thermal properties Heat partition ratios for hsp = 200 µm, vc = 150 m/min
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 116,16 | 123,78 | 131,40 | 139,02 | 146,65 | 154,27 | 161,89 | 169,51 | 177,13 | 184,76 | 192,38 | 200,00
VP45_2_H200_V150_C45_MF_425 - Summe von Percent - Heat through workpiece/Total heat | 0.27522 | 0.29803 | 0.2962 | 0.29165 | 0.27595 | 0.26609 | 0.27677 | 0.27256 | 0.27209 | 0.28413 | 0.28504 | 0.29894 | 0.27743 | 0.2601 | 0.26003 | 0.24399 | 0.20563 | 0.20343
VP45_2_H200_V150_C45_MF_425 - Summe von Percent - Heat through chip/Total heat | 0.67329 | 0.65163 | 0.6527 | 0.65474 | 0.67163 | 0.67741 | 0.6685 | 0.66906 | 0.66967 | 0.65823 | 0.65878 | 0.64473 | 0.66823 | 0.68563 | 0.68656 | 0.7006 | 0.7372 | 0.74156
VP45_2_H200_V150_C45_MF_425 - Summe von Percent - Heat inside tool/Total heat | 0.051485 | 0.05034 | 0.051101 | 0.053618 | 0.052413 | 0.056501 | 0.054729 | 0.05838 | 0.058238 | 0.057639 | 0.056184 | 0.056325 | 0.054337 | 0.054273 | 0.053404 | 0.055409 | 0.057172 | 0.055012
Tool
Workpiece
Chip

## Slide 31
Time and spatial varying thermal properties Temperature distribution for hsp = 200 µm, vc = 150 m/min
Workpiece position : 124 mm
Workpiece position : 200 mm
[°C]
Notes: With higher cutting speed and lower chip thickness more heat is transferred over tip

## Slide 32: Time and spatial varying thermal properties Heat partition ratios for hsp = 300 µm, vc = 100 m/min
Chart: Workpiece position [mm]
| 113,62 | 118,70 | 123,78 | 128,86 | 133,94 | 139,02 | 144,11 | 149,19 | 154,27 | 159,35 | 164,43 | 169,51 | 174,59 | 179,67 | 184,76 | 189,84 | 194,92 | 200,00
VP42_1_H300_V100_C45_MF_425 - Summe von Percent - Heat through workpiece/Total heat | 0.29041 | 0.30455 | 0.29101 | 0.29378 | 0.27577 | 0.29452 | 0.30196 | 0.29221 | 0.29382 | 0.29335 | 0.28622 | 0.2778 | 0.28075 | 0.25586 | 0.25077 | 0.25193 | 0.20479 | 0.2026
VP42_1_H300_V100_C45_MF_425 - Summe von Percent - Heat through chip/Total heat | 0.64915 | 0.63576 | 0.65008 | 0.64768 | 0.66579 | 0.64883 | 0.64075 | 0.65156 | 0.651 | 0.65515 | 0.6604 | 0.66746 | 0.6593 | 0.68398 | 0.69456 | 0.69385 | 0.74128 | 0.74377
VP42_1_H300_V100_C45_MF_425 - Summe von Percent - Heat inside tool/Total heat | 0.060437 | 0.059698 | 0.058916 | 0.058537 | 0.058441 | 0.056646 | 0.057286 | 0.05623 | 0.055181 | 0.051502 | 0.05338 | 0.054744 | 0.059944 | 0.060155 | 0.054665 | 0.054224 | 0.053925 | 0.053636
Tool
Workpiece
Chip

## Slide 33
Time and spatial varying thermal properties Temperature distribution for hsp = 300 µm, vc = 100 m/min
Workpiece position : 124 mm
Workpiece position : 200 mm
[°C]

## Slide 34: Time and spatial varying thermal properties Heat partition ratios for hsp = 300 µm, vc = 150 m/min
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 116,16 | 123,78 | 131,40 | 139,02 | 146,65 | 154,27 | 161,89 | 169,51 | 177,13 | 184,76 | 192,38 | 200,00
VP46_1_H300_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.28225 | 0.28169 | 0.26905 | 0.28761 | 0.27776 | 0.27277 | 0.29566 | 0.28318 | 0.28993 | 0.27692 | 0.28376 | 0.27449 | 0.26431 | 0.26452 | 0.26582 | 0.25385 | 0.21465 | 0.23562
VP46_1_H300_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.66998 | 0.66685 | 0.68161 | 0.66557 | 0.67351 | 0.67784 | 0.65414 | 0.66513 | 0.6577 | 0.67048 | 0.66193 | 0.67379 | 0.68303 | 0.68562 | 0.68513 | 0.69612 | 0.7349 | 0.71351
VP46_1_H300_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.047768 | 0.051453 | 0.049335 | 0.04682 | 0.048731 | 0.049393 | 0.050198 | 0.051688 | 0.052379 | 0.0526 | 0.054315 | 0.051723 | 0.052656 | 0.049862 | 0.049049 | 0.050027 | 0.050446 | 0.050867
VP46_2_H300_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.27063 | 0.29514 | 0.28115 | 0.27585 | 0.2741 | 0.27377 | 0.2683 | 0.27855 | 0.28198 | 0.25997 | 0.28286 | 0.27538 | 0.27817 | 0.27203 | 0.26472 | 0.25295 | 0.22522 | 0.21442
VP46_2_H300_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.67965 | 0.65739 | 0.66908 | 0.67632 | 0.67501 | 0.67747 | 0.68089 | 0.67016 | 0.66447 | 0.68696 | 0.66539 | 0.67218 | 0.67163 | 0.67882 | 0.68604 | 0.69692 | 0.72488 | 0.73585
VP46_2_H300_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.049716 | 0.04747 | 0.049768 | 0.047824 | 0.050893 | 0.048759 | 0.050807 | 0.051296 | 0.053544 | 0.053079 | 0.051742 | 0.052435 | 0.050199 | 0.049145 | 0.049244 | 0.050126 | 0.049901 | 0.049727
Tool
Workpiece
Chip

## Slide 35
Time and spatial varying thermal properties Temperature distribution for hsp = 300 µm, vc = 150 m/min
Workpiece position : 124 mm
Workpiece position : 200 mm
[°C]

## Slide 36: Time and spatial varying thermal properties Heat partition ratios for hsp = 400 µm, vc = 100 m/min
Chart: Workpiece position [mm]
| 113,62 | 118,70 | 123,78 | 128,86 | 133,94 | 139,02
VP43_1_H400_V100_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.29419 | 0.27971 | 0.25993 | 0.27278 | 0.26268 | 0.28555
VP43_1_H400_V100_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.6546 | 0.65895 | 0.67326 | 0.67017 | 0.67614 | 0.68593
VP43_1_H400_V100_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.051209 | 0.061336 | 0.066809 | 0.057046 | 0.061182 | 0.028524
Tool
Workpiece
Chip

## Slide 37: Time and spatial varying thermal properties Heat partition ratios for hsp = 400 µm, vc = 150 m/min
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 116,16 | 123,78 | 131,40 | 139,02 | 146,65 | 154,27 | 161,89 | 169,51 | 177,13 | 184,76 | 192,38 | 200,00
VP49_1_H400_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.33935 | 0.34885 | 0.32854 | 0.32454 | 0.29726 | 0.2727 | 0.29196 | 0.28587 | 0.31037 | 0.30348 | 0.29102 | 0.30067 | 0.29297 | 0.30175 | 0.29637 | 0.29628 | 0.27552 | 0.28659
VP49_1_H400_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.61087 | 0.60124 | 0.62253 | 0.62724 | 0.6512 | 0.67628 | 0.65578 | 0.66166 | 0.63675 | 0.64448 | 0.65762 | 0.64957 | 0.65903 | 0.65155 | 0.65757 | 0.65783 | 0.67749 | 0.66896
VP49_1_H400_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.04978 | 0.049907 | 0.048939 | 0.048224 | 0.051546 | 0.051024 | 0.052257 | 0.052471 | 0.052877 | 0.052042 | 0.051354 | 0.049768 | 0.048007 | 0.0467 | 0.046065 | 0.045885 | 0.046991 | 0.044451
VP49_2_H400_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.3318 | 0.30308 | 0.31372 | 0.2708 | 0.26256 | 0.26576 | 0.25114 | 0.2777 | 0.26098 | 0.26073 | 0.28081 | 0.27184 | 0.25728 | 0.24576 | 0.26175 | 0.2344 | 0.25278 | 0.28201
VP49_2_H400_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.61848 | 0.6449 | 0.63528 | 0.67858 | 0.68778 | 0.68292 | 0.69587 | 0.66985 | 0.68514 | 0.68665 | 0.668 | 0.67832 | 0.69443 | 0.70752 | 0.69182 | 0.71862 | 0.69867 | 0.67241
VP49_2_H400_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.049714 | 0.052013 | 0.050999 | 0.050627 | 0.049661 | 0.051321 | 0.052993 | 0.052446 | 0.053875 | 0.052615 | 0.051186 | 0.049843 | 0.048291 | 0.046721 | 0.046423 | 0.046982 | 0.048552 | 0.045579
Tool
Workpiece
Chip

## Slide 38
Time and spatial varying thermal properties Temperature distribution for hsp = 400 µm, vc = 150 m/min [1/2]
Workpiece position : 124 mm
Workpiece position : 200 mm
[°C]

## Slide 39
Time and spatial varying thermal properties Temperature distribution for hsp = 400 µm, vc = 150 m/min [2/2]
Workpiece position : 124 mm
Workpiece position : 200 mm
[°C]

## Slide 40: Time and spatial varying thermal properties Heat partition ratios for hsp = 500 µm, vc = 150 m/min
Chart: Workpiece position [mm]
| 70,43 | 78,05 | 85,67 | 93,29 | 100,91 | 108,54 | 116,16 | 123,78 | 131,40 | 139,02 | 146,65 | 154,27 | 161,89 | 169,51 | 177,13 | 184,76 | 192,38 | 200,00
VP50_1_H500_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.13622 | 0.12947 | 0.12241 | 0.11812 | 0.11404 | 0.11035 | 0.10746 | 0.1048 | 0.10472 | 0.10517 | 0.1002 | 0.097635 | 0.094481 | 0.091374 | 0.087008 | 0.084166 | 0.083078 | 0.054109
VP50_1_H500_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.6265 | 0.63812 | 0.65803 | 0.67398 | 0.70702 | 0.70043 | 0.68971 | 0.67757 | 0.67139 | 0.66681 | 0.65798 | 0.66806 | 0.66678 | 0.67553 | 0.69019 | 0.69354 | 0.70406 | 0.68549
VP50_1_H500_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.21495 | 0.21001 | 0.19709 | 0.18543 | 0.15647 | 0.16691 | 0.18046 | 0.19516 | 0.20142 | 0.20555 | 0.21955 | 0.21193 | 0.21641 | 0.21068 | 0.20042 | 0.2 | 0.19051 | 0.23807
VP50_2_H500_V150_C45_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.13555 | 0.13286 | 0.12401 | 0.12047 | 0.11436 | 0.11106 | 0.11061 | 0.10729 | 0.10389 | 0.10806 | 0.10416 | 0.099669 | 0.095733 | 0.091482 | 0.088766 | 0.087869 | 0.085412 | 0.053271
VP50_2_H500_V150_C45_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.6415 | 0.65939 | 0.65955 | 0.69394 | 0.73029 | 0.71535 | 0.71119 | 0.69405 | 0.69127 | 0.67765 | 0.68556 | 0.67657 | 0.68968 | 0.68217 | 0.69574 | 0.69898 | 0.70165 | 0.67331
VP50_2_H500_V150_C45_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.1998 | 0.18465 | 0.19342 | 0.16244 | 0.13225 | 0.15042 | 0.15502 | 0.17546 | 0.18179 | 0.19127 | 0.18713 | 0.20071 | 0.19138 | 0.20333 | 0.19242 | 0.19008 | 0.18992 | 0.2504
Tool
Workpiece
Chip

## Slide 41
Time and spatial varying thermal properties Temperature distribution for hsp = 500 µm, vc = 150 m/min
Workpiece position : 124 mm
Workpiece position : 200 mm
[°C]

## Slide 42: Time and spatial varying thermal properties Conclusion
XYZ

## Slide 43: Time and spatial varying thermal properties Means to enhance quality of measurement
Determine emissivity of chip/tool/workpiece
  Collect chips
  Heating + Pyrometer + Camera
  e (DL)
  Regression of Tcam (DL, ecam) for IT
Enhance quantity of valid pixels
  Expand field of measurement
  Measurement with multiple integration times
  Overlap pictures via algorithm
Determine workpiece directly
  Separate measurements for the work piece
  Compare Heat flows with Ptotal

## Slide 44: Gliederung
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Influence of uncut chip thickness and cutting velocity
3.2
Time and spatial varying thermal properties
3.1
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 45: Influence of uncut chip thickness and cutting velocity Workpiece position 124 mm
ap = 3,5 mm, = 6°, = 3°, < 5 µm, uncoated, workpiece position: 124 mm
Chart: Heat partition (chip)
| 100,00 | 150,00
200,00 | 0.60676 | 0.66906
300,00 | 0.65008 | 0.67723
400,00 | 0.66524 | 0.66084
500,00 | 0.67757
Chart: Heat partition (tool)
| 100,00 | 150,00
200,00 | 0.076738 | 0.05838
300,00 | 0.058916 | 0.051688
400,00 | 0.066809 | 0.052471
500,00 | 0.044716
Chart: Heat flow (chip) [W]
| 100,00 | 150,00
200,00 | 1451.366 | 2209.5729
300,00 | 2208.0209 | 3055.4101
400,00 | 2734.291 | 4006.6247
500,00 | 4892.1433
Chart: Heat flow (workpiece) [W]
| 100,00 | 150,00
200,00 | 757.0873 | 900.1506
300,00 | 988.4179 | 1277.6225
400,00 | 1064.3315 | 1731.0661
500,00 | 1976.532
Chart: Heat partition (workpiece)
| 100,00 | 150,00
200,00 | 0.31651 | 0.27256
300,00 | 0.29101 | 0.28318
400,00 | 0.25993 | 0.28587
500,00 | 0.27375
hsp [µm]
Cutting velocity [m/min]
Chart: Heat flow (tool) [W]
| 100,00 | 150,00
200,00 | 183.5584 | 192.8026
300,00 | 200.1116 | 233.1993
400,00 | 273.5606 | 317.7345
500,00 | 322.8553

## Slide 46: Influence of uncut chip thickness and cutting velocity Workpiece position 200 mm
ap = 3,5 mm, = 6°, = 3°, < 5 µm, uncoated, workpiece position: 200 mm
Chart: Heat flow (chip) [W]
| 100,00 | 150,00
200,00 | 1704.9593 | 2425.7515
300,00 | 2526.242 | 3375.8082
400,00 | 4015.3245
500,00 | 4981.0634
Chart: Heat partition (chip)
| 100,00 | 150,00
200,00 | 0.71637 | 0.74156
300,00 | 0.74377 | 0.74824
400,00 | 0.66469
500,00 | 0.68549
Chart: Heat partition (tool)
| 100,00 | 150,00
200,00 | 0.074456 | 0.055012
300,00 | 0.053636 | 0.050867
400,00 | 0.044451
500,00 | 0.03956
Chart: Heat flow (workpiece) [W]
| 100,00 | 150,00
200,00 | 497.8255 | 665.4578
300,00 | 688.1314 | 1070.5882
400,00 | 1731.242
500,00 | 1822.4747
Chart: Heat partition (workpiece)
| 100,00 | 150,00
200,00 | 0.20917 | 0.20343
300,00 | 0.2026 | 0.23562
400,00 | 0.28659
500,00 | 0.25081
Chart: Heat flow (tool) [W]
| 100,00 | 150,00
200,00 | 177.2033 | 179.9538
300,00 | 182.177 | 231.1235
400,00 | 268.5243
500,00 | 287.4556
hsp [µm]
Cutting velocity [m/min]

## Slide 47: Gliederung
Influence of uncut chip thickness and cutting velocity
4.2
Time and spatial varying thermal properties
4.1
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 48: Gliederung
Influence of uncut chip thickness and cutting velocity
4.2
Time and spatial varying thermal properties
4.1
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 49: Time and spatial varying thermal properties Temperature at tool tip [°C] for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 305.7037 | 359.0087 | 373.894 | 312.2685 | 360.8156 | 366.7087 | 372.1807 | 380.9632
VP33_1_H300_V150_ACF_MF_285 | 335.7945 | 135.8712 | 362.3886 | 327.2749 | 342.5201 | 288.9588 | 288.0323 | 371.5422
VP36_1_H200_V100_ABA_MF_285 | 316.5908 | 315.1712 | 292.0169 | 280.8572 | 296.6303 | 309.9306 | 325.7267 | 344.5932 | 350.3726 | 358.5259 | 358.7022
VP37_1_H200_V150_ABA_MF_425 | 295.4657 | 318.1522 | 324.3459 | 341.6017 | 341.4323 | 309.9544 | 304.425 | 330.101
VP38_1_H300_V100_ABA_MF_425 | 341.7368 | 363.4779 | 348.2248 | 327.5525 | 326.8533 | 353.8151 | 364.2259 | 384.6232 | 398.1447 | 397.0859 | 406.7007
VP39_1_H300_V150_ABA_MF_425 | 352.8635 | 312.1887 | 375.9718 | 370.9857 | 404.1945 | 383.358 | 380.4667 | 382.8193
VP4_1_H300_V100_ACF_MF_285 | 294.5303 | 293.4045 | 314.7375 | 289.1686 | 324.354 | 328.7716 | 294.2745 | 336.7471 | 273.9328 | 159.8445 | 413.0847
VP5_1_H200_V100_ACF_MF_285 | 354.8135 | 260.6953 | 252.9006 | 241.9538 | 266.5126 | 318.9569 | 244.8525 | 305.5209 | 287.8376 | 391.1507 | 350.3544
VP6_1_H100_V100_ACF_MF_285 | 207.9595 | 232.7021 | 240.8276 | 356.2291 | 253.0614 | 397.676 | 433.4986

## Slide 50: Time and spatial varying thermal properties Internal energy in tool [Joule] for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 0.5496 | 0.80782 | 1.0833 | 1.2851 | 1.645 | 2.0291 | 2.4 | 2.5047
VP33_1_H300_V150_ACF_MF_285 | 1.1127 | 1.3071 | 1.6818 | 1.1978 | 1.675 | 2.253 | 2.7183 | 2.9855
VP36_1_H200_V100_ABA_MF_285 | 0.75171 | 0.95339 | 1.2146 | 1.3612 | 1.4699 | 1.555 | 1.6303 | 1.6805 | 1.7328 | 1.7881 | 1.8598
VP37_1_H200_V150_ABA_MF_425 | 0.57231 | 0.67533 | 0.8089 | 0.99411 | 1.1883 | 1.4484 | 1.6506 | 1.6177
VP38_1_H300_V100_ABA_MF_425 | 0.97041 | 1.2301 | 1.4664 | 1.8019 | 2.0327 | 2.2325 | 2.4148 | 2.5202 | 2.5836 | 2.7293 | 2.8055
VP39_1_H300_V150_ABA_MF_425 | 0.85018 | 0.92941 | 1.2235 | 1.4735 | 1.6777 | 2.1493 | 2.5398 | 2.703
VP4_1_H300_V100_ACF_MF_285 | 0.97925 | 1.258 | 1.586 | 2.0673 | 2.2472 | 2.6177 | 2.7775 | 2.9476 | 3.0778 | 3.4084 | 3.9398
VP5_1_H200_V100_ACF_MF_285 | 0.62438 | 0.61766 | 0.77684 | 1.0456 | 1.1331 | 1.5858 | 1.464 | 1.6027 | 1.7143 | 2.5029 | 2.5716
VP6_1_H100_V100_ACF_MF_285 | 0.57683 | 0.69313 | 0.77616 | 0.994 | 0.88849 | 1.1495 | 1.1785

## Slide 51: Time and spatial varying thermal properties Internal energy rate of the tool [W] for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 12.7277 | 12.7277 | 12.7277 | 12.7277 | 12.7277 | 12.7277 | 12.7277 | 12.7277
VP33_1_H300_V150_ACF_MF_285 | 11.4532 | 11.4532 | 11.4532 | 11.4532 | 11.4532 | 11.4532 | 11.4532 | 11.4532
VP36_1_H200_V100_ABA_MF_285 | 4.3945 | 4.3945 | 4.3945 | 4.3945 | 4.3945 | 4.3945 | 4.3945 | 4.3945 | 4.3945 | 4.3945 | 4.3945
VP37_1_H200_V150_ABA_MF_425 | 7.3294 | 7.3294 | 7.3294 | 7.3294 | 7.3294 | 7.3294 | 7.3294 | 7.3294
VP38_1_H300_V100_ABA_MF_425 | 7.9584 | 7.9584 | 7.9584 | 7.9584 | 7.9584 | 7.9584 | 7.9584 | 7.9584 | 7.9584 | 7.9584 | 7.9584
VP39_1_H300_V150_ABA_MF_425 | 12.297 | 12.297 | 12.297 | 12.297 | 12.297 | 12.297 | 12.297 | 12.297
VP4_1_H300_V100_ACF_MF_285 | 11.8029 | 11.8029 | 11.8029 | 11.8029 | 11.8029 | 11.8029 | 11.8029 | 11.8029 | 11.8029 | 11.8029 | 11.8029
VP5_1_H200_V100_ACF_MF_285 | 8.4246 | 8.4246 | 8.4246 | 8.4246 | 8.4246 | 8.4246 | 8.4246 | 8.4246 | 8.4246 | 8.4246 | 8.4246
VP6_1_H100_V100_ACF_MF_285 | 4.3497 | 4.3497 | 4.3497 | 4.3497 | 4.3497 | 4.3497 | 4.3497

## Slide 52: Time and spatial varying thermal properties Internal energy carried away by chip [W] for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 1440.7798 | 1409.6175 | 1575.8269 | 1597.1321 | 1524.1344 | 1545.9622 | 1536.5762 | 1737.7919
VP33_1_H300_V150_ACF_MF_285 | 2279.2673 | 2211.4647 | 2145.7486 | 2226.8733 | 2243.05 | 2163.0123 | 2214.0318 | 2501.462
VP36_1_H200_V100_ABA_MF_285 | 1000.0666 | 1041.6505 | 1032.0091 | 1055.0515 | 1047.0781 | 1066.5142 | 1083.8348 | 1046.1131 | 1047.9808 | 1055.4452 | 979.5612
VP37_1_H200_V150_ABA_MF_425 | 1513.4059 | 1492.3547 | 1566.5455 | 1580.8656 | 1538.5796 | 1605.1663 | 1659.9065 | 1664.4079
VP38_1_H300_V100_ABA_MF_425 | 1528.9569 | 1564.0366 | 1499.5168 | 1499.2694 | 1597.8732 | 1498.4805 | 1622.2786 | 1571.0286 | 1567.6816 | 1690.7209 | 1574.3611
VP39_1_H300_V150_ABA_MF_425 | 2317.0557 | 2233.4372 | 2208.7731 | 2303.8621 | 2295.3274 | 2294.6617 | 2216.7907 | 2434.1194
VP4_1_H300_V100_ACF_MF_285 | 1399.4917 | 1334.4974 | 1360.9848 | 1420.2373 | 1446.1944 | 1440.8875 | 1460.274 | 1468.3725 | 1477.692 | 1662.3925 | 1658.4424
VP5_1_H200_V100_ACF_MF_285 | 1068.9325 | 963.4712 | 959.7932 | 991.5921 | 986.4712 | 1017.9059 | 1014.6047 | 1066.8849 | 1058.5964 | 1094.6674 | 1151.3422
VP6_1_H100_V100_ACF_MF_285 | 501.0422 | 496.3653 | 525.5356 | 505.9998 | 519.2836 | 528.8747 | 522.0725

## Slide 53: Time and spatial varying thermal properties Heat partition to the chip for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 0.56276 | 0.55058 | 0.61628 | 0.62383 | 0.59531 | 0.60384 | 0.59703 | 0.67702
VP33_1_H300_V150_ACF_MF_285 | 0.67654 | 0.65923 | 0.63691 | 0.66383 | 0.66652 | 0.64203 | 0.6579 | 0.74249
VP36_1_H200_V100_ABA_MF_285 | 0.51458 | 0.53225 | 0.52788 | 0.54077 | 0.53502 | 0.54609 | 0.55439 | 0.53565 | 0.53821 | 0.54204 | 0.50258
VP37_1_H200_V150_ABA_MF_425 | 0.55082 | 0.54419 | 0.57125 | 0.57647 | 0.56052 | 0.58308 | 0.60111 | 0.6052
VP38_1_H300_V100_ABA_MF_425 | 0.5311 | 0.54203 | 0.52436 | 0.52653 | 0.56233 | 0.52513 | 0.57092 | 0.55288 | 0.54578 | 0.5925 | 0.55172
VP39_1_H300_V150_ABA_MF_425 | 0.52306 | 0.50865 | 0.49861 | 0.52469 | 0.52274 | 0.52479 | 0.50377 | 0.55316
VP4_1_H300_V100_ACF_MF_285 | 0.60646 | 0.58066 | 0.59059 | 0.61545 | 0.6267 | 0.62778 | 0.63623 | 0.63719 | 0.64381 | 0.72706 | 0.72533
VP5_1_H200_V100_ACF_MF_285 | 0.63678 | 0.57561 | 0.57421 | 0.59241 | 0.59017 | 0.60982 | 0.60867 | 0.63828 | 0.63154 | 0.6567 | 0.68279
VP6_1_H100_V100_ACF_MF_285 | 0.5272 | 0.52829 | 0.55933 | 0.536 | 0.55182 | 0.56375 | 0.55028

## Slide 54: Time and spatial varying thermal properties Heat flow into the tool [W] for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 65.5839 | 86.8098 | 109.1073 | 109.7055 | 112.6048 | 132.3857 | 139.5123 | 148.5252
VP33_1_H300_V150_ACF_MF_285 | 130.1048 | 142.8628 | 144.9249 | 165.0306 | 182.4697
VP36_1_H200_V100_ABA_MF_285 | 79.8033 | 104.5351 | 84.4706 | 106.2927 | 99.2007 | 103.6522 | 98.4563 | 96.3378 | 88.8485 | 87.6501 | 89.7364
VP37_1_H200_V150_ABA_MF_425 | 72.8462 | 89.2887 | 85.3062 | 105.8772 | 96.8446 | 108.3974 | 103.0662 | 114.6173
VP38_1_H300_V100_ABA_MF_425 | 111.7438 | 100.5062 | 116.7321 | 119.2276 | 115.185 | 123.2276 | 121.2042 | 110.5073 | 102.1146 | 94.39 | 84.4351
VP39_1_H300_V150_ABA_MF_425 | 107.7731 | 121.9937 | 117.5184 | 132.8298 | 118.3248 | 128.2041 | 124.2826 | 136.6738
VP4_1_H300_V100_ACF_MF_285 | 47.5744 | 64.8222 | 83.2182 | 123.9846 | 130.5876 | 131.4153 | 119.0624
VP5_1_H200_V100_ACF_MF_285 | 53.0803 | 76.2592 | 98.3489 | 87.0271
VP6_1_H100_V100_ACF_MF_285 | 59.0144 | 55.2371 | 60.7101 | 67.6686

## Slide 55: Time and spatial varying thermal properties Heat partition into the tool for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 0.025616 | 0.033907 | 0.04267 | 0.04285 | 0.043982 | 0.051709 | 0.054207 | 0.057863
VP33_1_H300_V150_ACF_MF_285 | 0.038618 | 0.042587 | 0.043017 | 0.049039 | 0.054161
VP36_1_H200_V100_ABA_MF_285 | 0.041062 | 0.053414 | 0.043207 | 0.054481 | 0.050688 | 0.053074 | 0.050361 | 0.049328 | 0.04563 | 0.045014 | 0.04604
VP37_1_H200_V150_ABA_MF_425 | 0.026513 | 0.032559 | 0.031107 | 0.038608 | 0.035282 | 0.039375 | 0.037324 | 0.041676
VP38_1_H300_V100_ABA_MF_425 | 0.038815 | 0.034831 | 0.04082 | 0.041871 | 0.040537 | 0.043184 | 0.042655 | 0.03889 | 0.035551 | 0.033078 | 0.02959
VP39_1_H300_V150_ABA_MF_425 | 0.024329 | 0.027783 | 0.026529 | 0.030251 | 0.026947 | 0.02932 | 0.028244 | 0.03106
VP4_1_H300_V100_ACF_MF_285 | 0.020616 | 0.028205 | 0.036112 | 0.053728 | 0.056896 | 0.057475 | 0.052073
VP5_1_H200_V100_ACF_MF_285 | 0.031621 | 0.045686 | 0.059 | 0.05161
VP6_1_H100_V100_ACF_MF_285 | 0.062513 | 0.058698 | 0.064713 | 0.071325

## Slide 56: Time and spatial varying thermal properties Heat flow into the workpiece [W] for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 1053.8602 | 1063.7966 | 872.0637 | 853.3864 | 923.4847 | 881.876 | 897.6035 | 680.5211
VP33_1_H300_V150_ACF_MF_285 | 959.6397 | 1000.2656 | 1078.3382 | 1102.2945 | 1035.8593 | 1078.1801 | 986.2507 | 685.0801
VP36_1_H200_V100_ABA_MF_285 | 863.5911 | 810.8866 | 838.5316 | 789.671 | 810.7935 | 782.8267 | 772.7202 | 810.5422 | 810.3416 | 804.0756 | 879.7777
VP37_1_H200_V150_ABA_MF_425 | 1161.2784 | 1160.686 | 1090.4777 | 1055.5866 | 1109.4836 | 1039.3562 | 998.4389 | 971.175
VP38_1_H300_V100_ABA_MF_425 | 1238.1642 | 1220.9686 | 1243.4414 | 1228.9753 | 1128.455 | 1231.8211 | 1098.0303 | 1159.9772 | 1202.5548 | 1068.4184 | 1194.733
VP39_1_H300_V150_ABA_MF_425 | 2004.9905 | 2035.5072 | 2103.5278 | 1954.2461 | 1977.2858 | 1949.6744 | 2059.3084 | 1829.5885
VP4_1_H300_V100_ACF_MF_285 | 860.5709 | 898.9104 | 860.2357 | 763.415 | 778.782 | 723.737 | 745.8603 | 754.4088 | 738.6688 | 492.6575 | 508.9606
VP5_1_H200_V100_ACF_MF_285 | 556.6329 | 680.9456 | 689.2776 | 655.4119 | 658.8899 | 575.0226 | 637.8856 | 548.7624 | 565.3425 | 473.9059 | 447.8599
VP6_1_H100_V100_ACF_MF_285 | 389.355 | 379.015 | 366.5125 | 348.5527 | 358.9992

## Slide 57: Time and spatial varying thermal properties Heat partition into the workpiece for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 0.41163 | 0.41551 | 0.34105 | 0.33332 | 0.3607 | 0.34445 | 0.34876 | 0.26512
VP33_1_H300_V150_ACF_MF_285 | 0.28484 | 0.29818 | 0.32008 | 0.32859 | 0.3078 | 0.32003 | 0.29306 | 0.20335
VP36_1_H200_V100_ABA_MF_285 | 0.44436 | 0.41434 | 0.42891 | 0.40475 | 0.41429 | 0.40083 | 0.39525 | 0.41503 | 0.41616 | 0.41295 | 0.45138
VP37_1_H200_V150_ABA_MF_425 | 0.42266 | 0.42325 | 0.39765 | 0.38492 | 0.4042 | 0.37755 | 0.36157 | 0.35313
VP38_1_H300_V100_ABA_MF_425 | 0.43009 | 0.42314 | 0.43482 | 0.4316 | 0.39713 | 0.43168 | 0.38642 | 0.40823 | 0.41867 | 0.37442 | 0.41869
VP39_1_H300_V150_ABA_MF_425 | 0.45261 | 0.46357 | 0.47486 | 0.44506 | 0.45031 | 0.44589 | 0.46798 | 0.41578
VP4_1_H300_V100_ACF_MF_285 | 0.37292 | 0.39113 | 0.3733 | 0.33082 | 0.33748 | 0.31532 | 0.32496 | 0.32737 | 0.32183 | 0.21547 | 0.2226
VP5_1_H200_V100_ACF_MF_285 | 0.3316 | 0.40682 | 0.41237 | 0.39156 | 0.39419 | 0.34449 | 0.38267 | 0.32831 | 0.33727 | 0.2843 | 0.2656
VP6_1_H100_V100_ACF_MF_285 | 0.4144 | 0.40149 | 0.38948 | 0.37154 | 0.3784

## Slide 58: Time and spatial varying thermal properties Friction coefficient µ for different vc and hsp
Chart: Workpiece position [mm]
| 26,65 | 29,19 | 34,27 | 39,35 | 41,89 | 44,43 | 49,51 | 54,59 | 57,13 | 59,67 | 64,76 | 69,84 | 72,38 | 74,92 | 80,00
VP32_1_H200_V150_ACF_MF_285 | 0.59167 | 0.59167 | 0.59167 | 0.59167 | 0.59167 | 0.59167 | 0.59167 | 0.59167
VP33_1_H300_V150_ACF_MF_285 | 0.48325 | 0.48325 | 0.48325 | 0.48325 | 0.48325 | 0.48325 | 0.48325 | 0.48325
VP36_1_H200_V100_ABA_MF_285 | 0.42608 | 0.42608 | 0.42608 | 0.42608 | 0.42608 | 0.42608 | 0.42608 | 0.42608 | 0.42608 | 0.42608 | 0.42608
VP37_1_H200_V150_ABA_MF_425 | 0.42314 | 0.42314 | 0.42314 | 0.42314 | 0.42314 | 0.42314 | 0.42314 | 0.42314
VP38_1_H300_V100_ABA_MF_425 | 1.052 | 1.052 | 1.052 | 1.052 | 1.052 | 1.052 | 1.052 | 1.052 | 1.052 | 1.052 | 1.052
VP39_1_H300_V150_ABA_MF_425 | 1.0281 | 1.0281 | 1.0281 | 1.0281 | 1.0281 | 1.0281 | 1.0281 | 1.0281
VP4_1_H300_V100_ACF_MF_285 | 0.58779 | 0.58779 | 0.58779 | 0.58779 | 0.58779 | 0.58779 | 0.58779 | 0.58779 | 0.58779 | 0.58779 | 0.58779
VP5_1_H200_V100_ACF_MF_285 | 0.64224 | 0.64224 | 0.64224 | 0.64224 | 0.64224 | 0.64224 | 0.64224 | 0.64224 | 0.64224 | 0.64224 | 0.64224
VP6_1_H100_V100_ACF_MF_285 | 0.73325 | 0.73325 | 0.73325 | 0.73325 | 0.73325 | 0.73325 | 0.73325

## Slide 59: Time and spatial varying thermal properties Heat partition ratios for hsp = 100 µm, vc = 100 m/min (ACF)
Chart: Workpiece position [mm]
| 59,67 | 64,76 | 69,84 | 74,92 | 80,00
VP6_1_H100_V100_ACF_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.4144 | 0.40149 | 0.38948 | 0.37154 | 0.3784
VP6_1_H100_V100_ACF_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.55933 | 0.536 | 0.55182 | 0.56375 | 0.55028
VP6_1_H100_V100_ACF_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.02627 | 0.062513 | 0.058698 | 0.064713 | 0.071325
Tool
Workpiece
Chip

## Slide 60
Time and spatial varying thermal properties Temperature distribution for hsp = 100 µm, vc = 100 m/min (ACF)
Workpiece position : 49,51 mm
Workpiece position : 80 mm
[°C]

## Slide 61: Time and spatial varying thermal properties Heat partition ratios for hsp = 200 µm, vc = 100 m/min (ACF)
Chart: Workpiece position [mm]
| 29,19 | 34,27 | 39,35 | 44,43 | 49,51 | 54,59 | 59,67 | 64,76 | 69,84 | 74,92 | 80,00
VP5_1_H200_V100_ACF_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.3316 | 0.40682 | 0.41237 | 0.39156 | 0.39419 | 0.34449 | 0.38267 | 0.32831 | 0.33727 | 0.2843 | 0.2656
VP5_1_H200_V100_ACF_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.63678 | 0.57561 | 0.57421 | 0.59241 | 0.59017 | 0.60982 | 0.60867 | 0.63828 | 0.63154 | 0.6567 | 0.68279
VP5_1_H200_V100_ACF_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.031621 | 0.017574 | 0.013413 | 0.016028 | 0.015632 | 0.045686 | 0.0086578 | 0.033409 | 0.031188 | 0.059 | 0.05161
Tool
Workpiece
Chip

## Slide 62
Time and spatial varying thermal properties Temperature distribution for hsp = 200 µm, vc = 100 m/min (ACF)
Workpiece position : 34,27 mm
Workpiece position : 80 mm
[°C]

## Slide 63: Time and spatial varying thermal properties Heat partition ratios for hsp = 300 µm, vc = 100 m/min (ACF)
Chart: Workpiece position [mm]
| 29,19 | 34,27 | 39,35 | 44,43 | 49,51 | 54,59 | 59,67 | 64,76 | 69,84 | 74,92 | 80,00
VP4_1_H300_V100_ACF_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.37292 | 0.39113 | 0.3733 | 0.33082 | 0.33748 | 0.31532 | 0.32496 | 0.32737 | 0.32183 | 0.21547 | 0.2226
VP4_1_H300_V100_ACF_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.60646 | 0.58066 | 0.59059 | 0.61545 | 0.6267 | 0.62778 | 0.63623 | 0.63719 | 0.64381 | 0.72706 | 0.72533
VP4_1_H300_V100_ACF_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.020616 | 0.028205 | 0.036112 | 0.053728 | 0.03582 | 0.056896 | 0.03881 | 0.035435 | 0.034355 | 0.057475 | 0.052073
Tool
Workpiece
Chip

## Slide 64
Time and spatial varying thermal properties Temperature distribution for hsp = 300 µm, vc = 100 m/min (ACF)
Workpiece position : 34,27 mm
Workpiece position : 80 mm
[°C]

## Slide 65: Time and spatial varying thermal properties Heat partition ratios for hsp = 200 µm, vc = 150 m/min (ACF)
Chart: Workpiece position [mm]
| 26,65 | 34,27 | 41,89 | 49,51 | 57,13 | 64,76 | 72,38 | 80,00
VP32_1_H200_V150_ACF_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.41163 | 0.41551 | 0.34105 | 0.33332 | 0.3607 | 0.34445 | 0.34876 | 0.26512
VP32_1_H200_V150_ACF_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.56276 | 0.55058 | 0.61628 | 0.62383 | 0.59531 | 0.60384 | 0.59703 | 0.67702
VP32_1_H200_V150_ACF_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.025616 | 0.033907 | 0.04267 | 0.04285 | 0.043982 | 0.051709 | 0.054207 | 0.057863
Workpiece
Tool
Chip

## Slide 66
Time and spatial varying thermal properties Temperature distribution for hsp = 200 µm, vc = 150 m/min (ACF)
Workpiece position : 34,27 mm
Workpiece position : 80 mm
[°C]

## Slide 67: Time and spatial varying thermal properties Heat partition ratios for hsp = 300 µm, vc = 150 m/min (ACF)
Chart: Workpiece position [mm]
| 26,65 | 34,27 | 41,89 | 49,51 | 57,13 | 64,76 | 72,38 | 80,00
VP33_1_H300_V150_ACF_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.28484 | 0.29818 | 0.32008 | 0.32859 | 0.3078 | 0.32003 | 0.29306 | 0.20335
VP33_1_H300_V150_ACF_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.67654 | 0.65923 | 0.63691 | 0.66383 | 0.66652 | 0.64203 | 0.6579 | 0.74249
VP33_1_H300_V150_ACF_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.038618 | 0.042587 | 0.043017 | 0.0075793 | 0.025675 | 0.03794 | 0.049039 | 0.054161
Tool
Workpiece
Chip

## Slide 68
Time and spatial varying thermal properties Temperature distribution for hsp = 300 µm, vc = 150 m/min (ACF)
Workpiece position : 34,27 mm
Workpiece position : 80 mm
[°C]

## Slide 69: Time and spatial varying thermal properties Heat partition ratios for hsp = 200 µm, vc = 100 m/min (ABA)
Chart: Workpiece position [mm]
| 29,19 | 34,27 | 39,35 | 44,43 | 49,51 | 54,59 | 59,67 | 64,76 | 69,84 | 74,92 | 80,00
VP36_1_H200_V100_ABA_MF_285 - Summe von Percent - Heat through workpiece/Total heat | 0.44436 | 0.41434 | 0.42891 | 0.40475 | 0.41429 | 0.40083 | 0.39525 | 0.41503 | 0.41616 | 0.41295 | 0.45138
VP36_1_H200_V100_ABA_MF_285 - Summe von Percent - Heat through chip/Total heat | 0.51458 | 0.53225 | 0.52788 | 0.54077 | 0.53502 | 0.54609 | 0.55439 | 0.53565 | 0.53821 | 0.54204 | 0.50258
VP36_1_H200_V100_ABA_MF_285 - Summe von Percent - Heat inside tool/Total heat | 0.041062 | 0.053414 | 0.043207 | 0.054481 | 0.050688 | 0.053074 | 0.050361 | 0.049328 | 0.04563 | 0.045014 | 0.04604
Tool
Workpiece
Chip

## Slide 70
Time and spatial varying thermal properties Temperature distribution for hsp = 200 µm, vc = 100 m/min (ABA)
Workpiece position : 34,27 mm
Workpiece position : 80 mm
[°C]

## Slide 71: Time and spatial varying thermal properties Heat partition ratios for hsp = 200 µm, vc = 150 m/min (ABA)
Chart: Workpiece position [mm]
| 26,65 | 34,27 | 41,89 | 49,51 | 57,13 | 64,76 | 72,38 | 80,00
VP37_1_H200_V150_ABA_MF_425 - Summe von Percent - Heat through workpiece/Total heat | 0.42266 | 0.42325 | 0.39765 | 0.38492 | 0.4042 | 0.37755 | 0.36157 | 0.35313
VP37_1_H200_V150_ABA_MF_425 - Summe von Percent - Heat through chip/Total heat | 0.55082 | 0.54419 | 0.57125 | 0.57647 | 0.56052 | 0.58308 | 0.60111 | 0.6052
VP37_1_H200_V150_ABA_MF_425 - Summe von Percent - Heat inside tool/Total heat | 0.026513 | 0.032559 | 0.031107 | 0.038608 | 0.035282 | 0.039375 | 0.037324 | 0.041676
Tool
Workpiece
Chip

## Slide 72
Time and spatial varying thermal properties Temperature distribution for hsp = 200 µm, vc = 150 m/min (ABA)
Workpiece position : 34,27 mm
Workpiece position : 80 mm
[°C]

## Slide 73: Time and spatial varying thermal properties Heat partition ratios for hsp = 300 µm, vc = 100 m/min (ABA)
Chart: Workpiece position [mm]
| 29,19 | 34,27 | 39,35 | 44,43 | 49,51 | 54,59 | 59,67 | 64,76 | 69,84 | 74,92 | 80,00
VP38_1_H300_V100_ABA_MF_425 - Summe von Percent - Heat through workpiece/Total heat | 0.43009 | 0.42314 | 0.43482 | 0.4316 | 0.39713 | 0.43168 | 0.38642 | 0.40823 | 0.41867 | 0.37442 | 0.41869
VP38_1_H300_V100_ABA_MF_425 - Summe von Percent - Heat through chip/Total heat | 0.5311 | 0.54203 | 0.52436 | 0.52653 | 0.56233 | 0.52513 | 0.57092 | 0.55288 | 0.54578 | 0.5925 | 0.55172
VP38_1_H300_V100_ABA_MF_425 - Summe von Percent - Heat inside tool/Total heat | 0.038815 | 0.034831 | 0.04082 | 0.041871 | 0.040537 | 0.043184 | 0.042655 | 0.03889 | 0.035551 | 0.033078 | 0.02959
Tool
Workpiece
Chip

## Slide 74
Time and spatial varying thermal properties Temperature distribution for hsp = 300 µm, vc = 100 m/min (ABA)
Workpiece position : 34,27 mm
Workpiece position : 80 mm
[°C]

## Slide 75: Time and spatial varying thermal properties Heat partition ratios for hsp = 300 µm, vc = 150 m/min (ABA)
Chart: Workpiece position [mm]
| 26,65 | 34,27 | 41,89 | 49,51 | 57,13 | 64,76 | 72,38 | 80,00
VP39_1_H300_V150_ABA_MF_425 - Summe von Percent - Heat through workpiece/Total heat | 0.45261 | 0.46357 | 0.47486 | 0.44506 | 0.45031 | 0.44589 | 0.46798 | 0.41578
VP39_1_H300_V150_ABA_MF_425 - Summe von Percent - Heat through chip/Total heat | 0.52306 | 0.50865 | 0.49861 | 0.52469 | 0.52274 | 0.52479 | 0.50377 | 0.55316
VP39_1_H300_V150_ABA_MF_425 - Summe von Percent - Heat inside tool/Total heat | 0.024329 | 0.027783 | 0.026529 | 0.030251 | 0.026947 | 0.02932 | 0.028244 | 0.03106
Tool
Workpiece
Chip

## Slide 76
Time and spatial varying thermal properties Temperature distribution for hsp = 300 µm, vc = 150 m/min (ABA)
Workpiece position : 34,27 mm
Workpiece position : 80 mm
[°C]

## Slide 77: Gliederung
Influence of uncut chip thickness and cutting velocity
4.2
Time and spatial varying thermal properties
4.1
Orthogonal cutting of AISI 4140 (41CrMo4) normalized/quenched and tempered
4
Orthogonal cutting of AISI 1040 (C45 E+N) normalized
3
Post processing of thermal pictures
2
Experimental Setup
1

## Slide 78: Influence of uncut chip thickness and cutting velocity Workpiece position 34 mm (ACF)
Chart: Heat flow (chip) [W]
| 100,00 | 150,00
200,00 | 963.4712 | 1409.6175
300,00 | 1334.4974 | 2211.4647
Chart: Heat flow (tool) [W]
| 100,00 | 150,00
200,00 | 29.4158 | 86.8098
300,00 | 64.8222 | 142.8628
Chart: Heat flow (workpiece) [W]
| 100,00 | 150,00
200,00 | 680.9456 | 1063.7966
300,00 | 898.9104 | 1000.2656
Chart: Heat partition (chip)
| 100,00 | 150,00
200,00 | 0.57561 | 0.55058
300,00 | 0.58066 | 0.65923
Chart: Heat partition (tool)
| 100,00 | 150,00
200,00 | 0.017574 | 0.033907
300,00 | 0.028205 | 0.042587
Chart: Heat partition (workpiece)
| 100,00 | 150,00
200,00 | 0.40682 | 0.41551
300,00 | 0.39113 | 0.29818
ap = 2,8 mm, = 6°, = 3°, = 66 µm, normalized, uncoated, workpiece position: 34mm
hsp [µm]

## Slide 79: Influence of uncut chip thickness and cutting velocity Workpiece position 80 mm (ACF)
Chart: Heat flow (chip) [W]
| 100,00 | 150,00
100,00 | 522.0725
200,00 | 1151.3422 | 1737.7919
300,00 | 1658.4424 | 2501.462
Chart: Heat flow (tool) [W]
| 100,00 | 150,00
100,00 | 67.6686
200,00 | 87.0271 | 148.5252
300,00 | 119.0624 | 182.4697
Chart: Heat flow (workpiece) [W]
| 100,00 | 150,00
100,00 | 358.9992
200,00 | 447.8599 | 680.5211
300,00 | 508.9606 | 685.0801
Chart: Heat partition (chip)
| 100,00 | 150,00
100,00 | 0.55028
200,00 | 0.68279 | 0.67702
300,00 | 0.72533 | 0.74249
Chart: Heat partition (tool)
| 100,00 | 150,00
100,00 | 0.071325
200,00 | 0.05161 | 0.057863
300,00 | 0.052073 | 0.054161
Chart: Heat partition (workpiece)
| 100,00 | 150,00
100,00 | 0.3784
200,00 | 0.2656 | 0.26512
300,00 | 0.2226 | 0.20335
ap = 2,8 mm, = 6°, = 3°, = 66 µm, normalized, uncoated, workpiece position: 80 mm
hsp [µm]

## Slide 80: Influence of uncut chip thickness and cutting velocity Workpiece position 34 mm (ABA)
Chart: Heat partition (workpiece)
| 100,00 | 150,00
200,00 | 0.41434 | 0.42325
300,00 | 0.42314 | 0.46357
Chart: Heat flow (chip) [W]
| 100,00 | 150,00
200,00 | 1041.6505 | 1492.3547
300,00 | 1564.0366 | 2233.4372
Chart: Heat flow (tool) [W]
| 100,00 | 150,00
200,00 | 104.5351 | 89.2887
300,00 | 100.5062 | 121.9937
Chart: Heat flow (workpiece) [W]
| 100,00 | 150,00
200,00 | 810.8866 | 1160.686
300,00 | 1220.9686 | 2035.5072
Chart: Heat partition (tool)
| 100,00 | 150,00
200,00 | 0.053414 | 0.032559
300,00 | 0.034831 | 0.027783
Chart: Heat partition (chip)
| 100,00 | 150,00
200,00 | 0.53225 | 0.54419
300,00 | 0.54203 | 0.50865
ap = 2,8 mm, = 6°, = 3°, = 66 µm, tempered, uncoated, workpiece position: 34 mm
hsp [µm]

## Slide 81: Influence of uncut chip thickness and cutting velocity Workpiece position 80 mm (ABA)
Chart: Heat partition (workpiece)
| 100,00 | 150,00
200,00 | 0.45138 | 0.35313
300,00 | 0.41869 | 0.41578
Chart: Heat flow (chip) [W]
| 100,00 | 150,00
200,00 | 979.5612 | 1664.4079
300,00 | 1574.3611 | 2434.1194
Chart: Heat flow (tool) [W]
| 100,00 | 150,00
200,00 | 89.7364 | 114.6173
300,00 | 84.4351 | 136.6738
Chart: Heat flow (workpiece) [W]
| 100,00 | 150,00
200,00 | 879.7777 | 971.175
300,00 | 1194.733 | 1829.5885
Chart: Heat partition (tool)
| 100,00 | 150,00
200,00 | 0.04604 | 0.041676
300,00 | 0.02959 | 0.03106
Chart: Heat partition (chip)
| 100,00 | 150,00
200,00 | 0.50258 | 0.6052
300,00 | 0.55172 | 0.55316
ap = 2,8 mm, = 6°, = 3°, = 66 µm, tempered, uncoated, workpiece position: 80 mm
hsp [µm]